## Slide 1
FY2015’s 3rd, CREST Workshop
Norio Takenaka1,2
Graduate School of Information Science, Nagoya University1,
Elements Strategy Initiative for Catalysts and Batteries (ESICB), Kyoto University2
Exploring Transport Pathway of Sodium Ion in Solid Electrolyte Interphase Using Targeted Molecular Dynamics Method
Tue. Jun. 30th

## Slide 2: Background of Present Research
2
Among several processes of ion and electron transport, the lithium (or sodium) ion transfer at an anode/electrolyte interface is an essential process of the charge-discharge reaction of lithium (or sodium) ion batteries.
Resistances of ion transfer
Rct: charge transfer resistance from SEI film to anode
RSEI: resistance of ion transfer in SEI film
Rbulk: resistance of ion transfer in bulk electrolyte
Battery resistance is typically the sum of the bulk electrolyte resistance (Rbulk), resistance of the SEI (RSEI), and an ion transfer resistance (Rct).
Schematic illustration

## Slide 3: Previous Studies on Ion Transfer ①
resistance of SEI (RSEI) was quite small according to impedance spectroscopy,
(2) desolvation energy (< 12 kcal/mol) was similar to the activation barrier.
According to experimental studies, an activation barrier of the Li+ transfer from the electrolyte to graphite was found to be 12 ~ 24 kcal/mol.
Abe and Ogumi et al. concluded that the desolvation of Li+ is a rate-determining step of the interfacial transfer at graphite [1,2] because
[1] Abe and Ogumi et al., J. Electrochem. Soc., 151(8), A1120 (2004).
[2] Abe and Ogumi el al., Langumir, 25(21), 12766 (2009).
However, its kinetics is influenced by the composition of SEI film [2].
Such a microscopic origin was not found.

## Slide 4: Previous Studies on Ion Transfer ②
To directly estimate an activation barrier of RSEI, Xu et al. have investigated the Li+ transfer in the SEI film by using both experiment and MD simulation, considering a simple system which includes only Li2EDC molecules because they were well-known to be the main component in the SEI film [3].
Calculation model for MD simulation [3]
Li2EDC
Ion conductivity [3]
[3] Xu et al., J. Phys. Chem. C, 117, 7433 (2013).
The activation barrier of RSEI was estimated to be 15 kcal/mol, which is similar to that of the Li+ transfer from the electrolyte to graphite (12 ~ 24 kcal/mol).
The Li+ transfer in the SEI film should be a rate-determining step.

## Slide 5: Purpose of Present Research
According to the previous studies in lithium-ion batteries (LIB), there are two possibilities of the rate-determining step on the ion transfer, i.e., (1) desolvation of Li+ and (2) Li+ transfer in the SEI film.
However, these studies have two weak points.
① It is difficult to assign RSEI by using impedance spectroscopy.
② Simple model consisting of only Li2EDC is different from real SEI film.
On the other hand, in ESICB project, it is expected to investigate Na+ transfer in sodium-ion batteries (NIB) to develop the high-performance NIB. Previously, we could get the realistic model of SEI film using hybrid MC/MD reaction method [4,5].
[4] NT et al., J. Phys. Chem. C, 118(20), 10874 (2014); [5] NT et al., J. Phys. Chem. C, in revision.
Therefore, I investigated the Na+ transfer in the SEI film obtained by the hybrid MC/MD reaction method [5]. First, I searched for a migration pathway into the anode surface through the SEI film. Next, I calculated a free energy profile along a migration pathway to compare the activation barrier with the previous experimental and theoretical values [1-3].

## Slide 6: Implementation of Targeted MD Method
To search for the migration pathways of Na+ inside the SEI film, I implemented targeted molecular dynamics (TMD) method [6] into AMBER program.
[6] J. Schlitter et al., Mol. Simul., 10(2), 291-309 (1993).
: force constant
: current ion position on z-axis
: targeted position on z-axis
In the method, to pull the selected ion into the targeted position, the additional force is applied to the selected ion during the MD simulation.
On the other hand, to roughly know the energetic information along migration pathway, I calculated the interaction energies between selected ion and other species (e.g., electrolyte solution, SEI film).

## Slide 7: Model System
SEI film
(a) Side View (SEI film, surface view; Na+ and PF6-, van der Waals view; PC and Gas, stick view)
(b) Front view of SEI film from the side of anode
(0 < z < 20 Å)
Anode
・ For this purpose, I employed the system including NaPF6-PC electrolyte solution and SEI film (This was obtained by a hybrid MC/MD reaction simulation.)
Species in SEI film

## Slide 8: Procedure of TMD Simulations
・ In the simulation, I first selected one Na+ (purple), and pulled it into the anode surface (target position) by using TMD method.
Selected Na+
Additional force
・In the TMD method, the force constant was set to 1.0 kcal/molÅ2.

## Slide 9: Change in the Positon of a Selected Na+
・ During the TMD simulation, a selected Na+ was close to the anode surface (z = 0 Å) from the initial positon (z = 48 Å) inside the SEI film.
Time [ps]
z [Å]

## Slide 10: Change in the Interaction Energy
Time [ps]
Interaction energy [kcal/mol]
・ According to the interaction energy between a selected Na+ and other species, there is a large barrier until a selected Na+ moves into the anode surface.
Cut-off distance: 17 Å

## Slide 11: Relation between the Positon and Interaction Energy
Time [ps]
z [Å]
Time [ps]
Interaction energy [kcal/mol]
(a) Position of a selected Na+
(b) Interaction energy
・ The barrier was presented in the interface region of SEI film (0 < z < 20 Å). In this case, a selected Na+ was found to pass through a cavity in this region.
0 < z < 20 Å
cavity

## Slide 12: Free Energy Calculation on Migration Pathway
To obtain the free energy profiles along the migration pathways of Na+ obtained by TMD method, I employed thermodynamic integration (TI) method.
In the TI method, when a selected Na+ moves from 0 to a along z axis, the free energy change ΔG(a) is obtained as follows.
: Average force in z direction of a selected Na+
fixed at z = a
: interval
Difference formula
In the present analysis, I have fixed only z coordinate, meaning that a selected Na+ can move on x-y plane in each zk (Δzk = 1 Å). Additionally, I have estimated the free energy using 1 ns MD sampling (100 ps relaxation) along the calculated migration pathway of a selected Na+.

## Slide 13: Free Energy Profile and Mass Density Distribution
5.3 kcal/mol
z [Å]
Free energy [kcal/mol]
z [Å]
Mass density [g/cm3]
(a) Free energy profile of a selected Na+
(b) Mass densities of reaction products in the present SEI film
・ The free energy was stable as a selected Na+ moves into the anode surface because the electrostatic interactions should be stronger inside the SEI film.
Initial position
・ There was a free energy barrier of 5.3 kcal/mol near the anode surface. This peak position corresponds to that in the mass density of the present SEI film.
NaPC
Na2DMBDC
Na2CO3

## Slide 14: Front Views of All Samples (N = 10)
Sample.1
(Present)
Sample.2
Sample.3
Sample.4
Sample.5
Sample.6
Sample.7
Sample.8
Sample.9
Sample.10
・ In all samples, it was found that there are some cavities where a Na+ can pass through. (By rotating these structures, such cavities were clearly found.)
Previously, we obtained 10 SEI films by using 10 different initial structures.

## Slide 15: Summary and Future Work
・Using TMD method, I can obtain a migration pathway of Na+ into the anode surface in the SEI film obtained by the hybrid MC/MD reaction simulation.
・In the present study, we have investigated the transport properties of Na+ in the SEI film of NIB by using both TMD and TI methods.
・To confirm this prediction, I will estimate the free energy barriers using all samples (N = 10), and compare their average value with the experimental one.
・It was found that there is a free energy barrier of 5.3 kcal/mol for a migration of Na+ into the anode surface.
・The calculated free energy barrier was smaller than the experimental value (12~24 kcal/mol) and previous calculated one using the simple model including only Li2EDC (15 kcal/mol). Thus, it is predicted that the desolvation is a rate-determining step of Na+ transfer from the electrolyte to anode.

## Slide 16: Thank you for your attention