## Slide 1: CREST Workshop Uppula Purushotham
Mechanistic Study of DiFluoro Ethylene Carbonate as Electrolyte Additive for Rechargeable Na-Ion Batteries: A Hybrid MC/MD Simulation Study

## Slide 2: Background of Present Study
Based on recent experimental study by Prof. Komaba, fluoroethylene carbonate (FEC) was the only an effective additive in the Na-ion battery among the FEC, difluoroethylene carbonate (DFEC), vinylene carbonate (VC) and ethylene sulfite (ES).
S. Komaba et al., ACS Appl. Mater. Interfaces, 3, 4165 (2011).
FEC-free
FEC-added (10 vol%)
Figure. Reversible capacity versus cycle number plots in Na-ion battery

In the present study we would like to investigate the origin of mechanism of 2SEI film formation in DFEC additive PC electrolyte Na-ion battery.

## Slide 3
Chart: 
| R1 | IN-2 | TS-3 | IN-4 | IN-5 | TS-6 | IN-7 | IN-8
DFEC | 0 | -87.092 | -71.967 | -104.074 | -111.347 | -109.766 | -129.214 | -159.686
 | 0 | -53.098 | -39.366 | -71.173 | -42.287 | -41.498 | -62.405 | -101.582
FEC | 0 | -88.41 | -81.36 | -90.314 | -83.784 | -87.172 | -67.658 | -61.387 | -100.742
 | -2.51e-06 | -53.8217 | -47.2277 | -55.1466 | -49.3447 | -52.8276 | -13.4851 | -8.7021 | -53.9581
PC | 0 | -84.678 | -72.982 | -99.566 | -133.743
 | -0.0002259 | -46.8474 | -35.4417 | -61.5758 | -57.3426
Relative energy in kcal/mol
DFEC-TS
FEC-TS
DFEC-Product
PC-TS
FEC-Product
PC-Product
Reduction Mechanism of PC, FEC and DFEC
Activation energy (kcal/mol):
6.594 (FEC) < 11.405 (PC) < 13.732 (DFEC)
Lower activation energy barrier facilitates the faster decomposition of FEC than DFEC which results into the formation of primary SEI film. In DFEC added system mainly PC decomposed products form SEI film.

## Slide 4
Simulation Model and Reaction Scheme
Carbon anode
NaPF6 electrolyte with DFEC
y
z
x
+ e-, + Na+
+
+ NaPC
Na2CO3
+ e-, + Na+
PC
NaPC
C3H6
(CH3CHCH2OCO2Na)2
Na2DMBDC
+
+
PF3
3NaF
+ 2e-, + 3Na+
+
PF6
DFEC
+ 2e-, + Na+
Na2CO3
+
C2H2F2
Based on quantum chemical results DFEC is less reactive than PC with its higher activation energy. In the real situation more intact DFEC molecules present in the electrolyte during SEI film formation.
Thus, to evaluate the intact DFEC effect we have carried out the MC/MD simulations where DFEC is non-reactive.
Along with this we have also included the dissociation of DFEC after PC reduction.
0 to 2000 MC/MD cycles
PC – Reactive
DFEC – Non-reactive
PC – Reactive
DFEC – Reactive
2001 to 3000 MC/MD cycles
1.1M NaPF6 PC electrolyte
(with 10 vol% DFEC)
PC: 850
Na+: 87
PF6-: 85
DFEC: 115

## Slide 5
SEI Film Formation Processes
C4H7O3Na
C8H12O6Na2
Na2CO3
NaF
Species
C2H2F2
(a) 100 cycle
(b) 500 cycle
(c) 1500 cycle
FEC-added electrolyte
Addition of FEC and DFEC additives decreased the width of SEI film.
DFEC-added electrolyte
(a) 100 cycle
(b) 2001 cycle
(c) 3000 cycle
(a) 100 cycle
(b) 500 cycle
(c) 1500 cycle
PC electrolyte

## Slide 6
Figure. Change in the concentration of the reductive products with the MC/MD cycles.
Change in Number Densities of Reaction Products
Chart: 
| 0 | 40 | 80 | 120 | 160 | 200 | 240 | 280 | 320 | 360 | 400 | 440 | 480 | 520 | 560 | 600 | 640 | 680 | 720 | 760 | 800 | 840 | 880 | 920 | 960 | 1000 | 1040 | 1080 | 1120 | 1160 | 1200 | 1240 | 1280 | 1320 | 1360 | 1400 | 1440 | 1480 | 1520 | 1560 | 1600 | 1640 | 1680 | 1720 | 1760 | 1800 | 1840 | 1880 | 1920 | 1960 | 2000
 | 0 | 0.86442 | 1.6733 | 2.4188 | 3.0453 | 3.3387 | 3.7749 | 4.1001 | 4.2983 | 4.2666 | 4.2666 | 4.2428 | 4.1159 | 3.8939 | 3.537 | 2.7836 | 2.4347 | 2.1333 | 1.7923 | 1.5861 | 1.3958 | 1.3085 | 1.2372 | 1.2292 | 1.1975 | 1.1578 | 1.1261 | 1.0785 | 1.0627 | 1.0706 | 1.0627 | 1.0627 | 1.0548 | 1.0627 | 1.0785 | 1.0785 | 1.0706 | 0.99924 | 0.99924 | 0.99924 | 1.0072 | 1.0072 | 0.99131 | 0.99131 | 0.98338 | 0.95166 | 0.95166 | 0.95166 | 0.95959 | 0.94373 | 0.92786
 | 0 | 0 | 0.031722 | 0.063444 | 0.15068 | 0.2855 | 0.44411 | 0.61858 | 0.81684 | 1.0785 | 1.3244 | 1.5226 | 1.7923 | 2.0699 | 2.4109 | 2.8232 | 3.0691 | 3.2118 | 3.3863 | 3.5132 | 3.6163 | 3.6718 | 3.7115 | 3.7273 | 3.7352 | 3.759 | 3.767 | 3.7828 | 3.7987 | 3.7987 | 3.7987 | 3.7987 | 3.8066 | 3.8066 | 3.8066 | 3.8066 | 3.8146 | 3.8463 | 3.8463 | 3.8463 | 3.8463 | 3.8463 | 3.8542 | 3.8542 | 3.8621 | 3.878 | 3.878 | 3.8859 | 3.8859 | 3.8939 | 3.9018
 | 9.3579 | 9.2152 | 9.0487 | 8.9694 | 8.7473 | 8.6997 | 8.549 | 8.3984 | 8.2873 | 8.1684 | 8.0494 | 7.9067 | 7.7243 | 7.5736 | 7.4626 | 7.3753 | 7.3278 | 7.304 | 7.2643 | 7.2167 | 7.2167 | 7.2167 | 7.1771 | 7.1533 | 7.1453 | 7.1374 | 7.1374 | 7.1295 | 7.1295 | 7.1295 | 7.1216 | 7.1216 | 7.1136 | 7.1136 | 7.1136 | 7.1136 | 7.1136 | 7.1057 | 7.1057 | 7.1057 | 7.0978 | 7.0978 | 7.0978 | 7.0898 | 7.0898 | 7.0898 | 7.0898 | 7.0898 | 7.0898 | 7.0898 | 7.0898
 | 0 | 0.095166 | 0.34894 | 0.64237 | 0.80098 | 1.1023 | 1.2847 | 1.4751 | 1.7209 | 1.943 | 2.1888 | 2.4743 | 2.7122 | 2.9422 | 3.196 | 3.4339 | 3.5291 | 3.7115 | 3.7987 | 3.8304 | 3.8701 | 3.9018 | 3.9097 | 3.9097 | 3.9335 | 3.9494 | 3.9652 | 3.989 | 3.989 | 3.997 | 4.0207 | 4.0287 | 4.0366 | 4.0366 | 4.0366 | 4.0366 | 4.0366 | 4.0445 | 4.0445 | 4.0604 | 4.0604 | 4.0604 | 4.0604 | 4.0604 | 4.0604 | 4.0604 | 4.0604 | 4.0604 | 4.0763 | 4.0763 | 4.0763
 | 0 | 0.13482 | 0.31722 | 0.45997 | 0.6503 | 0.76926 | 0.89614 | 1.0072 | 1.1341 | 1.253 | 1.4116 | 1.5226 | 1.6654 | 1.8319 | 1.9668 | 2.0461 | 2.0857 | 2.1254 | 2.165 | 2.1967 | 2.1967 | 2.1967 | 2.2126 | 2.2364 | 2.2443 | 2.2523 | 2.2523 | 2.2602 | 2.2602 | 2.2602 | 2.2681 | 2.2681 | 2.276 | 2.276 | 2.276 | 2.276 | 2.276 | 2.284 | 2.284 | 2.284 | 2.2919 | 2.2919 | 2.2919 | 2.2998 | 2.2998 | 2.2998 | 2.2998 | 2.2998 | 2.2998 | 2.2998 | 2.2998
 | 67.409 | 66.4494 | 65.3232 | 64.2209 | 63.2613 | 62.3969 | 61.4611 | 60.5967 | 59.7561 | 59.0423 | 58.3048 | 57.6466 | 56.9963 | 56.4332 | 55.8543 | 55.545 | 55.3071 | 55.1405 | 55.0454 | 54.9661 | 54.9105 | 54.855 | 54.8392 | 54.8154 | 54.8074 | 54.7837 | 54.7837 | 54.7757 | 54.7599 | 54.744 | 54.7281 | 54.7202 | 54.7044 | 54.6964 | 54.6806 | 54.6806 | 54.6726 | 54.6726 | 54.6726 | 54.6568 | 54.6488 | 54.6488 | 54.6488 | 54.6488 | 54.6409 | 54.6409 | 54.6409 | 54.625 | 54.6013 | 54.6013 | 54.6013
PC
FEC
MC/MD cycles
[10-2Å-2]
NaPC
Na2DMBDC
Na2CO3
NaF
29
162
(b) FEC added
The number density of inorganic salts (CO3-2) are increased in the DFEC added system, where the number density of NaF molecules are increased in the FEC-added system.
Decomposition of more FEC molecules (29) than DFEC molecules (14) reveals the significant contribution of FEC decomposition products in the SEI film formation.
Chart: 
| 20 | 60 | 100 | 140 | 180 | 220 | 260 | 300 | 340 | 380 | 420 | 460 | 500 | 540 | 580 | 620 | 660 | 700 | 740 | 780 | 820 | 860 | 900 | 940 | 980 | 1020 | 1060 | 1100 | 1140 | 1180 | 1220 | 1260 | 1300 | 1340 | 1380 | 1420 | 1460 | 1500 | 1540 | 1580 | 1620 | 1660 | 1700 | 1740 | 1780 | 1820 | 1860 | 1900 | 1940 | 1980
Na2DMBDC | 0.0079305 | 0.039652 | 0.11896 | 0.1824 | 0.38066 | 0.53134 | 0.75339 | 1.0627 | 1.3561 | 1.6971 | 1.9905 | 2.3316 | 2.7122 | 2.9819 | 3.1563 | 3.2356 | 3.307 | 3.3308 | 3.4022 | 3.4418 | 3.4577 | 3.4656 | 3.5053 | 3.5211 | 3.5291 | 3.5528 | 3.5528 | 3.5608 | 3.5766 | 3.5766 | 3.5846 | 3.5846 | 3.5846 | 3.5925 | 3.6163 | 3.6163 | 3.6242 | 3.6242 | 3.6322 | 3.6322 | 3.6322 | 3.6322 | 3.648 | 3.648 | 3.6559 | 3.6559 | 3.6639 | 3.6718 | 3.6718 | 3.6797
Na2CO3 | 0.079305 | 0.30929 | 0.53927 | 0.66616 | 0.95959 | 1.1499 | 1.4354 | 1.7209 | 1.9271 | 2.1888 | 2.5219 | 2.855 | 3.1801 | 3.3625 | 3.4656 | 3.5053 | 3.5449 | 3.5687 | 3.6004 | 3.6163 | 3.6163 | 3.648 | 3.6559 | 3.6718 | 3.6797 | 3.6877 | 3.6877 | 3.6956 | 3.7035 | 3.7115 | 3.7115 | 3.7115 | 3.7115 | 3.7115 | 3.7194 | 3.7194 | 3.7273 | 3.7432 | 3.7432 | 3.7432 | 3.7432 | 3.7511 | 3.7511 | 3.759 | 3.759 | 3.759 | 3.759 | 3.759 | 3.7749 | 3.7749
NaPC | 0.99131 | 1.9747 | 2.7281 | 3.6084 | 3.8542 | 4.3459 | 4.4966 | 4.3459 | 4.2587 | 4.0604 | 3.8225 | 3.3625 | 2.6488 | 2.1254 | 1.8081 | 1.6813 | 1.5464 | 1.5306 | 1.3878 | 1.3402 | 1.3244 | 1.2927 | 1.2213 | 1.1896 | 1.1658 | 1.1261 | 1.1261 | 1.1103 | 1.0706 | 1.0627 | 1.0548 | 1.0548 | 1.0548 | 1.0468 | 0.99131 | 0.99131 | 0.97545 | 0.96752 | 0.95166 | 0.95166 | 0.95166 | 0.94373 | 0.912 | 0.912 | 0.89614 | 0.89614 | 0.88028 | 0.87235 | 0.87235 | 0.85649
NaF | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
DF1 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12 | 9.12
PC | 66.3225 | 65.0457 | 63.9037 | 62.7696 | 61.8338 | 60.8505 | 59.9702 | 59.2168 | 58.511 | 57.7655 | 57.0835 | 56.5284 | 56.1556 | 55.9574 | 55.8225 | 55.7512 | 55.7036 | 55.6481 | 55.6164 | 55.5688 | 55.5529 | 55.5371 | 55.5212 | 55.5053 | 55.5053 | 55.4895 | 55.4895 | 55.4815 | 55.4815 | 55.4815 | 55.4736 | 55.4736 | 55.4736 | 55.4657 | 55.4657 | 55.4657 | 55.4577 | 55.4498 | 55.4498 | 55.4498 | 55.4498 | 55.4498 | 55.4498 | 55.4419 | 55.4419 | 55.4419 | 55.4419 | 55.434 | 55.4181 | 55.4181
(c) DFEC (Non-reactive) added
[10-2Å-2]
MC/MD cycles
155
Chart: 
(c) DFEC (Reactive) added
MC/MD cycles
14

## Slide 7
Mass Density Distributions of Reaction Products
Figure. Mass density distribution of the reductive products in the SEI films.
z [Å]
(a) PC
(c) DFEC added
The width of SEI film in FEC and DFEC added systems is almost similar.
With the addition of additive the thickness of SEI film was found to be reduced by 32%.
In DFEC added system inorganic salts are increased compare to FEC and PC systems.
z [Å]
(b) FEC added
z [Å]
Chart: 
Chart: 
| 1 | 3 | 5 | 7 | 9 | 11 | 13 | 15 | 17 | 19 | 21 | 23 | 25 | 27 | 29 | 31 | 33 | 35 | 37 | 39 | 41 | 43 | 45 | 47 | 49 | 51 | 53 | 55 | 57 | 59 | 61 | 63 | 65 | 67 | 69 | 71 | 73 | 75 | 77 | 79 | 81
PC3 | 0 | 0 | 0 | 1.6532e-06 | 0.027901 | 0.079242 | 0.093667 | 0.052185 | 0.046048 | 0.056385 | 0.088984 | 0.10743 | 0.0454 | 0.02001 | 0.01537 | 0.031731 | 0.016797 | 0.019055 | 0.01067 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC4 | 0 | 0 | 0.036744 | 0.11653 | 0.35932 | 0.51654 | 0.84662 | 0.78629 | 0.98455 | 0.95544 | 0.9393 | 0.82957 | 0.68242 | 0.32006 | 0.25947 | 0.20503 | 0.11094 | 0.12839 | 0.073102 | 0.010795 | 0.0057714 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
N2C | 0 | 0.0011462 | 0.12169 | 0.36733 | 0.74922 | 0.82944 | 0.7709 | 0.65102 | 0.42104 | 0.35102 | 0.12789 | 0.085065 | 0.027888 | 0.020017 | 0.0009329 | 0.0089506 | 0.0189 | 0.00012238 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
F | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
TDF | 0 | 0.011741 | 0.30258 | 0.099303 | 0.12091 | 0.048151 | 0.022727 | 0.010319 | 0.0030742 | 0.0072732 | 0.00019508 | 0.00019508 | 0.00019508 | 0.00019508 | 0.00019508 | 0.00019508 | 0.00019508 | 0.00019508 | 0.00019508 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
NaPC
Na2DMBDC
Na2CO3
NaF
39 Å
[gcm-3]
NaPC
Na2DMBDC
Na2CO3
NaF
[gcm-3]
39 Å
Chart: 
[gcm-3]
NaPC
Na2DMBDC
Na2CO3
NaF
57 Å

## Slide 8
Comparison of Smoothness of SEI Films
(b) DFEC added
(a) FEC added
This reveals that in the FEC-added electrolyte, the surface structure of SEI film in contact with the electrolyte is smoother than DFEC-added SEI film.

## Slide 9
System | STDV(Å) | Distance(Å)
DFEC | 10.862 | 31.010
FEC | 10.346 | 32.279
PC | 11.652 | 39.576
Roughness of SEI Film
Order of Roughness: PC > DFEC > FEC
The roughness is estimated through the standard deviation (STDV) of measured width at various parts (15X15 grid) of the SEI film.
Figure. A rough surface of arbitrary profile
Distance
T. Adams et.al. Int. J. Mech. Eng. Mechat. 1, 66 (2012)

## Slide 10
Systems | FAV | Total Grid Points
PC | 0.050 (0.018) | 816519
FEC added PC | 0.042 (0.019) | 833351
DFEC added PC | 0.064 (0.017) | 812374
To calculate the fractional accessible free volume (FAV), we have chosen the region where the density of three SEI films is high.
z [Å]
[gcm-3]
Chart: 
| 1 | 3 | 5 | 7 | 9 | 11 | 13 | 15 | 17 | 19 | 21 | 23 | 25 | 27 | 29 | 31 | 33 | 35 | 37 | 39 | 41 | 43 | 45 | 47 | 49 | 51 | 53 | 55 | 57 | 59 | 61 | 63 | 65 | 67 | 69 | 71 | 73 | 75 | 77 | 79 | 81 | 83 | 85 | 87
 | 0 | 0 | 0.02308 | 0.32041 | 1.0831 | 1.6942 | 1.6143 | 1.498 | 1.4521 | 1.385 | 1.1014 | 0.9407 | 0.58178 | 0.62182 | 0.27576 | 0.21058 | 0.099884 | 0.093299 | 0.072242 | 0.058256 | 0.020872 | 5.3729e-05 | 0 | 3.2238e-05 | 3.2238e-05 | 3.2238e-05 | 3.2238e-05 | 3.2238e-05 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
SEI_DFEC | 0 | 0.0011462 | 0.15844 | 0.48387 | 1.1364 | 1.4252 | 1.7112 | 1.4895 | 1.4516 | 1.3628 | 1.1562 | 1.0221 | 0.7557 | 0.36008 | 0.27577 | 0.24571 | 0.14664 | 0.14757 | 0.083772 | 0.010795 | 0.0057714 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
SEI-FEC | 0 | 0.0035769 | 0.059195 | 0.43849 | 0.87829 | 1.5049 | 1.3652 | 1.5388 | 1.3506 | 1.297 | 1.2421 | 1.0485 | 0.87194 | 0.64375 | 0.38442 | 0.31158 | 0.22922 | 0.12767 | 0.058521 | 0.049942 | 0.0087529 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
SEI-PC | 0 | 0 | 0.074176 | 0.15351 | 0.75863 | 1.3087 | 1.5302 | 1.4956 | 1.4775 | 1.4218 | 1.3104 | 1.167 | 0.83462 | 0.78549 | 0.71385 | 0.7215 | 0.57453 | 0.66139 | 0.53686 | 0.41182 | 0.32662 | 0.32867 | 0.23042 | 0.21523 | 0.22459 | 0.1731 | 0.12182 | 0.074319 | 0.084124 | 0.030799 | 0.010258 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Figure. Mass density distribution of various SEI films.
Table: The FAV of different systems along with standard deviation in parenthesis.
Cavity Size
18Å

## Slide 11
Coordination of Inorganic Molecules with Additives
Table: The averaged coordination number of inorganic molecules around additives with in 3.4Å distance of SEI film (width 30Å) formed after addition of FEC and DFEC additives.
Systems | Coordination Number
FEC added PC | 0.35
DFEC added PC | 0.46
The clustering of inorganic molecules around intact DFEC molecules is increased in the DFEC added PC electrolyte system.
This clustering results to formation of larger cavities.

## Slide 12
Systems | Number of Electrolyte molecules
PC | 34
FEC added PC | 33 (27 PC + 6 FEC)
DFEC added PC | 45 (36 PC + 9 DFEC)
We have calculated the number of electrolyte molecules present in the SEI film. For this purpose we have chosen the SEI region where the density of three SEI films are more.
More number of intact electrolyte molecules present in DFEC added system than PC and FEC added systems.
It is clear that presence of more intact molecules in the SEI film is responsible for the large cavities in the DFEC added system.
Electrolyte Molecules Present in SEI film

## Slide 13
Role of DFEC Residues in the SEI film Formation
100 MC/MD cycles
500 MC/MD cycles
NaPC
CO3-2
DFEC
Na+
NaPC
DFEC
CO3-2
Na2DMBDC
Intact DFEC molecules coordinate with reaction products during the SEI film formation.
DFEC also enhance the clustering of inorganic molecules which can be responsible for larger cavity sizes.

## Slide 14
Conclusions
To gauge the effect of DFEC on the formation of SEI film, we have performed the MC/MD simulations on DFEC added PC electrolyte system which resembles real situation where both the effects such as effect of intact DFEC molecules and DFEC dissociation after the PC SEI film formation were included.
DFEC-added PC electrolyte system resulted roughened surface structure of SEI film in contact with the electrolyte compare to the FEC added system.
Decomposition of more FEC molecules during the SEI film formation reveals the higher contribution of FEC molecules in the SEI film formation than DFEC molecules.
The clustering of inorganic molecules around intact DFEC molecules is more favorable in the DFEC added PC electrolyte system. This clustering reduce the aggregation between inorganic and organic products in the SEI film formation.
Intact electrolyte molecules present in the SEI film are responsible for large cavities in DFEC added system.
Finally, the inefficient aggregation of reaction products in the DFEC-added system results roughened surface structure and intact electrolyte molecules in SEI film and clustering of inorganic products with DFEC molecules results larger cavities in the SEI film.