## Slide 1
FY2015’s 9th, CREST Workshop
Norio Takenaka1,2
Graduate School of Information Science, Nagoya University1,
Elements Strategy Initiative for Catalysts and Batteries (ESICB), Kyoto University2
SEI Film Formation Simulation
in Na-Ion Batteries with Highly Concentrated Electrolyte
Fri. Mar. 18th

## Slide 2
[1] Y. Yamada et al., J. Am. Chem. Soc., 136, 5039 (2014).
[2] Y. Yamada et al., J. Electrochem. Soc., 162, A2406 (2015).
Superconcentration solutions are emerging as a new class of liquid electrolytes with various unusual functionalities for advanced battery applications [1,2].
It was reported that a highly concentrated acetonitrile (AN) solutions (> 4 M) shows the enhanced reductive stability in lithium-ion batteries.
Stability of Highly Concentrated Electrolyte
Fig. 1 Reactivity of Li metal and LiTFSA/AN solutions at 1.0 M and 4.2 M at room temperature.
Fig. 2 Reversible capacity
good
bad
Notes: First, I talk about the background of this study. Superconcentration solutions are emerging as a new class of liquid electrolytes because they have various unusual functionalities for advanced battery applications. As one of example, Figure 1 shows the reactivity of lithium metal and LiTFSA/AN solutions at 1 M and 4.2 M at room temperature. In this experiment, the authors put the lithium metal into the electrolyte, and observed the color change. As you can see, after one week, 1 M electrolyte shows the yellow color, showing the electrolyte continue to be decomposed on the lithium metal. On the other hand, at 4.2 M, there is no color change because the stable SEI film was formed on the lithium metal. And, Figure 2 shows the reversible capacities by using 4.5 M LiFSA/AN electrolyte and 1 M LiPF6/EC:EMC electrolyte. As a result, in the high concentration electrolyte, the capacity change was stable, so the irreversible capacity drastically decreased.

## Slide 3
Previous DFT-MD Study
Fig. 3. Supercells used in DFT MD simulations at (a) 4.2 M and (b) 0.4 M TFSA/AN electrolyte.
Fig. 4. Projected density of states (PDOS) at (a) 4.2 M and (b) 0.4 M.
(a)
(b)
DFT-MD study shows the TFSA anions sacrificially accept the reductive electron at high concentration condition, which is ascribe to the shift of electron affinity of anions [1,3].
This is attributed to the strong interaction between the TFSA anion and Li cation, as a consequence of high concentration concept.
[3] K. Sodeyama et al., J. Phys. Chem. C, 118, 14091 (2014).
Notes: To investigate the reduction mechanism of electrolytes at high concentration condition, Sodeyama and Tateyama executed the DFT-MD simulations. They performed the simulations by using 4.2 M and 0.4 M TFSA/AN electrolyte like this. And, Figure 4 shows the projected density of states at 4.2 M and 0.4 M. As a result, it was found that the TFSA anions sacrificially accept the reductive electron at high concentration condition, which is ascribe to the shift of electron affinity of anions shown in Figure 4a. The authors said this is attributed to the strong interaction between the TFSA anion and Li cation at the high concentration condition.

## Slide 4
Purpose of this study
Salt concentration has been recently proposed as an important control parameter of reduction stability of electrolytes.
In the previous studies, the decomposition mechanism of electrolytes has been investigated by using the quantum chemical calculations and DFT-MD simulations. However, its effect on the SEI film formation is still not found.
In the present study, the effect of salt concentration on the SEI film formation is investigated by using the hybrid MC/MD reaction method.
On the other hand, the use of high concentration electrolyte is becoming the important strategy to develop the sodium-ion battery.
Notes: So, ~.

## Slide 5
Target system
(a) Low concentration (1.0 M)
(b) High concentration (4.5 M)
For this purpose, I employed the electrolyte solutions consisting of AN-NaFSA electrolyte solution at the (a) low and (b) high concentration conditions.
: Acetonitrile
: Na+
: FSA-
(bis(fluorosulfonyl)amide)
800 Acetonitrile
52 Na+
50 FSA-
800 Acetonitrile
302 Na+
300 FSA-
Negative charge: -2e
Negative charge: -2e
Notes: Next, I explain the target system of this study. In this study, I employed the electrolyte solutions consisting of AN-NaFSA electrolyte solution at the low and high concentration conditions like this. According to the previous experimental condition, I selected these two concentrations. And, you can see the number of molecules in these two systems.

## Slide 6
Elementary reactions for MC/MD simulation
CH3CN
+ e-
CH3CN-
+ e-
+
dec-FSA-
CH3CN
CN-
CH3-
+
+ FSA
+
F-
+ CH3CN-
FSA
+ e-
dec-FSA-
+
F-
These elementary reaction processes are considered for the hybrid MC/MD reaction simulation.
[1] Y. Yamada et al., J. Am. Chem. Soc., 136, 5039 (2014).
47.1 kcal/mol
26.8 kcal/mol
64.9 kcal/mol
17.8 kcal/mol
17.8 kcal/mol
Red: Potential energy difference
-13.6 kcal/mol
Blue: Free energy difference
with SMD model
Calculation level: B3LYP/cc-pvdz
-54.4 kcal/mol
-28.8 kcal/mol
-15.2 kcal/mol
-15.2 kcal/mol
Notes: Next, I explain the elementary reactions for MC/MD simulation. These elementary reaction processes are decided by reference to the previous studies. First, the AN solvents are reduced on the anode surface, and the AN anions are formed. But, they do not decompose. And, AN anions can accept the additional electron, and decompose into CN and CH3 anions. On the other hand, FSA salt is also reduced on the anode surface to form fluoride anion and this species. I called this molecule dec-FSA anion. And, if AN anion is close to the FSA anion, the electron can move from AN anion to FSA salt like this. And, in this slide, I showed the potential energy and free energy differences by using red and blue colors, respectively.

## Slide 7
SEI film Formation Simulations
on
(b) High concentration
(a) Low concentration
Orange: CH3-, Red: CN-, Yellow: CH3CN-, Pink: F-, Right green: dec-FSA-
Notes: Next, I showed the animation of SEI film formation simulations. The left figure shows the result at low concentration, and right one is high concentration. These colors correspond to these species. First, the AN solvents are reduced on the anode surface. Comparing these two systems, at the low concentration, the aggregation of dec-FSA anions became insufficient. On the other hand, at the high concentration, the stable film by the dec-FSA anions was formed in the outer region like this. This is a important point.

## Slide 8
Change in number of molecules during simulations
Chart: 
| 20 | 60 | 100 | 140 | 180 | 220 | 260 | 300 | 340 | 380 | 420 | 460 | 500 | 540 | 580 | 620 | 660 | 700 | 740 | 780 | 820 | 860 | 900 | 940 | 980 | 1020 | 1060 | 1100 | 1140 | 1180 | 1220 | 1260 | 1300 | 1340 | 1380 | 1420 | 1460 | 1500 | 1540 | 1580 | 1620 | 1660 | 1700 | 1740 | 1780 | 1820 | 1860 | 1900 | 1940 | 1980
 | 24.8 | 40.6 | 56.2 | 72.2 | 86.8 | 95.4 | 109.2 | 124.2 | 131.6 | 142.8 | 153 | 151.6 | 144.8 | 133.8 | 124.8 | 116.6 | 108.8 | 105.8 | 105 | 104.2 | 103.4 | 102.6 | 102 | 101.2 | 101 | 100.2 | 99.8 | 99.6 | 99.4 | 98.8 | 98 | 97.6 | 97 | 96.8 | 96.8 | 96.4 | 96.2 | 95.4 | 95.2 | 95 | 94.4 | 94.2 | 94.2 | 93.6 | 93.2 | 92.8 | 92.8 | 92.4 | 92 | 91.8
 | 0.4 | 1.4 | 2 | 3.4 | 5.2 | 7.2 | 9.4 | 11.8 | 15 | 18.8 | 25.2 | 34.6 | 45.2 | 58.4 | 69.6 | 78.4 | 84.6 | 87 | 87.4 | 87.4 | 87.8 | 87.8 | 88 | 88 | 88 | 88 | 88.2 | 88.2 | 88.2 | 88.2 | 88.2 | 88.2 | 88.2 | 88.2 | 88.2 | 88.2 | 88.2 | 88.2 | 88.2 | 88.2 | 88.2 | 88.4 | 88.4 | 88.6 | 88.6 | 88.6 | 88.6 | 88.6 | 88.6 | 88.6
 | 1 | 4.2 | 5.2 | 6.6 | 7.2 | 8.4 | 9.4 | 9.6 | 10.6 | 11.4 | 11.6 | 11.8 | 12.8 | 13.8 | 14.8 | 15.2 | 17 | 17.8 | 18.2 | 19 | 19.4 | 20.2 | 20.6 | 21.4 | 21.6 | 22.4 | 22.6 | 22.8 | 23 | 23.6 | 24.4 | 24.8 | 25.4 | 25.6 | 25.6 | 26 | 26.2 | 27 | 27.2 | 27.4 | 28 | 28 | 28 | 28.4 | 28.8 | 29.2 | 29.2 | 29.6 | 30 | 30.2
 | 49 | 45.8 | 44.8 | 43.4 | 42.8 | 41.6 | 40.6 | 40.4 | 39.4 | 38.6 | 38.4 | 38.2 | 37.2 | 36.2 | 35.2 | 34.8 | 33 | 32.2 | 31.8 | 31 | 30.6 | 29.8 | 29.4 | 28.6 | 28.4 | 27.6 | 27.4 | 27.2 | 27 | 26.4 | 25.6 | 25.2 | 24.6 | 24.4 | 24.4 | 24 | 23.8 | 23 | 22.8 | 22.6 | 22 | 22 | 22 | 21.6 | 21.2 | 20.8 | 20.8 | 20.4 | 20 | 19.8
 | 774.8 | 758 | 741.8 | 724.4 | 708 | 697.4 | 681.4 | 664 | 653.4 | 638.4 | 621.8 | 613.8 | 610 | 607.8 | 605.6 | 605 | 606.6 | 607.2 | 607.6 | 608.4 | 608.8 | 609.6 | 610 | 610.8 | 611 | 611.8 | 612 | 612.2 | 612.4 | 613 | 613.8 | 614.2 | 614.8 | 615 | 615 | 615.4 | 615.6 | 616.4 | 616.6 | 616.8 | 617.4 | 617.4 | 617.4 | 617.8 | 618.2 | 618.6 | 618.6 | 619 | 619.4 | 619.6
Chart: 
| 20 | 60 | 100 | 140 | 180 | 220 | 260 | 300 | 340 | 380 | 420 | 460 | 500 | 540 | 580 | 620 | 660 | 700 | 740 | 780 | 820 | 860 | 900 | 940 | 980 | 1020 | 1060 | 1100 | 1140 | 1180 | 1220 | 1260 | 1300 | 1340 | 1380 | 1420 | 1460 | 1500 | 1540 | 1580 | 1620 | 1660 | 1700 | 1740 | 1780 | 1820 | 1860 | 1900 | 1940 | 1980
 | 10.4 | 16.8 | 20 | 27.6 | 28.6 | 31.6 | 37.6 | 42.2 | 44.4 | 51 | 62.4 | 70.6 | 81.6 | 93.6 | 104.2 | 113.8 | 121.4 | 127.2 | 136.6 | 144.6 | 151.8 | 164.2 | 168 | 168.2 | 162.8 | 157.2 | 149.6 | 144.2 | 140.8 | 139.2 | 138.4 | 138.4 | 137.8 | 137.6 | 137.6 | 137.6 | 137.4 | 137.2 | 137.2 | 137 | 136.6 | 136.6 | 136.6 | 136.6 | 136.6 | 136.6 | 136.6 | 136.6 | 136.6 | 136.6
 | 0.4 | 0.4 | 0.6 | 0.8 | 0.8 | 0.8 | 1.2 | 1.4 | 1.4 | 1.8 | 1.8 | 2.6 | 4 | 6 | 7 | 8.8 | 11 | 13.6 | 17.2 | 22.4 | 25.8 | 27.8 | 33.8 | 41 | 49.6 | 59 | 69 | 76.6 | 80 | 81.6 | 82.4 | 82.4 | 82.8 | 83 | 83 | 83 | 83.2 | 83.2 | 83.2 | 83.4 | 83.6 | 83.6 | 83.6 | 83.6 | 83.6 | 83.6 | 83.6 | 83.6 | 83.6 | 83.6
 | 10 | 19 | 29.8 | 36.6 | 46 | 50.6 | 56.2 | 63.2 | 69.6 | 75 | 77.8 | 81.2 | 84 | 85.4 | 85.8 | 86.8 | 87.6 | 87.8 | 88 | 88 | 88.2 | 88.4 | 88.4 | 88.6 | 88.8 | 89 | 89.2 | 89.2 | 89.4 | 89.4 | 89.4 | 89.4 | 89.6 | 89.6 | 89.6 | 89.6 | 89.6 | 89.8 | 89.8 | 89.8 | 90 | 90 | 90 | 90 | 90 | 90 | 90 | 90 | 90 | 90
 | 290 | 281 | 270.2 | 263.4 | 254 | 249.4 | 243.8 | 236.8 | 230.4 | 225 | 222.2 | 218.8 | 216 | 214.6 | 214.2 | 213.2 | 212.4 | 212.2 | 212 | 212 | 211.8 | 211.6 | 211.6 | 211.4 | 211.2 | 211 | 210.8 | 210.8 | 210.6 | 210.6 | 210.6 | 210.6 | 210.4 | 210.4 | 210.4 | 210.4 | 210.4 | 210.2 | 210.2 | 210.2 | 210 | 210 | 210 | 210 | 210 | 210 | 210 | 210 | 210 | 210
 | 789.2 | 782.8 | 779.4 | 771.6 | 770.6 | 767.6 | 761.2 | 756.4 | 754.2 | 747.2 | 735.8 | 726.8 | 714.4 | 700.4 | 688.8 | 677.4 | 667.6 | 659.2 | 646.2 | 633 | 622.4 | 608 | 598.2 | 590.8 | 587.6 | 583.8 | 581.4 | 579.2 | 579.2 | 579.2 | 579.2 | 579.2 | 579.4 | 579.4 | 579.4 | 579.4 | 579.4 | 579.6 | 579.6 | 579.6 | 579.8 | 579.8 | 579.8 | 579.8 | 579.8 | 579.8 | 579.8 | 579.8 | 579.8 | 579.8
CH3-, CN-
F-, dec-FSA-
CH3CN-
CH3CN (or AN)
FSA-
CH3-, CN-
F-, dec-FSA-
CH3CN-
CH3CN (or AN)
FSA-
MC/MD cycle
MC/MD cycle
Number of molecule
Number of molecule
At the low concentration, the FSA anions were continue to be reduced.
At the high concentration, the FSA anions were reduced in first stage.
Then, the solvent AN molecules were reduced in second stage.
(a) Low concentration (1.0 M)
(b) High concentration (4.5 M)
Notes: Next, I show the change in the number of molecules during simulations. In these two figures, the horizontal axis is MC/MD cycle, and vertical one is number of molecules. And, these values are averaged one obtained by using 5 different initial configurations. And, it is noted the right vertical axis correspond to the number of AN molecule. In both conditions, the number of AN molecules converged. But, at the low concentration, the number of FSA anions were continue to decrease during the simulation. This shows the SEI film is not stable. On the other hand, at the high concentration, the FSA anions were reduced in first stage. Then, the solvent AN molecules were reduced in second stage.

## Slide 9
Discussion on first stage
(a) Low concentration (1.0 M)
(a) High concentration (4.5 M)
In the first stage, at the high concentration, the dec-FSA- formed the stable film to prevent the further decomposition of FSA anions.
Orange: CH3-, Red: CN-, Yellow: CH3CN-, Pink: F-, Right green: dec-FSA-
Decomposed products from salts
Notes: Next, I discuss on the first stage of SEI film formation. I showed the snapshots at 400 MC/MD cycles like this. In the first stage, ~ as shown in this figure.

## Slide 10
Discussion on second stage
dissolution
At the low concentration, the reaction products drifted away from the SEI film.
At the high concentration, such dissolution was clearly suppressed.
Orange: CH3-, Red: CN-, Yellow: CH3CN-, Pink: F-, Right green: dec-FSA-
(a) Low concentration (1.0 M)
(a) High concentration (4.5 M)
Notes: Next, I showed the snapshots at 1000 MC/MD cycles like this. As you can see, at the low concentration, ~/

## Slide 11
Atomistic structures of SEI films (at 2000 cycle)
Orange: CH3-, Red: CN-, Yellow: CH3CN-, Pink: F-, Right green: dec-FSA-
At the low concentration, the surface of SEI film became rough.
At the high concentration, the surface became smoother because the stable film originated from the salts were formed in the outer region of the SEI film.
rough
smooth
(a) Low concentration (1.0 M)
(a) High concentration (4.5 M)

## Slide 12
Chart: 
| 1 | 3 | 5 | 7 | 9 | 11 | 13 | 15 | 17 | 19 | 21 | 23 | 25 | 27 | 29 | 31 | 33 | 35 | 37 | 39 | 41 | 43 | 45 | 47 | 49 | 51 | 53 | 55 | 57 | 59 | 61 | 63 | 65 | 67 | 69 | 71 | 73 | 75 | 77 | 79
 | 0 | 9.4531e-06 | 0.00091748 | 0.0079578 | 0.0063493 | 0.0074463 | 0.0059247 | 0.0048479 | 0.0018486 | 0.00044518 | 0.00016092 | 1.7455e-05 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0.01317 | 0.011299 | 0.0062701 | 0.003028 | 0.0013627 | 0.0011018 | 0.0001039 | 0.000144 | 7.8512e-07 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0.0071048 | 0.0068458 | 0.012008 | 0.0045397 | 0.0033727 | 0.001413 | 0.00065934 | 0.00040022 | 9.032e-05 | 4.5933e-05 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0.00022108 | 1.6836e-05 | 7.7322e-06 | 0.0004906 | 0.00031447 | 0.00080247 | 0.00079009 | 0.0013687 | 0.0014447 | 0.0012755 | 0.0012342 | 0.0010349 | 0.0012863 | 0.00066329 | 0.00034909 | 9.2501e-05 | 0.00014703 | 0.00014659 | 0.00010528 | 0.00010904 | 0.00014042 | 0.00013293 | 7.9796e-05 | 4.2737e-05 | 5.7425e-05 | 4.625e-05 | 2.9033e-05 | 1.0595e-05 | 4.8534e-06 | 3.3546e-06 | 7.4546e-07 | 1.5544e-06 | 3.4101e-07 | 3.1722e-07 | 0 | 0 | 0 | 0 | 0
 | 0 | 7.9233e-05 | 0.00024733 | 0.00098781 | 0.0016869 | 0.0014273 | 0.0012548 | 0.0011703 | 0.0010959 | 0.00096727 | 0.00070894 | 0.00065422 | 0.00071538 | 0.00056336 | 0.00026064 | 0.00020768 | 2.7225e-05 | 1.4275e-07 | 1.5226e-06 | 2.529e-05 | 0.00010465 | 0.00014018 | 4.2563e-05 | 8.8345e-06 | 1.1729e-05 | 3.2475e-05 | 2.4648e-05 | 4.3142e-06 | 1.7447e-07 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: 
| 1 | 3 | 5 | 7 | 9 | 11 | 13 | 15 | 17 | 19 | 21 | 23 | 25 | 27 | 29 | 31 | 33 | 35 | 37 | 39 | 41 | 43 | 45 | 47 | 49 | 51 | 53 | 55 | 57 | 59 | 61 | 63 | 65 | 67 | 69 | 71 | 73 | 75 | 77 | 79
 | 0 | 7.9305e-09 | 0.00045765 | 0.0028394 | 0.0044002 | 0.0056479 | 0.006825 | 0.0052574 | 0.0045481 | 0.0043433 | 0.0028444 | 0.0016399 | 0.0010005 | 0.00060893 | 0.00011205 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0.011147 | 0.013561 | 0.005125 | 0.0033509 | 0.0017033 | 0.00093877 | 0.0005067 | 0.00011628 | 0.00010006 | 0.00016878 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0.0060672 | 0.007353 | 0.0091003 | 0.0064168 | 0.0036302 | 0.0014845 | 0.0014156 | 0.00080643 | 0.0001788 | 0.00018602 | 0 | 6.66e-05 | 1.2705e-05 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 5.9701e-05 | 0.00024923 | 2.7106e-05 | 2.2562e-05 | 8.6402e-05 | 0.00012735 | 9.2739e-05 | 0.00015922 | 0.00073934 | 0.00092282 | 0.0012576 | 0.0015461 | 0.0022567 | 0.0019832 | 0.0019857 | 0.0021344 | 0.0014317 | 0.0010793 | 0.0011783 | 0.00032364 | 9.8695e-05 | 2.3871e-06 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 9.3516e-05 | 0.00028941 | 0.001246 | 0.0022578 | 0.0029421 | 0.0035408 | 0.0028631 | 0.0022381 | 0.0012085 | 0.00059463 | 0.0001223 | 2.1698e-05 | 5.6624e-05 | 5.5593e-05 | 0.00012752 | 2.3173e-05 | 8.3222e-05 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Number density distributions of reaction products
CH3CN-
CH3-
CN-
dec-FSA-
F-
(b) High concentration
z [Å]
Number density [Å-3]
CH3CN-
CH3-
CN-
dec-FSA-
F-
z [Å]
(a) Low concentration
The CH3 and CN anions were mainly distributed near the anode surface. On the other hand, CH3CN- were existing at the outside of CH3- and CN-.
At the high concentration, there was a stable film of dec-FSA- in the outer region.
Number density [Å-3]
Notes: Next, I show the number density distributions of reaction products. The horizontal axis is z coordinate from the anode surface. According to these figures, ~

## Slide 13
Summary
In the present study, the salt concentration effect on the SEI film formation was investigated in the AN/FSA electrolytes by using the hybrid MC/MD reaction method.
At the low concentration, since the aggregation of reaction products was insufficient, they were found to drift away from the SEI film, showing that the irreversible capacity increases.
On the other hand, at the high concentration, the dissolution of reaction products was clearly suppressed owing to the presence of stable film originated from the salt decomposition. As a result, the surface of SEI film became smoother at the high concentration.
It was concluded that the high concentration AN/FSA electrolytes can improve the SEI film formation so as to suppress the decomposition and dissolution of the salts.