## Slide 1
FY2018’s 3th, CREST Workshop
Norio Takenaka1,2
Graduate School of Information Science, Nagoya University1,
Elements Strategy Initiative for Catalysts and Batteries (ESICB), Kyoto University2
Microscopic Structural Analyses of Hydrate Melt Electrolyte on Electrode Surface
Tue. Nov. 20th

## Slide 2
Introduction
Portable electronic device
Electric vehicle
Lithium-ion battery (LIB)
Next-generation battery
Aqueous lithium-ion battery
● Non-toxic
● Non-flammable
● Low-price

## Slide 3
3
LiTFSI
LiBETI
Fig. Potential window [1]
Hydrate Melt
By using a Li salt hydrate melt, Li(TFSI)0.7(BETI)0.3・2H2O, the high voltage aqueous Li-ion battery has been developed [1].
[1] Y. Yamada, K. Usui, K. Sodeyama, S. Ko, Y. Tateyama and A. Yamada, Nature energy, 16129 (2016).
2.0 V
3.8 V

## Slide 4
Presence of “Isolated Water” in Hydrate Melt
Raman Spectroscopy
DFT-MD
The experimental and theoretical studies indicated the presence of “isolated water” that water molecules (i.e., oxygen atoms) coordinate with Li+.
4
anion
water
Li+

## Slide 5
Effective Lennard-Jones parameters of Pt were obtained by DFT calculations [2]
Non-bond interaction
 | σ [Å] | ε [kcal/mol]
Pt | 1.205 | 4.645
C (graphite) | 1.70 | 0.0556
O (water) | 1.58 | 0.152
5
Temperature: 298 K
Force filed: GAFF, TIP3P water, Pt(111) [1,2], graphite [3]
Constant potential method developed by Inagaki-san
[1] S. Duan, X. Xu, Z. Tian, Y. Luo, Phys. Rev. B, 86, 045450 (2012).
[3] C. Li, T-W. Chou, Int. J. Solids Struct., 40, 2487 (2005).
[2] S. Y. Liem, K-Y. Chan, Molecular Physics, 86, 939 (1995).
Calculation Condition
Table. Lennard-Jones parameters

## Slide 6
MD Simulations in Bulk Hydrate Melt
: H2O
: TFSI
: BETI
: Li+
10 ns NPT MD
(TFSI)0.7(BETI)0.3(H2O)2
TFSI: 280
BETI: 120
H2O: 800
Li+: 400
Number of molecules
Chart: 
Integrated value in first solvation shell: 0.14
(pure water: 2.0)
Figures. O-H radial distribution function
R(O-H), Å
G(R)
2.3 Å
6
Pure water
Hydrate melt
W. Jorgensen et al., J. Chem. Phys., 79, 926 (1983)

## Slide 7
Number of “Isolated Water”
10 ns NPT MD
(TFSI)0.7(BETI)0.3(H2O)2
By checking all water molecules whether they satisfy the criteria, the number of isolated water molecules was estimated.
r
r ≦ 2.3 Å
not isolated
r > 2.3 Å
isolated
Number of isolated water: 722.6
(90.3 %)
TFSI: 280
BETI: 120
H2O: 800
Li+: 400
Number of molecules
7
: H2O
: TFSI
: BETI
: Li+

## Slide 8
8
graphite-hydrate melt
Pt(111)-hydrate melt
TFSI: 280, BETI: 120, H2O: 800, Li+: 400
The two types of electrode materials were employed.
MD Simulations with Hydrate Melt on Electrode
TFSI: 280, BETI: 120, H2O: 800, Li+: 400
By using the constant potential method, the voltage dependency of the hydrate melt structures was investigated.
Total simulation time: 50 ns NVT MD (time step: 0.2 fs)
Fictitious mass of charge: 1519 fs2V/e

## Slide 9
Chart: 
Potential Change of Electrode near Pt Surface
0 V (PZC)
-1 V versus PZC
z [Å]
Potential [V]
The potential difference between the electrode and electrolyte became 0.4 V at potential of zero charge (PZC) condition.
By considering the open-circuit voltage of 3.3 V versus Li+/Li, the lower limit of potential window on Pt almost corresponds to -1 V versus PZC.
Figure. potential window
Y. Yamada, K. Usui, K. Sodeyama, S. Ko, Y. Tateyama, A. Yamada, Nature Energy, 16129 (2016).
9

## Slide 10
Number Density Distribution on Graphite
Chart: 
| 0.25 | 0.75 | 1.25 | 1.75 | 2.25 | 2.75 | 3.25 | 3.75 | 4.25 | 4.75 | 5.25 | 5.75 | 6.25 | 6.75 | 7.25 | 7.75 | 8.25 | 8.75 | 9.25 | 9.75
 | 0 | 0 | 0 | 3.4018e-05 | 0.019194 | 0.037253 | 0.059395 | 0.40901 | 1.0357 | 1.2505 | 1.7906 | 1.2584 | 0.92376 | 1.2835 | 2.7226 | 2.755 | 1.7484 | 1.4132 | 0.68636 | 0.57716
 | 0 | 0 | 0 | 0 | 0 | 0.28134 | 2.2825 | 1.275 | 0.65464 | 0.41779 | 0.3406 | 0.59908 | 0.80721 | 0.81392 | 1.0721 | 1.4855 | 1.6538 | 1.7127 | 1.2983 | 0.89127
 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.010641 | 1.5928 | 5.1281 | 1.1452 | 2.4154 | 2.5608 | 0.92991 | 0.29773 | 0.18763 | 0.58631 | 0.98415 | 1.5875 | 2.0086
 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.0019347 | 1.4532 | 5.4709 | 0.8026 | 0.010047 | 0.0011608 | 0.31099 | 0.90605 | 1.1563 | 0.076962 | 0.074679 | 0.22729 | 0.56342
ρ/ρbulk
z [Å]
Chart: 
| 0.25 | 0.75 | 1.25 | 1.75 | 2.25 | 2.75 | 3.25 | 3.75 | 4.25 | 4.75 | 5.25 | 5.75 | 6.25 | 6.75 | 7.25 | 7.75 | 8.25 | 8.75 | 9.25 | 9.75
 | 0 | 0 | 0 | 0.038176 | 0.22421 | 0.053034 | 0.40422 | 1.3227 | 1.9062 | 2.0064 | 1.5294 | 0.6536 | 0.59139 | 1.2349 | 1.9755 | 1.9833 | 1.7804 | 1.3416 | 0.77852 | 0.57328
 | 0 | 0 | 0 | 0 | 1.2364e-05 | 1.2272 | 3.8549 | 1.2681 | 0.52232 | 0.37444 | 0.39373 | 0.88803 | 0.94074 | 0.70802 | 0.76452 | 1.0245 | 1.3191 | 1.2245 | 0.97579 | 0.68275
 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.038839 | 2.2607 | 3.6326 | 1.6095 | 2.8529 | 2.9938 | 0.78985 | 0.32441 | 0.6859 | 0.8153 | 1.2904 | 1.7039 | 1.9025
 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 1.1754 | 3.0441 | 0.39046 | 0.70242 | 0.80154 | 0.67087 | 0.17757 | 0.035289 | 0.101 | 0.21498 | 0.47272 | 0.91178
Chart: 
| 0.25 | 0.75 | 1.25 | 1.75 | 2.25 | 2.75 | 3.25 | 3.75 | 4.25 | 4.75 | 5.25 | 5.75 | 6.25 | 6.75 | 7.25 | 7.75 | 8.25 | 8.75 | 9.25 | 9.75
 | 0 | 0 | 0 | 0 | 0 | 0 | 0.00016252 | 0.0084427 | 0.30844 | 1.1544 | 1.1335 | 1.2339 | 0.86253 | 1.1928 | 3.5576 | 3.2581 | 2.0272 | 1.3149 | 0.79865 | 0.52819
 | 0 | 0 | 0 | 0 | 0 | 0.022646 | 1.0523 | 1.1546 | 0.65221 | 0.31873 | 0.22294 | 0.3403 | 0.63187 | 0.9304 | 1.538 | 2.051 | 1.9588 | 2.0685 | 1.5202 | 1.0013
 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.0019031 | 1.0728 | 5.587 | 1.4411 | 1.6808 | 2.1638 | 0.53445 | 0.214 | 0.026201 | 0.0090598 | 0.22377 | 1.6056 | 2.1666
 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 1.1105 | 7.177 | 1.1128 | 0.010462 | 1.2005 | 1.522 | 1.1493 | 0.73561 | 0.083415 | 0.004655 | 0.0014576 | 0.73942
z [Å]
z [Å]
Li+
H2O
TFSI
BETI
Li+
H2O
TFSI
BETI
Li+
H2O
TFSI
BETI
+1 V versus PZC
-1 V versus PZC
0 V (PZC)
Figures. Number density profiles of molecules (center of mass)
On the graphite surface, the peak height of water molecules decreased with increasing electrode potential, while that of anions increased.
10

## Slide 11
Electrode: Graphite surface
Temperature: 363 K
constant potential method [2]
[2] S. K. Reed, O. J. Lanning, P. A. Madden, J. Chem. Phys. 126, 084704 (2007).
Calculation condition
Force filed: APPLE&P
z
Simulation time: 7 ns
Comparison with Previous Theoretical Research
[*] J. Vatamanu, O.Borodin, J. Phys. Chem. Lett., 8, 4362-4367 (2017).
OTF
trifluoromethanesulfonate

## Slide 12
Comparison with Previous Theoretical Research
[*] J. Vatamanu, O.Borodin, J. Phys. Chem. Lett., 8, 4362-4367 (2017).
The present simulation results showed the similar tendency as the previous study where the number of water molecules decreases with the increase in the electrode potential.
Figures. Cumulative atom number density profiles on graphite [*]
+2 V versus PZC
-2 V versus PZC
0 V (PZC)

## Slide 13
Chart: 
| 0.25 | 0.75 | 1.25 | 1.75 | 2.25 | 2.75 | 3.25 | 3.75 | 4.25 | 4.75 | 5.25 | 5.75 | 6.25 | 6.75 | 7.25 | 7.75 | 8.25 | 8.75 | 9.25 | 9.75
 | 0 | 0 | 0 | 0.045821 | 1.3906 | 1.7569 | 3.7066 | 1.1764 | 0.32033 | 0.48993 | 0.27932 | 0.082521 | 0.8276 | 0.96889 | 0.35904 | 0.64669 | 0.8864 | 1.2212 | 1.265 | 0.75972
 | 0 | 0 | 0 | 0 | 0.20255 | 4.2437 | 0.5819 | 0.10234 | 0.078171 | 0.51106 | 1.8845 | 0.4474 | 0.41015 | 1.0038 | 2.3755 | 1.5876 | 1.0121 | 0.84895 | 0.7452 | 0.83625
 | 0 | 0 | 0 | 0 | 0 | 0 | 1.625 | 4.796 | 6.5456 | 0.12502 | 0.00036658 | 0 | 0 | 0.0018591 | 0.28844 | 0.31211 | 0.62103 | 1.211 | 1.1935 | 2.1776
 | 0 | 0 | 0 | 0 | 0 | 0 | 0.0080576 | 4.9157 | 4.1206 | 0.58673 | 1.2484 | 0.52153 | 0.37341 | 0.51028 | 0.0065553 | 0.0065553 | 0.71789 | 0.78303 | 0.94954 | 1.5509
Chart: 
| 0.25 | 0.75 | 1.25 | 1.75 | 2.25 | 2.75 | 3.25 | 3.75 | 4.25 | 4.75 | 5.25 | 5.75 | 6.25 | 6.75 | 7.25 | 7.75 | 8.25 | 8.75 | 9.25 | 9.75
 | 0 | 0 | 0.22605 | 4.5951 | 4.3065 | 1.6732 | 0.65619 | 0.27979 | 0.098225 | 0.097757 | 0.071722 | 0.40145 | 2.6397 | 1.9015 | 0.45896 | 0.52459 | 1.1454 | 1.0008 | 1.0611 | 0.70161
 | 0 | 0 | 0 | 0 | 1.0881 | 3.8319 | 0.16559 | 0.038821 | 0.023838 | 0.23055 | 0.58281 | 0.40707 | 0.67377 | 1.6583 | 2.8291 | 1.7482 | 1.1927 | 0.88007 | 0.78548 | 0.82006
 | 0 | 0 | 0 | 0 | 0 | 0 | 4.6687 | 7.1661 | 3.3142 | 1.2054 | 0.14244 | 0.13305 | 0.10292 | 0.25676 | 0.1597 | 0.17589 | 1.1134 | 0.96726 | 1.3667 | 1.7822
 | 0 | 0 | 0 | 0 | 0 | 0 | 0.00071016 | 1.1328 | 1.5378 | 1.6614 | 1.7281 | 0.22225 | 0.24804 | 0.2972 | 8.1941e-05 | 0.0073201 | 0.32195 | 1.8112 | 1.9452 | 2.0465
Number Density Distribution on Pt
Chart: 
| 0.25 | 0.75 | 1.25 | 1.75 | 2.25 | 2.75 | 3.25 | 3.75 | 4.25 | 4.75 | 5.25 | 5.75 | 6.25 | 6.75 | 7.25 | 7.75 | 8.25 | 8.75 | 9.25 | 9.75
 | 0 | 0 | 0.0032412 | 1.3668 | 3.7572 | 2.4118 | 1.593 | 0.3254 | 0.17467 | 0.052859 | 0.027881 | 0.089657 | 2.2264 | 1.9476 | 0.43741 | 0.72241 | 1.1529 | 1.3184 | 0.74258 | 0.47881
 | 0 | 0 | 0 | 0 | 0.86047 | 4.153 | 0.21233 | 0.053933 | 0.057933 | 0.51643 | 0.92866 | 0.38574 | 0.56116 | 1.6413 | 3.4545 | 2.0016 | 1.1652 | 0.80962 | 0.57412 | 0.7583
 | 0 | 0 | 0 | 0 | 0 | 0 | 2.8618 | 7.0907 | 3.89 | 0.50869 | 0.11292 | 0 | 0 | 0.001755 | 0.098459 | 0.26968 | 0.42568 | 1.1193 | 1.7099 | 1.9229
 | 0 | 0 | 0 | 0 | 0 | 0 | 0.074074 | 4.56 | 1.4165 | 1.6184 | 1.5691 | 0.59102 | 0.00057574 | 5.617e-05 | 0.072515 | 0.79004 | 0.82746 | 1.5533 | 1.2747 | 1.604
ρ/ρbulk
z [Å]
z [Å]
z [Å]
Figures. Number density profiles of molecules (center of mass)
On the Pt surface, the Li+ cations adsorbed due to the strong van der Waals attractive interaction in comparison to the graphite.
As the electrode potential increases, the Li+ cations were expelled due to the repulsive electrostatic interaction.
+1 V versus PZC
-1 V versus PZC
0 V (PZC)
Li+
H2O
TFSI
BETI
Li+
H2O
TFSI
BETI
Li+
H2O
TFSI
BETI

## Slide 14
Chart: 
| -2 | -1 | 0 | 1 | 2
 | 1.6864 | 1.4321 | 1.1194 | 0.77126 | 0.50799
 | 3.9438 | 3.2244 | 2.2841 | 1.4967 | 0.96029
 | 1.4189 | 1.4019 | 1.4077 | 1.251 | 1.2722
 | 0.29967 | 0.36493 | 0.42105 | 0.63336 | 0.5819
Chart: 
| -2 | -1 | 0 | 1 | 2
 | 2.5293 | 2.2764 | 1.8335 | 1.5245 | 1.1636
 | 1.9566 | 2.1556 | 2.3216 | 2.59 | 1.0758
 | 1.6714 | 1.7089 | 1.5042 | 1.3371 | 1.3371
 | 0.33287 | 0.31972 | 0.46798 | 0.57638 | 0.60168
Li+
H2O
TFSI
BETI
Electrode potential [V]
Electrode potential [V]
Number of molecules [nm-2]
Number of molecules [nm-2]
The integrated number was estimated from 0 to 6 Å.
(a) Pt
(b) Graphite
Integrated Number of Electrolyte Molecules
Li+
H2O
TFSI
BETI
In the interfacial region near the graphite surface, the number of water and Li+ lineally decreased with the increase in the electrode potential.
On the Pt surface, water molecules showed a peak at 1 V.

## Slide 15
Chart: 
| 0.05 | 0.15 | 0.25 | 0.35 | 0.45 | 0.55000000000000004 | 0.65 | 0.75 | 0.85 | 0.95
 | 0.059596 | 0.055959 | 0.05047 | 0.044953 | 0.040031 | 0.036389 | 0.034157 | 0.039279 | 0.091461 | 0.5477
 | 0.060673 | 0.06041 | 0.05957 | 0.060135 | 0.061636 | 0.066598 | 0.076088 | 0.098792 | 0.15251 | 0.30386
Normal vector
Normal vector
θ
cosθ
Parallel
Perpendicular
ρangle
Graphite
Pt
Angle between two vectors
The water plane mainly took the parallel orientation to the surface.
15
The values were estimated within 4 Å from the surface.
Angle Distributions in Pure Water

## Slide 16
Chart: 
| 0.05 | 0.15 | 0.25 | 0.35 | 0.45 | 0.55000000000000004 | 0.65 | 0.75 | 0.85 | 0.95
 | 0.23982 | 0.20553 | 0.15648 | 0.11034 | 0.078222 | 0.056536 | 0.04324 | 0.036858 | 0.035536 | 0.037435
 | 0.28409 | 0.23528 | 0.17039 | 0.11574 | 0.077052 | 0.050443 | 0.030684 | 0.019294 | 0.011458 | 0.0055568
 | 0.32775 | 0.26821 | 0.17456 | 0.095461 | 0.052934 | 0.032525 | 0.02112 | 0.01488 | 0.009373 | 0.0031896
Parallel
0 V
cosθ
cosθ
On the Pt, the water plane showed the perpendicular orientation, while it took parallel orientation on the graphite.
-1 V
1 V
Perpendicular
ρangle
ρangle
16
Angle Distributions of Water in Hydrate Melt
(a) Pt
(b) Graphite
Chart: 
| 0.05 | 0.15 | 0.25 | 0.35 | 0.45 | 0.55000000000000004 | 0.65 | 0.75 | 0.85 | 0.95
 | 0.10012 | 0.099596 | 0.097229 | 0.095108 | 0.093159 | 0.092225 | 0.092873 | 0.096659 | 0.10648 | 0.12654
 | 0.093115 | 0.092197 | 0.090551 | 0.088689 | 0.087482 | 0.087958 | 0.09238 | 0.10213 | 0.12015 | 0.14534
 | 0.051393 | 0.051597 | 0.053753 | 0.056537 | 0.061338 | 0.068826 | 0.084738 | 0.11309 | 0.17055 | 0.28818
Perpendicular
0 V
-1 V
1 V
Parallel

## Slide 17
Chart: 
| 0.25 | 0.75 | 1.25 | 1.75 | 2.25 | 2.75 | 3.25 | 3.75 | 4.25 | 4.75 | 5.25 | 5.75 | 6.25 | 6.75 | 7.25 | 7.75 | 8.25 | 8.75 | 9.25 | 9.75 | 10.25
 | 0 | 0 | 0 | 0 | 1.1036 | 3.8361 | 0.17288 | 0.040309 | 0.030705 | 0.2564 | 0.55877 | 0.3981 | 0.64953 | 1.6444 | 2.9052 | 1.7544 | 1.1774 | 0.91486 | 0.79874 | 0.8297 | 0.89296
 | 0 | 0 | 0.06374 | 1.1899 | 2.146 | 2.0509 | 0.79091 | 0.21391 | 0.086008 | 0.16027 | 0.36312 | 0.76843 | 1.6337 | 1.5628 | 1.3619 | 1.5296 | 1.3952 | 0.99882 | 0.80577 | 0.76838 | 0.89426
H
O
ρ/ρbulk
Figures. Atom density profile of water (upper) and number density profile (lower) at PZC
z [Å]
On Pt surface, the water molecules formed the bridge by coordinating with both Li+ and anions.
17
Orientation of Water on Pt(111) Surface at PZC
TFSI
Li+
H2O
Pt
Chart: 
| 0.25 | 0.75 | 1.25 | 1.75 | 2.25 | 2.75 | 3.25 | 3.75 | 4.25 | 4.75 | 5.25 | 5.75 | 6.25 | 6.75 | 7.25 | 7.75 | 8.25 | 8.75 | 9.25 | 9.75
 | 0 | 0 | 0.0032412 | 1.3668 | 3.7572 | 2.4118 | 1.593 | 0.3254 | 0.17467 | 0.052859 | 0.027881 | 0.089657 | 2.2264 | 1.9476 | 0.43741 | 0.72241 | 1.1529 | 1.3184 | 0.74258 | 0.47881
 | 0 | 0 | 0 | 0 | 0.86047 | 4.153 | 0.21233 | 0.053933 | 0.057933 | 0.51643 | 0.92866 | 0.38574 | 0.56116 | 1.6413 | 3.4545 | 2.0016 | 1.1652 | 0.80962 | 0.57412 | 0.7583
 | 0 | 0 | 0 | 0 | 0 | 0 | 2.8618 | 7.0907 | 3.89 | 0.50869 | 0.11292 | 0 | 0 | 0.001755 | 0.098459 | 0.26968 | 0.42568 | 1.1193 | 1.7099 | 1.9229
 | 0 | 0 | 0 | 0 | 0 | 0 | 0.074074 | 4.56 | 1.4165 | 1.6184 | 1.5691 | 0.59102 | 0.00057574 | 5.617e-05 | 0.072515 | 0.79004 | 0.82746 | 1.5533 | 1.2747 | 1.604
ρ/ρbulk
z [Å]
Li+
H2O
TFSI
BETI

## Slide 18
Configuration of Anions on Pt at -1 V
-1 V vs. PZC
-0.49 e
-0.13 e
-0.60 e
TFSI
BETI
water
Li+
Typical structure
18
-0.56 e
-0.48 e
-0.11 e
The molecules are visualized within the region from 0 Å to 10 Å.

## Slide 19
Configuration of Anions on graphite at -1 V
19
-1 V vs. PZC
-0.49 e
-0.13 e
-0.60 e
TFSI
BETI
water
Li+
Typical structure
-0.56 e
-0.48 e
-0.11 e
The molecules are visualized within the region from 0 Å to 10 Å.

## Slide 20
20
Chart: 
| 0.25 | 0.75 | 1.25 | 1.75 | 2.25 | 2.75 | 3.25 | 3.75 | 4.25 | 4.75 | 5.25 | 5.75 | 6.25 | 6.75 | 7.25 | 7.75 | 8.25 | 8.75 | 9.25 | 9.75
 | 0 | 0 | 0 | 0 | 0 | 0.23602 | 0.90309 | 0.56839 | 0.56349 | 0.82313 | 2.0337 | 3.1447 | 2.274 | 1.6658 | 1.4492 | 1.5254 | 1.479 | 1.3842 | 1.231 | 1.2674
 | 0 | 0 | 0 | 0 | 0.00016415 | 1.5913 | 3.0175 | 1.5754 | 1.2893 | 1.3011 | 0.84134 | 0.50262 | 0.49915 | 0.6915 | 0.96241 | 1.228 | 1.4012 | 1.4853 | 1.4251 | 1.4339
 | 0 | 0 | 0 | 0 | 0 | 0.11141 | 0.50459 | 0.16115 | 0.25076 | 0.39679 | 0.97065 | 1.141 | 1.3614 | 1.2777 | 0.55527 | 0.56903 | 0.60303 | 0.68808 | 0.43945 | 0.32914
 | 0 | 0 | 0 | 0 | 6.728e-05 | 0.84179 | 1.8342 | 0.74995 | 0.53763 | 0.89646 | 0.80945 | 0.56639 | 0.21141 | 0.14821 | 0.24856 | 0.48515 | 0.55543 | 0.59345 | 0.56915 | 0.52738
Chart: 
| 0.25 | 0.75 | 1.25 | 1.75 | 2.25 | 2.75 | 3.25 | 3.75 | 4.25 | 4.75 | 5.25 | 5.75 | 6.25 | 6.75 | 7.25 | 7.75 | 8.25 | 8.75 | 9.25 | 9.75
 | 0 | 0 | 0 | 9.7423e-06 | 4.8332 | 6.4965 | 0.24715 | 0.022761 | 0.3124 | 4.0238 | 0.26643 | 0.22239 | 0.22663 | 0.32475 | 0.81266 | 0.64829 | 0.47091 | 0.67492 | 1.0338 | 1.1854
 | 0 | 0 | 0 | 2.1571e-06 | 1.4653 | 2.7492 | 0.42077 | 0.41851 | 2.188 | 3.3658 | 3.1286 | 2.2917 | 0.34397 | 0.6715 | 0.90322 | 1.0252 | 0.91125 | 0.82308 | 0.82004 | 0.93
 | 0 | 0 | 0 | 0 | 1.4333 | 2.1293 | 0.24135 | 0.11661 | 0.2859 | 0.91822 | 0.58644 | 0.31134 | 0.16626 | 0.46629 | 1.1998 | 1.1075 | 0.91996 | 0.81375 | 1.16 | 1.5168
 | 0 | 0 | 0 | 2.7467e-06 | 0.59884 | 0.8383 | 0.16575 | 0.23763 | 0.61816 | 0.92397 | 0.92129 | 0.41759 | 0.43001 | 0.81868 | 1.0727 | 1.2995 | 1.283 | 1.2224 | 1.2181 | 1.3173
F (TFSI)
O (TFSI)
F (BETI)
O (BETI)
ρ/ρbulk
z [Å]
z [Å]
ρ/ρbulk
(a) Pt(111)
(b) Graphite
On the graphite surface, the fluorine atoms oriented to the surface. Such orientation should enhance the formation of LiF which is the main component of SEI film.
The anions were localized near the Pt surface, while they were delocalized near the graphite.
F (TFSI)
O (TFSI)
F (BETI)
O (BETI)
Atomic Distributions of Anions at -1 V

## Slide 21
Conclusion
21
In the hydrate melt, most of water molecules were found to present as the isolated form without hydrogen-bond.
The interfacial structures of hydrate melt strongly depend on not only the electrode potential but also the material (i.e., Pt or graphite).
On the Pt surface, the water molecules took the perpendicular orientation by forming the bridge between Li+ cations and anions.
The weak van der Waals interactions between the anions and electrode could be favorable to form the LiF layer which is the main component of SEI.

## Slide 22
Future Perspective
Electronic properties of “isolated water”
Reduction mechanism of water and salts
22
H2O + e- → H(ad) + OH-
OH- + Li+ → LiOH
H(ad) + H(ad) → H2
Nucleophilic attack of LiOH
⇒ Decomposition of TFSI anions
To understand the SEI formation mechanism in the concentrated water system,
the important key factors are
N. Dubouis et al., Energy & Environ. Sci. 2018, Doi: 10.1039/c8ee02456a.
Solubility of reduction products as a function of electrode potential