## Slide 1: Microscopic Origin of the Salt Concentration Effect on the Formation of Solid Electrolyte Interface Layer in Fire-Extinguishing Electrolyte
Amine Bouibes
5th CREST workshop
March 5th, 2019

## Slide 2
Increase in
temperature and pressure
Increase in the reactions propagation
Under
an abuse condition
Generation of heat
Propagation of heat
Ejection of flammable vapour
Explosion and fire
Thermal runway into organic electrolyte
Ultimate solution: Non flammable electrolyte
Very low flash point
Very short self-extinguishing time
Encountering
the oxygen abruptly
Secondary battery
Fire
Explosion
Sever safety concerns
Secondary batteries concerns
[1] J. Wang; et al. and A. Yamada, Nat. Energy, 3, 22-29 (2018)
Introduction

## Slide 3
Salt
Carbonate Solvent
Non-flammable solvent
Conventional carbonate electrolyte
Conventional non-flammable electrolyte
Non-flammable concentrated electrolyte
High salt concentration
Solvent: Trimenthyl phosphate (TMP)
Salt: Lithium bis (fluorosulfonyl) amide (LiFSA)
Li+
-
Design a fire-extinguishing electrolyte
[Ref] J. Wang; et al. and A. Yamada, Nat. Energy, 3, 22-29 (2018)
Introduction

## Slide 4
LiFSA/TMP fire-extinguishing electrolyte
Purpose: Microscopic origin of salt concentration effect on SEI Layer formation in fire-extinguishing electrolyte for safe batteries.
[1] J. Wang; et al. and A. Yamada, Nat. Energy, 3, 22-29 (2018)
The SEI film was formed at high salt concentration.
The irreversible capacity decreased by increasing salt concentration.
At high salt concentration, safe LIB showed a high performance through a long lifetime.
Introduction

## Slide 5
For this purpose, we employed the LiFSA/TMP electrolyte solution at dilute (1.0 Mol.L-1), moderate (2.3 Mol.L-1) and very high (5.3 Mol.L-1) concentration conditions.
Calculation condition:
Molecule number of LiFSA/TMP electrolyte
 |  |  | Salt concentration (Mol.L-1) |  | 
 |  |  | 1 | 2.3 | 5.3
Number of Species |  | TMP | 800 | 800 | 800
 |  | FSA- | 105 | 250 | 830
 |  | Li+ | 105 | 250 | 830
Molecular ratio (Li) |  | TMP/ FSA | 7.6 | 3.2 | 0.96
TMP
FSA-
Li+
GAFF Force Field
Temperature: 298K
Model system

## Slide 6
Calculation level: m062x/def2TZVP
SMD method with ε = 20.6 (TMP solvents)
+e-
DMP-
OCH3-
-90.87 kcal/mol
(No barrier)
CH3
PO4(CH3)2-
+e-
TMP-
TMP
-23.01 kcal/mol
(18 kcal/mol)
-48.25 kcal/mol
C2H6
CH3
CH3
(No barrier)
.
.
.
-82.56 kcal/mol
1 electron reduction
2 electrons reduction
Red: Free energy of reaction
Blue: Free energy of activation
The decomposition of TMP solvent

## Slide 7
Calculation level: m062x/def2TZVP
SMD method with ε = 20.6 (TMP solvents)
+e-
FSA-
F -
FS2O4N-
-55.86 kcal/mol
(No barrier)
+e-
FS2O4N-
-103.05 kcal/mol
SO2N-
FSO2-
68.47 kcal/mol
TMP-
FSA-
F -
FS2O4N-
TMP
-32.85 kcal/mol
(No barrier)
Red: Free energy of reaction
Blue: Free energy of activation
The decomposition of FSA- anion

## Slide 8
Anode surface : 3.408nm×3.7nm,
Negative charge of anode surface: -2e,
Temperature: 298 K,
10 initial configurations ,
Relaxation time 30 ps,
Mixing time 70 ps,
Aggregated salts were preferentially selected for chemical reduction.
Anode
LiFSA/TMP electrolyte
Red Moon simulation

## Slide 9
SEI layers were obtained at 2000 MC/MD cycles.
FSA- anion were preferentially reduced than TMP solvents.
The decomposition of TMP solvent was supressed by increasing salt concentration.
Surface number densities of SEI layers and electrolyte compounds
SEI layer formation

## Slide 10
200 MC/MD cycle
800 MC/MD cycle
2000 MC/MD cycle
Anode
1Mol concentration
2.3Mol concentration
5.3Mol concentration
[2] Z. Liu. Et al., J. Chem. Phys. Lett., 9, 5508 (2018).
The formation mechanism of obtained SEI layers with RM simulation was Bottom-Up, which was in good agreement with experimental observations [2].
Formation process of SEI layer

## Slide 11
The production of DMP- was not related to the salt concentration.
The production of PO4(CH3)2- anion was reduced by increasing salt concentration.
The production of FS2O4N- anion was increased by increasing salt concentration.
The phase separation between FS2O4N- anion (salt derived product) and solvent derived products was enhanced by increasing salt concentration.
Mass density distribution of SEI layer compounds
SEI layer properties

## Slide 12
 | Salt concentration |  | 
 | 1 Mol/L | 2.3 Mol/L | 5.3 Mol/L
d (nm) | 4.64 | 4.07 | 3.66
Error | ±0.31 | ±0.26 | ±0.17
 | Salt concentration |  | 
 | 1 Mol/L | 2.3 Mol/L | 5.3 Mol/L
Cavity (FAV) | 0.19 | 0.08 | 0.06
Error | ±0.04 | ±0.01 | ±0.02
Thickness of SEI layers
Cavity of SEI layers
By increasing salt concentration, the SEI layers became thinner and denser.
This results was in good agreement with experimental observation [3].
[3] J. Zheng. Et al., Adv. sci., 4, 1700032 (2017).
SEI layer properties

## Slide 13
By increasing salt concentration, the dissociation products of SEI layers was supressed.
This results was in good agreement with experimental observation [3].
Dissolution of SEI layer products
[3] J. Zheng. Et al., Adv. sci., 4, 1700032 (2017).
Salt concentration effect

## Slide 14
The presence of TMP solvent inside SEI layer decreased by increasing salt concentration.
The presence of FSA- anion increased on SEI film surface by increasing salt concentration.
A pure inorganic layer was formed from FSA- anion and its derived SEI layer at high salt concentration.
Mass density distribution of SEI layer and electrolyte compounds
Pure inorganic layer
Salt concentration effect

## Slide 15
Red Moon methodology showed a high efficiency to reproduce experimental observations regarding SEI layer formation.
The dissolution of SEI layer products was supressed by increasing salt concentration.
SEI layer became thinner and denser by increasing salt concentration.
At high salt concentration, very stable inorganic layer was formed from salt anion and its derived SEI layer, leading to long lifetime of safe LIB during charge-discharge cycles.
Conclusion