## Slide 1
Towards Understanding the Zr-FI Catalyzed Polymerization Reaction
Soumen Saha
Nagaoka Laboratory,
Graduate School of Informatics,
Nagoya University, Japan
20/XI/2018
The 3rd CREST-WS

## Slide 2
Outline
Most Preferable Conformations of Zr-FI Catalyst
      Neutral Form
      Cation
      Ion-pair
      Cation & Monomer
      Ion-pair & Monomer
Ethylene Insertion Polymerization by Zr-FI Catalyst
      Insertion
      Propagation
      Termination
Coordinative Chain Transfer Polymerization (CCTP) by Zr-FI Cation and ZnEt2 (On going)
Anion
Borate
Monomer
Ethylene
Zr-FI Cation
Cation

## Slide 3
One of the most influential breakthroughs were the discoveries of metal-phenoxy-imine (or FI: Fenokishi-Imin Haiishi) catalysts.[1,2]
Neutral Form[1,2,3]
Zr-FI Catalyst
Most Preferable Conformations of Zr-FI Catalyst
[1]. Chem. Rev. 2011, 111, 2363. [2]. Acc. Chem. Res. 2009, 42, 1532. [3]. Saha et al J. Phys. Chem.A, 2018, 122, 2198.
M06/6-31G** (LANL2DZ +f polarization functions: Zr).

## Slide 4
Precatalyst Activation[1]
Zr-FI Cation
Zr-FI Cation
+
+
M06/B1
40 ns
Strategy for Finding The Most Preferable Conformations[2]
B1 = 6-31G** (LANL2DZ +f polarization functions: Zr);
[1]. Acc. Chem. Res. 2014, 47, 2545. [2]. Saha et al J. Phys. Chem.A, 2018, 122, 2198.

## Slide 5
QM Free Energy (kcal/mol)[1] w.r.t. A
0.00 [35%] | 1.81 [4%] | -0.45 [62%]
M06/B2
A and C are equivalent in energy.
0.00 [57%] | 1.33 [11%] | 0.45 [32%]
0.00 [35%] | 1.27 [7%] | -0.39 [57%]
MP2/B2†
Solvent (Heptane)
0.00 [73%] | 3.05 [2%] | 0.83 [26%]
0.00 [58%] | 1.41 [10%] | 0.48 [32%]
MP2/B1
M06/B1
M06/B2†
Zr-FI Cation
B1 = 6-31G** (LANL2DZ +f polarization functions: Zr); B2 = Def2-TZVPP; †M06/B2//M06/B1; ‘Red Colour’ is more stable;
[existing probability: e.g.,
[1]. Saha et al J. Phys. Chem.A, 2018, 122, 2198.

## Slide 6
Ion-pair
Eight different possibilities have been considered.

## Slide 7
Ion-pair
0.00 | 1.18
M06/B1
Free Energy
(kcal/mol)
Altogether 160 different structures have been generated by using MD simulations, and subsequently, QM optimization of these structures has been performed to obtain the most preferable conformation for ion-pair.
Forming Hexa-coordinated Zr system.
B1 = 6-31G** (LANL2DZ +f polarization functions: Zr);
Type | Ɛ (kcal/mol) | r (Å)
Zr-H (CH3) | 0.050 | 2.500
Zr-F | 0.250 | 2.880
The LJ parameters for intermolecular interaction between Zr-cation and anion

## Slide 8
Cation & Monomer
0.00 | 4.17
M06/B1
Free Energy
(kcal/mol)
Using FF parameters of cation A and C, we have generated 80 different structures by using MD simulations.
Most Stable
cis-N/trans-O
trans-N/cis-O
B1 = 6-31G** (LANL2DZ +f polarization functions: Zr);
The LJ parameters for intermolecular interaction between Zr-cation and monomer
Type | Ɛ (kcal/mol) | r (Å)
Zr-CEthylene | 5.000 | 2.973

## Slide 9
Ion-pair & Monomer
240 different structures have been generated by using MD simulations.
Subsequently, QM optimization of these structures has been performed.
Eight possibilities have been considered.

## Slide 10
Ion-pair & Monomer
0.00 | 1.28
M06/B1
Free Energy
(kcal/mol)
Most Stable
Forming Hexa-coordinated Zr-system.
B1 = 6-31G** (LANL2DZ +f polarization functions: Zr);

## Slide 11
Ethylene Insertion Polymerization by Zr-FI Catalyst
Olefin Polymerization Reaction[1,2]
[1] J. Chem. Theory Comput. 2013, 9, 3491. [2]. Osakada, K. Organometallic Reactions and Polymerization, 2014, Vol. 85. [3]. Rappé, A. K.; Skiff, W. M.; Casewit. C. J.; Chem. Rev. 2000, 100, 1435
First Insertion
Second Insertion
Termination
(Hydrogenolysis)
Termination[2,3]
β-hydrogen elimination (β-hydrogen transfer to metal): Unfavorable
β-hydrogen transfer to monomer
Metal-carbon bond cleavage by hydrogen molecule (Hydrogenolysis): Commercial process
#Mt = Zr

## Slide 12
Ethylene Insertion Polymerization by Zr-FI Cation
B1 = 6-31G** (LANL2DZ +f polarization functions: Zr).
[Single point SMD calculation: Solvent= Heptane, + ]
QM Results
β-hydrogen transfer to monomer

## Slide 13
Ethylene Insertion Polymerization by Zr-FI Cation
Red Moon simulation
Cation
Ethylene
Molecules: 1 Cation, 120 ethylene and 480 heptane molecules
Activation energy (Ea) in ‘Gas Phase (QM)’ : 7.06 kcal/mol
Heptane

## Slide 14
Ethylene Insertion Polymerization by Zr-FI Ion-pair
An-
M06/B1 [Heptane]
B1 = 6-31G** (LANL2DZ +f polarization functions: Zr).
[Single point SMD calculation: Solvent= Heptane, + ]
QM Results

## Slide 15
Ethylene Insertion Polymerization by Zr-FI Ion-pair
Red Moon simulation
Cation
Ethylene
Heptane
Molecules: 1 Cation, 1 Anion, 120 ethylene and 480 heptane molecules
Activation energy (Ea) in ‘Gas Phase (QM)’ : 8.34 kcal/mol
Anion

## Slide 16
CCTP by Zr-FI Cation and ZnEt2
Coordinative Chain Transfer Polymerization (CCTP) Reaction
Zr-FI Cation
Ethylene
Monomer
ZnEt2
Chain Transfer Agent

## Slide 17
CCTP by Zr-FI Catalyst and ZnEt2
RC
IC
Pdt.C
RC
TS1
0.00 (0.00)
4.76 (2.46)
IC
-16.22 (-13.77)
TS2
2.51 (2.43)
Pdt.C
-1.74 (-2.06)
Energy (kcal/mol)
6-31G* and LANL2DZ +f polarization functions for Zr (6-31G**; LANL2DZ for Zn and LANL2DZ +f polarization functions for Zr)
18.73 (16.20)

## Slide 18
CCTP by Zr-FI Catalyst and ZnEt2
+
IC
Pdt.C
R
RC
R
RC
0.00 (0.00)
-22.19
IC
-22.52
TS2
-3.42
Pdt.C
-11.92
Energy (kcal/mol)
19.11
M06/6-31G**; LANL2DZ for Zn and LANL2DZ +f polarization functions for Zr.
TS1
-21.50
0.69

## Slide 19
CCTP by Zr-FI Catalyst and ZnEt2
Comparison between 4-membered and 5-membered IC
IC
IC
0.00
8.56
4.54
7.02
M06/6-31G**; LANL2DZ for Zn and LANL2DZ +f polarization functions for Zr.
Relative energy (kcal/mol)
5-membered IC is more stable.

## Slide 20
Future Perspectives
Realizing the polymerization process via Red Moon simulation. Need to include the solvent phase activation energy as well as hydrogenolysis (termination) process in the Red Moon simulation.
To understand the ‘Coordinative Chain Transfer Polymerization’ (CCTP) for Zr-FI catalyst with ZnEt2 by quantum mechanically as well as by Red Moon simulation.
Thank you …