## Slide 1: Mechanisms of Shuttling Polyolefins: A DFT Study
Dr. Sandhya
15/1/2016

## Slide 2: Outline
Aim of the study
General background of the chain shuttling polymerization of dual catalyst with monomers
Scheme of reaction mechanism
Reaction mechanism of propagation step and chain exchange (transmetallation)
Conclusion

## Slide 3
Understand the reaction mechanism of chain shuttling polymerization catalyzed by organometallic catalysts using DFT method
Aim of the study
Background of polyolefin (PO) catalysts for chain shuttling polymerization
Produce hard polymers
Produce soft polymers
cat1
cat2
DFT using Chain Shuttling Polymerization (CSP) Two metal catalysts for polyethylene and copolymer Chain shuttling agent (CSA), ZnEt2 to swap hard and soft polymer chains
No mechanistic information on the complicated CSP process

## Slide 4
Propagation steps of two catalysts
Transmetallation - I of two catalysts
Propagation affords catalysts bearing two different polymers in a same pot.
Transmetallation leads to the formation of four different reactive
species from two different reactants i.e. A, B, C and D
Possible mechanistic step
A
B
C
D

## Slide 5
Transmetallation - II of two catalysts
Propagation steps after transmetallation II
Propagation yields to olefin block polymers
in a single pot.
Transmetallation reaction of catalyst and CSA plays a pivotal role for the exchange of polymers between two catalyst
Continuation-> Possible mechanistic step

## Slide 6: Propagation step for ethylene and Zr catalyst
6.61

## Slide 7
Insertion steps of Hf catalyst- Two cases
Possible mechanistic step

## Slide 8: Stereochemistry of first insertion between Hf and sp3 carbon- Case 1
Method : M06/6-31G(d)and LanL2DZ
 E = 24.0 kcal/mol
 E = 20.77 k cal/mol
 E = 19.4 k cal/mol
 E = 18.84 kcal/mol
Cat3
 E = 17.06 k cal/mol

## Slide 9
 E = 3.49 kcal/mol
 E = 3.38 kcal/mol
 E = 2.82 kcal/mol
 E =4.85 kcal/mol
Stereochemistry of first insertion between
Hf and sp2 carbon- Case 2
 E = -1.54 kcal/mol

## Slide 10
Propagation steps of Hf catalyst- Two cases
Pathway I
Pathway II
Cat3
Cat4

## Slide 11
Real activate catalyst is cat4?
Cat3
cat4
The insertion of octene in cat4 is really required ????

## Slide 12: Reaction energy profile for the insertion step from cat4
Chart: Reaction coordinate
| 1 | 2 | 3 | 4 | 5 | 6 | 7
A | 0 | -19.3883 | -18.6383 | -45.6374 | -60.786 | -51.4689 | -73.2594
C | 0 | -19.3883 | -18.6383 | -45.6374 | -64.1987 | -58.8287 | -75.7609
D | 0 | -19.3883 | -18.6383 | -45.6374 | -58.3925 | -51.7267 | -69.6091
Cat3 + ethylene + octene
Cat4 + octene
R1b + octene

## Slide 13: Transmetallation Reaction process for Zr catalyst
REA
PD1
PD1
PD2

## Slide 14: Solvent corrected Free energy profile for transmetallation reaction on Zr catalyst and CSA
Chart: Reaction coordinate
| Int | reac | ts1 | four cneter | ts2 | pdt
 | 0 | 5.7229 | 7.4962 | -10.2046 | 6.437 | 3.6904

## Slide 15: Transmetallation reaction on Hf catalyst and CSA
TM1Hf
Step 1
RTM1
RTM2a
TM2aHf
PTM2a
RTM2a
Cyclic intermediate formed with the
assistance of phenylic group of N arm
and breaking of cyclic intermediate
require assistance of phenylic group of N arm

## Slide 16: Relative energy profile for the transmetallation of Hf complex with CSA
Chart: Reaction coordinate
| Int | Tsfrom94IRCCM1R | TS | D26TSIRCM1 | TS | D26TSIRCP1
 | 0 | -40.1521 | -38.4267 | -39.6766 | -39.3174 | -41.7505

## Slide 17: Conclusions
In the chain shuttling reaction mechanism, we have proposed all possibilities for the propagations of catalysts as well as the selectivity of monomers using DFT method.
We observed that in situ formed Hf complex can also catalyze the propagation process.
The four-membered ring intermediates between catalyst and ZnEt2 via transmetallation process shows the G of 16 kcal/mol for Zr complex and 2 kcal/mol for Hf complex. We believe that our work could understand the possibilities of reaction mechanism in depth insight.

## Slide 18
Thank you………