## Slide 1: CREST Workshop Uppula Purushotham
Graphene Electrode Dependency on the Reduction Mechanism of Propylene Carbonate in Sodium-ion Batteries: A Density
Functional Theory Study

## Slide 2
Background of Present Research
Recent theoretical studies revealed that electrolyte decomposition is strongly depend on the electrolyte-electrode interactions in presence of the electrode [1-2].
In a study, the one and two-electron transfer processes of EC and FEC on the Li+ adsorbed Si cluster revealed that the two-electron transfer process is more favorable for FEC reductive decomposition on the Si anode. [1]
Thus, to investigate the microscopic mechanism of the SEI film formation, it is essential and inevitable to consider explicitly the electrolyte-electrode interactions.
In the present study we investigate the graphene electrode effect on the reductive decomposition of propylene carbonate.
1. Ma, Y.; Balbuena, P. B. J. Electrochem. Soc. 2014, 161, E3097.
2. Martinez de la Hoz, J. M.; Leung, K.; and Balbuena, P. B. ACS Appl. Mater. Interfaces, 2013, 5, 13457.
Fig. Reduction Mechanisms of Ethylene Carbonate on Si Anodes of Lithium-Ion Batteries

## Slide 3
Method | ILS
B3LYP-D3 | 3.308
B3LYP | 3.712
M06-2X | 3.245
HF | 3.957
Table: Total Energy (TE) in hatrees and Inter Layer Spacing (ILS in Å) of the 3X3 graphene dimer model system at various level of theories with 6-31G(d) basis set.
Optimized geometry of graphene dimer at B3LYP-D3/6-31G(d) level of theory
Experimental Inter Layer Spacing
̴ 3.353 (±0.04) Å1
Theoretical prediction ̴ 3.4 Å2
B3LYP-D3 method provides reasonable Inter Layer Spacing and stable structure than other methods.
1Y. Baskin et al., Phys. Rev. 1955, 100, 544.
2 Cao et al., Nano Lett. 2012, 12, 3783.
Selection of Suitable Method
3.308
C84H36 Point Group: C2h

## Slide 4
Computational Details
All geometry optimizations and frequency analysis in this study was carried out with B3LYP-D3/6-31+G(d) level of theory.
All the calculations were carried out with using Gaussian 09.
= Adsorption energy
Total energy of the optimized substrate-adsorbate structures
Energy of the substrate in free state
Energy of adsorbates in free state
Adsorption energy defined by following equation

## Slide 5
Possible Na Adsorption Sites on Graphene
G-Na1 (-57.443)
G-Na2 (-56.315)
G-Na3 (-53.805)
G-Na4 (-58.640)
G-Na5 (-48.052)
G-Na6 (-48.422)
G-Na7 (-47.461)
G-Na8 (-42.783)
G-Na9 (-47.604)
Fig. Optimized geometries of possible Na adsorption sites on the graphene and their adsorption energies (Eads in kcal/mol) in parenthesis at B3LYP-D3/6-31G(d) level of theory.

## Slide 6
PC Adsorption Sites on Graphene Surface
G-PC-Na-1
G-PC-Na-2
G-PC-Na-3
G-PC-Na-4
G-PC-Na-5
G-PC-Na-6
G-PC-Na-7
G-PC-Na-8
G-PC-Na-9
G-PC-Na-10
Fig. Optimized geometries of possible G-PC-Na+ complex on graphene surface

## Slide 7
Structure | Eads
GPC-Na-1 | -47.513
GPC-Na-2 | -48.614
GPC-Na-3 | -47.951
GPC-Na-4 | -46.180
GPC-Na-5 | -46.808
GPC-Na-6 | -33.063
GPC-Na-7 | -33.369
GPC-Na-8 | -33.404
GPC-Na-9 | -34.494
GPC-Na-10 | -33.919
Table: Adsorption energy (Eads in kcal/mol) for possible PC adsorption sites on Graphene at B3LYP-D3/6-31G(d) level of theory.
Most Stable PC Complex
Fig. Optimised structure of G-PC-Na-2 complex
2.231
3.374

## Slide 8
Optimized Geometries of PC After One and Two Electron Reduction
G-PC-Na+ (Eads = -48.614 kcal/mol)
G-PC-Na (Eads = -55.378 kcal/mol)
G-PC-Na- (Eads = -104.150 kcal/mol)
2.231
3.374
3.264
2.274
3.113
2.324
3.234
Reaction energies (ΔΕ)
G-PC-Na+ → G-PC-Na : -100.602 kcal/mol
G-PC-Na+ → G-PC-Na- : -41.759 kcal/mol
The one electron reduction is favorable than two electron reduction. However negative reaction energy shows that it can also possible.
Fig. Optimized geometries of G-PC-Na+ complex, one electron reduction complex (G-PC-Na) and two electron reduction complex (G-PC-Na- )

## Slide 9
1
2
3
4
5
6
7
The Possible Bond Cleavages in the PC
After one electron reduction : C2-O3, C2-O1, C4-O3 and C5-O1
After two electron reduction : C5-O1/C4-O3 together
After one electron reduction C4-O3 and C5-O1 bond cleavage products and C5-O1/C4-O3 bonds cleavage product after two electron reduction has been investigated. However, the C2-O3 and C2-O1 bond cleavage products are not found.
PC molecule with possible bond cleavages
C4-O3 bond
C5-O1 bond
G-PC-Na-2 (Eads = -28.672 kcal/mol)
G-PC-Na-1 (Eads = -30.021 kcal/mol )
Fig. One electron reduction products
C4-O3 bond cleavage is favorable with lower reaction energy (-17.714 kcal/mol than C5-O1 bond cleavage (19.139 kcal/mol). The positive reaction energy shows that this bond cleavage is not thermodynamically favorable.
2.274
3.193
3.384
2.228
G-PC-Na (Eads = -55.378 kcal/mol)
3.264
2.274
3.113

## Slide 10
Relative energy (ΔΕ in kcal/mol)
Figure: Potential energy (ΔΕ in kcal/mol) profile for the reductive decomposition process of Na+- PC on the graphene surface.
Propylene Carbonate Reaction Scheme and Energy Profile
Chart: 
| PC_IN1 | PC_IN2 | PC_TS3 | PC_IN4 | PC_IN5 | PC_TS6 | PC_IN7 | PC_IN8
 | 1.255e-05 | -93.9091 | -65.4959 | -76.1925 | -124.2828 | -90.3249 | -102.0301 | -223.5651
Activation barrier energy for the cleavage of C4-O3 bond through G-PC-TS3 is 28.413 kcal/mol.
G-PC-IN5 complex is more stable than other intermediates.
The present reaction profile is also similar to PC-Na+ complex profile with out graphene, however, the activation energy is significantly increases in the present study.
It reveals that graphene surface showed significant effect on the decomposition of PC molecules.
28.413
G-PC-IN1
G-PC-IN2
G-PC-TS3
G-PC-IN5
G-PC-TS6
G-PC-IN7
G-PC-IN8

## Slide 11
Optimized Geometries and Adsorption Energy
Fig. Optimized geometries with representative bond lengths and adsorption energies (Eads in kcal/mol) in parenthesis.
After one electron reduction G-PC-IN2 adsorbed more strongly than other molecules. However, after dissociation of C4-O3 bond, weak adsorption appeared in the G-PC-IN4.
This reveals that PC electrolyte molecules show strong interaction with graphite surface than dissociative molecules after one electron reduction with high adsorption energy and short C-O distance.
G-PC-IN1 (Eads = -48.614)
2.231
3.374
G-PC-IN2 (Eads = -55.378)
3.264
2.274
3.113
G-PC-TS3 (Eads = -43.661)
2.188
3.255
2.274
3.193
G-PC-IN4 (Eads = -28.672)

## Slide 12
2.202
3.246
Optimized Geometries and Adsorption Energy
After 2 electron reduction G-PC-IN5 showed strong adsorption than other complexes.
The propene molecule moved away from the graphene surface in final product thus, it showed very low adsorption energy.
Overall, G-PC-IN5 showed strong interaction with graphene surface, which is also more stable complex with lower energy on the potential energy barrier.
Two electron reduced complexes are more strongly adsorbed on the graphene surface in comparison to one electron reduction complexes.
2.264
3.285
1.900
2.226
3.262
3.174
2.208
3.693
G-PC-IN5 (Eads = -89.501)
G-PC-TS6 (Eads = -49.776)
G-PC-IN7 (Eads = -66.784)
G-PC-IN8 (Eads = -35.209)

## Slide 13
The lower reaction energy and activation energy reveals that C5-O1/C4-O3 bonds cleavage is possible in two electro reduction products.
Along with C4-O3 bonds cleavage in one electron reduction decomposition, C5-O1/C4-O3 bonds cleavage can be possible in the two electro reduction of PC decomposition.
Two Electron Reduction Products
3.103
2.174
2.203
2.324
3.234
3.767
G-PC-Na- (Eads = -104.150 kcal/mol)
G-PC-Na-3 (Eads = -50.085 kcal/mol)
C5-O1/C4-O3 bonds
G-PC-Na- TS-(Eads = -71.267 kcal/mol)
2.319
3.199
Activation barrier energy 34.978 kcal/mol
Reaction energy
-15.534 kcal/mol

## Slide 14
In the present study we investigate the graphene electrode effect on the reductive decomposition of propylene carbonate.
B3LYP-D3/6-31+G(d) method provides reasonable Inter Layer Spacing for graphene dimer than various other methods.
The conformer with Na+ ion captured between two graphene layers is more reasonable than other conformers.
The one electron reduction is favorable than two electron reduction. However negative reaction energy shows that both the reductions are possible.
In one electron reduction C4-O3 bond cleavage is favorable with lower reaction energy (-17.714 kcal/mol than C5-O1 bond cleavage (19.139 kcal/mol).
The lower reaction energy and activation energy reveals that C5-O1/C4-O3 bonds cleavage is possible in two electro reduction products.
Along with C4-O3 bonds cleavage in one electron reduction decomposition, C5-O1/C4-O3 bonds cleavage also possible in two electro reduction of PC decomposition.
Conclusions