## Slide 1: CREST Workshop Dr. Uppula Purushotham
Mechanistic Study of DiFluoro Ethylene Carbonate as Electrolyte Additive for Rechargeable Na Batteries : A Hybrid MC/MD Simulation Study

## Slide 2
Background of Present Research
According to the experimental results[1], fluoroethylene carbonate (FEC) is the only an effective additive for Na-ion battery among the FEC, difluoroethylene carbonate (DFEC), vinylene carbonate (VC) and ethylene sulfite (ES).
The FEC addition improved the cycle performance by decreasing the irreversible capacity to form the SEI film. In case of DFEC, performance is decreased by lowering reversible capacity.
In the present study we would like to investigate the origin of mechanism to SEI film formation in DFEC additive PC electrolyte Na-ion battery.
Figure : Reversible capacity versus cycle number plot of PC electrolyte Na-ion battery.
[1] S. Komaba et al., ACS Appl. Mater. Interfaces, 3, 4165 (2011).

## Slide 3
Scheme: Schematic representation of two electron reduction mechanism of PC
Chart: 
| PC_Na + Na+ + 2e | IN2 + Na+ + e | TS1+ Na+ + e | IN3 + Na+ + e | IN4+Na | Product
dE | 0 | -84.678 | -72.982 | -99.566 | -133.743 | -247.432
dG | 0 | -50.134 | -39.981 | -68.433 | -66.574 | -235.645
PC-IN5
ΔΕ
ΔGsol
Figure: Potential energy (ΔΕ in kcal/mol) and gibbs free energy (ΔGsol in kcal/mol) profile for the two electron reductive decomposition process of Na+- PC.
Reduction Mechanism of PC
The two electron reductive mechanism of Na+- coordinated PC gives Na2CO3 and alkene as final products. This mechanism is similar to previously proposed for Li+- coordinated EC and PC.
PC is directly reduced and formed a stable product (PC-IN2), which gives an open anion radical due to the cleavage of C-O bond, through transition state (PC-TS3) with a barrier energy of 11.696 kcal/mol.
The PC-IN4 undergoes further reduction by accepting second electron and form PC-IN5. The addition of Na+ ion to PC-IN5 form Na2CO3 and propene gas and this step of the reaction proceeds without reaction barrier.

## Slide 4
Reduction Mechanism of DFEC
Scheme: Schematic representation of possible one and two electron reduction mechanism of DFEC
Initially DFEC reduce by accepting one electron and form DFEC-IN2. Further this product can dissociate in to two different pathways. One is dissociation of C(4)-O(3) bond which give Na2CO3 and DiFluoro alkene. Another one is the dissociation of C(2)-O(3) bond cleavage yield DFEC-IN12 as intermediate, this also dissociate in two ways one is cleavage of C(5)-O(6) and another is C(2)-O(6) bond.

## Slide 5
Figure : Potential energy (ΔΕ in kcal/mol) at B3LYP/6-311++G(d,p) level of theory and gibbs free energy (ΔGsol in kcal/mol, underlined) at SMD-B3LYP/6-311++G(d,p)//B3LYP/6-311++G(d,p) level of theory for possible reductive decomposition process of Na+-DiFluoro ethylene carbonate.
Potential Energy Profile of DFEC
Chart: 
| R1 | IN-2 | TS-3 | IN-4 | IN-5 | TS-6 | IN-7 | IN-8
 | 0 | -87.092 | -71.967 | -104.074 | -111.347 | -109.766 | -129.214 | -159.686
 | -87.092 | -64.409 | -93.276 | -84.347 | -86.663 | -63.845 | -57.896 | -101.98
 | -63.846 | -53.06 | -59.774 | -124.387 | -134.16
 | 0 | -53.098 | -39.366 | -71.173 | -42.287 | -41.498 | -62.405 | -101.582
 | 0 | -53.098 | -31.659 | -59.499 | -49.798 | -53.556 | -13.473 | -8.882 | -54.565
 | 0 | -53.098 | -31.659 | -59.499 | -49.798 | -53.556 | -13.473 | -5.379 | -31.609 | -59.912 | -78.749
Route 1
Route 2
Route 3
Relative energy in kcal/mol

## Slide 6
After one electron reduction of DFEC the C(4)-O(3) bond dissociation occurs via DFEC-TS3 with 15.125 kcal/mol activation energy barrier.
In Route 2 the homolytic fission of C(2)-O(3) bond form a radical anion (DFEC-IN9) with 22.683 kcal/mol activation energy barrier. Further dissociation of DFEC-IN12 via C(5)-O(6) bond proceeds with lower energy than C(2)-O(6) bond dissociation (Route 3).
In the DFEC mechanism C(4)-O(3) bond cleavage is favorable than C(2)-O(3) bond dissociation, thus Route 1 is favorable with lower reaction barrier.
The reduced product (PC-IN2) form an open anion radical due to the cleavage of C-O bond, through transition state (PC-TS3) with a barrier energy of 11.696 kcal/mol.
Route 1 is favorable with lower reaction barrier, thus we have considered route 1 for MC/MD simulation. DFEC is less reactive than PC with its higher activation energy.
We have carried out the MC/MD simulations in two different situations such as one where PC and DFEC are reactive. Second is in the real situation more intact DFEC molecules present in the electrolyte during SEI film formation. Thus, to evaluate the intact DFEC effect we have also carried out the MC/MD simulations where DFEC is non-reactive.
Conclusions

## Slide 7
Simulation Model and Reaction Scheme
1.1M NaPF6 PC electrolyte
(with 10 vol% DFEC)
PC: 850
Na+: 87
PF6-: 85
DFEC: 115
Carbon anode
NaPF6 electrolyte with DFEC
y
z
x
+ e-, + Na+
+
+ NaPC
Na2CO3
+ e-, + Na+
PC
NaPC
C3H6
(CH3CHCH2OCO2Na)2
Na2DMBDC
+
+
PF3
3NaF
+ 2e-, + 3Na+
+
PF6
DFEC
+ 2e-, + Na+
Na2CO3
+
C2H2F2
DFEC
+ 2e-, + Na+
Na2CO3
+
C2H2F2
In intact DFEC added system

## Slide 8
SEI Film Formation Processes
NaPC
Na2DMBDC
Na2CO3
NaF
Species
C2H2F2
Intact DFEC-added electrolyte
(a) 100 cycle
(b) 500 cycle
(c) 1500 cycle
DFEC-added electrolyte
(a) 100 cycle
(b) 500 cycle
(c) 1500 cycle
(a) 100 cycle
(b) 500 cycle
(c) 1500 cycle
FEC-added electrolyte
Intact DFEC showed significant effect on the formation of SEI film.
The addition of DFEC results roughened SEI film surface compare to the SEI film formed in the FEC-added system.

## Slide 9
(b) Intact DFEC added
(a) FEC added
(c) DFEC added
Comparison of Smoothness of SEI Films
DFEC-added PC electrolyte systems resulted roughened surface structure of SEI film in contact with the electrolyte compare to the FEC added system.

## Slide 10
Mass Density Distributions of Reaction Products in SEI Film
The width of SEI film in FEC and DFEC added systems is almost similar.
Near the surface of SEI film mass density of organic and inorganic products are less in DFEC added system. This reflects the poor aggregation of reaction products near the surface of SEI film, which results roughened surface .
The mass density decrease of dimers around 15Å in DFEC added system shows the uneven density distribution of organic salts in the SEI film.
Chart: 
Figure. Mass density distribution of the reductive products in the SEI films.
41 Å
Chart: 
| 1 | 3 | 5 | 7 | 9 | 11 | 13 | 15 | 17 | 19 | 21 | 23 | 25 | 27 | 29 | 31 | 33 | 35 | 37 | 39 | 41 | 43 | 45 | 47 | 49 | 51 | 53 | 55 | 57 | 59 | 61 | 63 | 65 | 67 | 69 | 71 | 73 | 75 | 77 | 79
PC3 | 0 | 0 | 0 | 0 | 0.01274 | 0.112 | 0.051392 | 0.11125 | 0.06455 | 0.11249 | 0.060764 | 0.032466 | 0.056585 | 0.10446 | 0.029528 | 0.014542 | 0.022196 | 0.025713 | 0.01313 | 0.0090687 | 0.001869 | 5.0423e-05 | 0 | 3.2238e-05 | 3.2238e-05 | 3.2238e-05 | 3.2238e-05 | 3.2238e-05 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC4 | 0 | 0 | 3.3064e-06 | 0.15727 | 0.36365 | 0.9279 | 0.67048 | 0.63206 | 0.82275 | 0.96559 | 0.81919 | 0.72543 | 0.46496 | 0.47503 | 0.21784 | 0.18973 | 0.076988 | 0.067586 | 0.059112 | 0.049187 | 0.019003 | 3.3064e-06 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
N2C | 0 | 0 | 0.023077 | 0.16314 | 0.70668 | 0.6527 | 0.88851 | 0.75337 | 0.56333 | 0.3069 | 0.22147 | 0.18001 | 0.057542 | 0.042325 | 0.0284 | 0.0063 | 0.0007 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
F | 0 | 0 | 0 | 0 | 0 | 0.0016091 | 0.0039254 | 0.0013527 | 0.00142 | 0 | 0 | 0.0028 | 0.0027 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
TDF | 0 | 0.0063592 | 0.21732 | 0.061584 | 0.068679 | 0.037524 | 0.025184 | 0.014891 | 0.003479 | 0.007592 | 0.0086901 | 0.002858 | 9.0548e-05 | 0 | 0 | 0 | 4.1536e-06 | 4.1536e-06 | 4.1536e-06 | 4.1536e-06 | 4.1536e-06 | 4.1536e-06 | 4.1536e-06 | 4.1536e-06 | 2.1045e-05 | 5.5381e-07 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
[gcm-3]
z [Å]
Na2DMBDC
NaPC
Na2CO3
NaF
C2H2F2
Chart: 
| 1 | 3 | 5 | 7 | 9 | 11 | 13 | 15 | 17 | 19 | 21 | 23 | 25 | 27 | 29 | 31 | 33 | 35 | 37 | 39 | 41 | 43 | 45 | 47 | 49 | 51 | 53 | 55 | 57 | 59 | 61 | 63 | 65 | 67 | 69 | 71 | 73 | 75 | 77 | 79 | 81
PC3 | 0 | 0 | 0 | 1.7359e-05 | 0.035554 | 0.13241 | 0.1273 | 0.0748 | 0.048959 | 0.078286 | 0.1152 | 0.075188 | 0.036829 | 0.036238 | 0.024361 | 0.008381 | 0.0031965 | 0.0051002 | 0 | 0 | 8.2661e-07 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC4 | 0 | 0 | 0.043827 | 0.12215 | 0.26633 | 0.66146 | 0.66642 | 0.91526 | 0.91518 | 0.908 | 0.76263 | 0.85641 | 0.51519 | 0.27524 | 0.17138 | 0.090933 | 0.1081 | 0.047323 | 0.038173 | 0.0069782 | 0 | 1.1572e-05 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
N2C | 0 | 6.9932e-07 | 0.04281 | 0.21515 | 0.56524 | 0.59004 | 0.54242 | 0.50122 | 0.39433 | 0.24608 | 0.12603 | 0.028047 | 0.046355 | 0.0040896 | 0.013989 | 0.012159 | 0.00080632 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
F | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
z [Å]
[gcm-3]
NaPC
Na2DMBDC
Na2CO3
NaF
39 Å
z [Å]
(b) Intact DFEC added
(a) FEC added
(c) DFEC added
NaPC
Na2DMBDC
Na2CO3
NaF
39 Å
[gcm-3]

## Slide 11
Figure. Change in the concentration of the reductive products with the MC/MD cycles.
The addition of DFEC increased the number of MC/MD cycles to form SEI film than FEC-added system.
The number density of inorganic salts (CO3-2) are increased in the DFEC added system, where the number density of NaF molecules are increased in the FEC-added system.
In DFEC added system decomposition of PC molecules(151) is less than FEC added system(162). It indicates that the intact DFEC molecules suppress the PC electrolyte decomposition.
Decomposition of more FEC molecules (29) than DFEC molecules (18) reveals the significant contribution of FEC decomposition products in the SEI film formation.
Change in Number Densities of Reaction Products
MC/MD cycles
MC/MD cycles
(b) Intact DFEC added
(a) FEC added
(c) DFEC added
MC/MD cycles

## Slide 12
Chart: 
| 0 | 100 | 200 | 300 | 400 | 500 | 600 | 700 | 800 | 900 | 1000 | 1100 | 1200 | 1300 | 1400 | 1500 | 1600 | 1700 | 1800 | 1900 | 2000
FEC | 33 | 30 | 25 | 22 | 19 | 15 | 12 | 12 | 11 | 11 | 11 | 11 | 11 | 11 | 11 | 11 | 11 | 11 | 10 | 11 | 10
DFEC | 27 | 25 | 24 | 22 | 21 | 18 | 13 | 12 | 11 | 11 | 11 | 10 | 11 | 11 | 11 | 12 | 11 | 11 | 11 | 11 | 11
MC/MD cycles
Number of DFEC/FEC residues
Figure. The number of residues present with in the 30Å width from graphite surface in DFEC and FEC added PC electrolyte during the SEI film formation.
Less number of DFEC molecules near the anode surface during initial cycles in comparison to FEC decrease the decomposition of DFEC molecules during the SEI film formation.
Thus, in DFEC added system the SEI film formation mainly occurs by the decomposition products of PC electrolyte.
The more number of DFEC molecules after 300 cycles can decrease the accumulation of reaction products during the SEI film formation.
Change in the Number of Molecules during SEI film Formation

## Slide 13
Cavity Size
Systems | FAV
PC | 0.311 (0.023)
FEC added PC | 0.282 (0.020)
DFEC added PC | 0.335 (0.026)
Intact DFEC added PC | 0.350 (0.016)
Table: The fractional accessible free volume (FAV) for the Na+ ion in the 30Å width of SEI film of PC, FEC added PC, DFEC added PC and intact DFEC added PC electrolytes, along with standard deviation in parenthesis.
The FAV of DFEC added PC electrolyte SEI films is considerably large compare with the van der Waals radius of Na+ 1.86Å.
Intact DFEC additive PC electrolyte resulted larger cavities than other systems.
After small amount of DFEC decomposition (DFEC added PC) also the cavity size is larger than FEC added system.
This results indicates that the in real system the intact DFEC molecules present in the SEI film can responsible for poor aggregation of reaction products and the larger cavities.

## Slide 14
Coordination of Additives with Inorganic Molecules
Table: The averaged coordination number in 5Å distance of additives with the inorganic molecules is calculated with in the 20Å width of SEI film formed after addition of FEC and DFEC additives.
Systems | With in 20Å
FEC added PC | 2
DFEC added PC | 4
The clustering of DFEC molecules with inorganic molecules is more favorable in the DFEC added PC electrolyte system. This clustering reduce the aggregation between inorganic and organic products in the SEI film formation. Finally, it results to formation of larger cavities.

## Slide 15
Role of DFEC Residues in the SEI film Formation
100 MC/MD cycles
500 MC/MD cycles
NaPC
CO3-2
DFEC
Na+
NaPC
DFEC
CO3-2
Na2DMBDC
Intact DFEC molecules coordinate with reaction products during the SEI film formation.
DFEC also enhance the clustering of inorganic molecules which can be responsible for larger cavity sizes.
Figure : Typical snapshots of SEI film formation process during SEI film formation.

## Slide 16
Conclusions
To gauge the effect of DFEC on the formation of SEI film, we have performed the MC/MD simulations on two model systems such as intact DFEC added PC which resembles real situation and DFEC added PC where DFEC also dissociate along with PC electrolyte.
Intact DFEC and reactive DFEC added systems form SEI film with similar width.
It is evident from the number analysis that intact DFEC molecules suppress the PC electrolyte decomposition.
Decomposition of more FEC molecules than DFEC during the SEI film formation reveals the higher contribution of FEC molecules in the SEI film formation than DFEC molecules.
Intact DFEC molecules in the SEI film can responsible for poor aggregation of reaction products which results larger cavities.
The clustering of DFEC molecules with inorganic molecules is more favorable in the DFEC added PC electrolyte system. This clustering reduce the aggregation between inorganic and organic products in the SEI film formation.
Finally, the inefficient aggregation of reaction products in the DFEC-added system results roughened surface structure and larger cavities in the SEI film compare to FEC added system.

## Slide 17
THANK YOU