## Slide 1
Molecular Dynamic Simulation on the Ansa-Zirconocene Propylene Complexes and the Product after First Insertion of Propylene
K. S. Sandhya and N. Koga
Dec. 3, 2014

## Slide 2
Insertion of propylene into Zr-P(polymer end) bond
isotactic
If one of them repeatedly occurs, the isotactic polymer is obtained.
primary
insertion
secondary
insertion

## Slide 3
Force field for reactants and product.
    Models in MD simulation for ansa-zirconocene complexes
    ESP atomic charges using CHELPG and MK schemes for reactants and product.
    Failure of CHELPG charges for product.
MD simulation of propylene complexes and product.
    Rotation of propylene
MD simulation of insertion product (isobutyl complex)
Future plan
Summary
Contents

## Slide 4
η5 Cp ring and four Zr/4 centers
η5 Cp ring and one Zr
η1 Cp ring and one Zr
Three different models are created for MD simulation studies.
A small tetrahedron of four Zr/4 centers to include 1,3-repulsive interaction (Brintzinger et al. J. Mol. Struct., 485-486, 409 1999)
0.001Å
2nd model
1st model
3rd model
The results obtained with this model was presented in the last workshop.
η1 model with one Zr is neglected due to the lack of various parameters for indenyl ligands and hence shown distorted structures during the simulations.
Different models of ansa-zirconocene complex

## Slide 5
Atom types are different for reactants and product.
For the third model, two dummy atoms are inserted into the centroids of the Cp ligands and one dummy atom is inserted to the center of the double bond of propylene.
du
du1
du
ca
2nd model
3rd model
product
hb
hd
c9
c2
C3
C5
C4
ha
ca
Description :
ca: aromatic carbon
c5: cyclopentadienyl carbon
c2,c9: unsaturated sp2 carbon in propylene
ha
ha
ha
du: dummy atoms at centroids of Cp rings
du1: dummy atom at centroid of propylene C=C bond
propylene complex
Atom types used for the A complex and product for different models
ha: hydrogen in unsaturated as well as aromatic carbon.
hb and hd: hydrogens bonded with unsaturated carbon c2
ca
hc
C3
C3
C3
C2
C5

## Slide 6
Bond | K1 | Distance [Å]
zr-c2 | 204(200) | 2.58 (2.60)d
zr-c9 | 258 | 3.011
c9-ha | 396 | 1.094
c2-hb(c2-hc) | 396(340) | 1.091(1.090)d,b
c2-hd | 399 | 1.093
c9-c2 | 590 | 1.324
c9-c3 | 314 | 1.481
zr-cp | 219 | 2.430
c4-ha | 367 | 1.099
zr-c4 | 150 | 2.242
Angle | K2 | Angle [º]
si-c5-zr | 7.50 | 98.85
zr-c2-hb | 1.28 | 103.10
zr-c2-hd | 2.09 | 86.42
zr-c9-ha | 3.96 | 95.58
zr-c2-c9 | 4.18 | 94.29
zr-c9-c2 | 0.03 | 59.07
zr-c9-c3 | 2.09 | 117.7
Dihedral angle | Multi-plicity | K3 | γ [º] | Perio-dicity, n
c4-zr-c2-c9 | 1 | 4.5 | 16.23 | 1
c4-zr-c9-c3 | 1 | 1.8 | 47.44 | 1
hc-c4-zr-c2 | 1 | 0 | 0 | 2
hc-c4-zr-c9 | 1 | 0 | 0 | 2
hc-c4-zr-c5 | 1 | 0 | 0 | 2
hc-c2-c3-c3b | 9 | 1.4 | 0 | 3
c2-c3-c3-hcb | 9 | 1.4 | 0 | 3
Bond | K1 | Distance [Å]
c3-hc | 345a | 1.09a
c4-hc | 340b | 1.09b
zr-c5 | 137b | 2.38b
zr-c4 | 200b | 2.26b
si-c5 | 506b | 1.90b
zr-zr | 500b | 0.001b
Angle | K2 | Angle [º]
c5-zr-c2 | 40b | 105.0b
hc-c4-hc | 35b | 109.5b
si-c3-hc | 35a | 109.5a
c3-si-c3 | 40a | 109.5a
zr-c4-hc | 150b | 109.5b
si-c5-c5 | 40a | 126.0a
c5-c3-c3 | 70b | 109.5b
c5-si-c5 | 70a | 109.5a
c3-si-c5 | 22a | 109.5a
Atom type | van der Waals depth,ε [kcal/mol] | van der Waals radius, [Å]
zr | 1.000b | 0.000b
si | 1.908b | 0.086b
c4 | 1.910b | 0.130b
a. Bosnich et. al., J. Am. Chem. Soc., 1995, 117, 1352-1368
b. Brintzinger et.al., J. Mol. Struc., 1999, 485-486, 409-419, Organometallics, 2000, 19, 3597 3604
Other parameters are also taken from
d Values in parenthesis values are
for product.
Parameters taken from literature
Force field parameters for reactants and product
Force field parameters for reactants and product created (DFT calculations)

## Slide 7: Structural comparison between DFT optimized geometry and MD minimized geometry (A complex)
Structural Parameters of A | DFT | MD (NPA charges) | MD (CHELPG charges) | MD (MK charges)
zr-c2 | 2.58 | 2.64 | 2.61 | 2.58
zr-c9 | 3.01 | 3.03 | 3.01 | 3.02
zr-c4 | 2.24 | 2.35 | 2.29 | 2.25
zr-cp | 2.43 | 2.41 | 2.43 | 2.40
zr-c2-hb | 104 | 104 | 104 | 102
zr-c2-hb | 85 | 73 | 80 | 74
zr-c9-ha | 95 | 125 | 95 | 93
zr-c9-c3 | 119 | 89 | 120 | 120
c4-zr-c2-c9 | –20 | –20 | –19 | –20
Atom type | Atomic charges |  | 
 | NPA | CHELPG | MK
zr | 0.937 | 1.237 | 0.6264
c4 | –0.456 | -1.123 | -0.598
c2 | -0.226 | -0.584 | -0.3847
c9 | 0.75 | -0.025 | 0.2248
si | 0.666 | 1.850 | 0.9372
MD minimized geometry obtained using CHELPG and MK atomic charges are more similar to DFT structure.

## Slide 8
One catalyst, one propylene and 270 pentane solvent
GAFF and ESP charges are used
  Basis set for Zr LanL2DZ and for all other atoms 6-31++G(d,p)
  CHELPG and MK methods were applied to calculate ESP charges for the complexes of the optimized geometries of reactants and product. However, MK method gave the more proper charges (next slide) and hence further calculations are proceeded with MK charges.
Periodic boundary conditions are applied
NPT-MD for 20ps (300K and 1atm) for relaxation
NVT-MD (300K) simulation time in one MD cycle was 1ps
Computational details

## Slide 9
Using CHELPG charges the systems are destroyed during MD simulation regardless of the presence or the absence of counter anion, Cl-. The same problem was encountered in the initial complex without propylene.
The main reason for this is that the highly positively charged Zr contacts with highly negatively charged chlorine.
In the absence of counter anion, the negative charge on the hydride (-0.108) of CH3 in the propylene will contact with Zr and destroy the system.
MD simulation for the isobutyl ansa-zirconocene complex (the product of the first insertion of propylene to type A complex )
Negative charge
–0.108
+1.024
on Zr
CHELPG charges
M06/ 6-31++G(d,p)
Positive charge
+0.121
+0.553
on Zr
MK charges
M06/ 6-31++G(d,p)

## Slide 10
c9-c2-zr-c4
η5 model with one Zr atom
At 20ps
This figure clearly shows the presence of stable structure where the averaged dihedral angle is –67˚ different from DFT structure.
Dihedral angle
MK charges
MD simulation for the propylene ansa-zirconocene complex (A complex)
–66.02
c9
c2
c4
ϕ

## Slide 11
100 K
400 K
At 100 K as well as at 400 K the meta stable structure was observed.
MK charges
MD simulation for propylene ansa-zirconocene complex (A complex): Longer time and various temperatures

## Slide 12
This shows the presence of metastable structures.
The average dihedral angle is –62˚.
This orientation of the propylene ligand is similar to that in A complex.
MK charges
Dihedral angle
c9-c2-zr-c4
MD simulation for the propylene ansa-zirconocene complex (C complex)
At 20ps
–49.92
c9
c2
c4
ϕ

## Slide 13
B complex changed to A complex
D complex changed to C complex
B and D are not stable and may not under go further reaction for first insertion.
Averaged dihedral angle is 17˚.
MK charges
MD simulation for the propylene ansa-zirconocene complex (B and D complexes)
D
C
B
A
Averaged dihedral angle is 10˚.

## Slide 14: DFT studies on rotation of propylene
0.83
TS1
2.35
TS2
–0.27
metastable
0.00 kcal/mol
A
0.59
B
0.13
metastable
2.43
TS1
2.35
TS2
0.00 kcal/mol
C
0.41
D
donation
back-donation
In ZrIV (d0) alkene complex, electron donation is responsible for the alkene coordination, whereas there is no back-donation which would prohibit the rotation.

## Slide 15
hc1
hc2
This MD graph clearly indicates that the cαcβ bond of isobutyl rotating along its axis
A close interaction of H with metal is observed. The average distance is 2.75 Å.
(In DFT, this value is 2.27 Å)
zr-hc1
zr-hc2
With the MK method, the atomic charge on Zr (0.55) is smaller than that by other methods (appr. 0.9 and 1.02) and the systems were not destroyed.
η5 Cp ring and one Zr
MD simulation for the isobutyl ansa-zirconocene complex (the product of the first insertion of propylene to type A complex )

## Slide 16
Trial and error method for the suitable models for MCMD simulation
MCMD for the propylene insertion reaction.
Future plan
Summary
Three models ((1)η5 and four Zr (2) η5 and one Zr (3) η1 model with one Zr ) were used for the MD simulation.
When CHELPG charges for the product as well as reactant complex without propylene were used, the systems were destroyed by counter anion (Cl-).
Therefore, MK charges were used in MD simulation for all systems and will be used in future work, since the systems are not destroyed by Cl- ion in MD simulation with MK charges.