## Slide 1
Masayoshi Takayanagi
Graduate School of Information Science, Nagoya University
Collaboration with “Hyper-nano-space” CREST and its Molecular Technological Basis
超空間CRESTと分子技術CRESTの協働
2014/July/28

## Slide 2: Hyper-nano-space CREST （超空間CREST）
CREST: Creation of Innovative Functional Materials with Advanced Properties by Hyper-nano-space Design
超空間制御に基づく高度な特性を有する革新的機能素材等の創製
Creation of Functional Polymer Materials in Tailor-Made Nanospaces
テーラーメイドナノ空間設計による高機能高分子材料の創製
Research Supervisor
Tohru Setoyama (Executive Officer Fellow, Mitsubishi Chemical Corporation)
Research Director Takashi Uemura (Associate Professor, Kyoto University)
Collaborator
M. Nagaoka M. Takayanagi
Other three groups

## Slide 3: Hyper-nano-space CREST （超空間CREST）
Strategic Objective
Creation of new functional materials by means of technology for controlling spaces and gaps in advanced materials in order to realize selective material storage, transport, chemical separation, and conversion, etc.
Other groups: application oriented projects
Zeolite membrane for separation & catalyst
Matsukata group, Waseda Univ.
Catalyst development for polar polypropylene
Nozaki group, Univ. of Tokyo
All-solid-state lithium ion battery
Teshima group, Shinshu Univ.

## Slide 4: Hyper-nano-space CREST （超空間CREST）
To improve Japanese industrial competitiveness, we have to create high-quality products which is not easily copied by other countries.
To this end, it is necessary to understand fundamental science under the technology.
During the 5.5 years project, I expect you to climb the “commercialization mountain” to the halfway point.
Research Supervisor
Tohru Setoyama
Commercialization
CREST
Handover to the following projects
Ideas, seeds
In contrast to the three groups for application, we expect Uemura group to promote fundamental science.

## Slide 5: Target of Uemura group
Living cells control reactions very precisely (e.g. DNA/protein synthesis)
By utilizing artificial nano-size spaces in PCPs (MOFs), create brand-new functional polymers.

## Slide 6: Porous Coordination Polymer (PCP) or Metal Organic Framework (MOF)
Organic ligands
+
Metal ions
Cu2+
Zn2+
…
Porous Coordination Polymer (PCP)
/ Metal Organic Framework (MOF)
→
Absorb guest molecules inside pores

## Slide 7: Porous Coordination Polymer (PCP) or Metal Organic Framework (MOF)
Wide variety of framework structures of PCPs
Large surface area of pores → efficient absorption of guest molecules, e.g. promising for H2 storage

## Slide 8: Polymerization in PCP pores
Control polymer conformations inside PCPs.
& Use PCP pores for polymerizations.
Create high-value plastic
heatproof
temperature
price
Insert monomers & radical polymerization
Remove PCP by chelate, acid, or base
High heat resistance polymer

## Slide 9: Target of Uemura group
Nagaoka group: Computational analysis

## Slide 10: Research goal of Nagaoka group
It is difficult to experimentally investigate behaviors of guest molecules inside PCP pores.
By using molecular simulation technique, we investigate various behaviors of guest molecules such as structures of each molecule, accumulated structure of multiple molecules, and diffusion.
Polymerization processes inside PCP pores are simulated by the hybrid MC/MD method to obtain information on the effects of PCP nanopores for the polymerization reactions.
→ Propose promising organic ligands of PCP for the polymerization.
Collaboration with the “Molecular Technology” CREST with MC/MD method

## Slide 11: Previous computational studies on PCPs in Nagaoka group with Uemura group 長岡グループが過去に行った 多孔性金属錯体の理論研究

## Slide 12: Analysis of guest molecules in PCP pores
All-atom models
（QM or MM）
Molecular simulation (MD or MC)
Experimental studies
* Angew. Chem. Int. Ed. 2006, 45, 4112
All-atom model building to explain experimental results.
Analysis of structures of guest molecules by MD simulations.
Analysis of thermodynamic properties (e.g. average adsorption energy, average number of adsorbed molecules) by grand canonical MC (GCMC) simulations.
PCP structures are fixed (since general forcefields is not applicable for PCP structures)
Notes: １．X線結晶構造解析では決まらないような、ディスオーダーのあるMOFの構造最適化
２．ナノ空間に導入したモノマーの配向構造を計算し、生成してきた高分子の構造と比較することで、どのように重合反応が起こっているかを調べる。反応の動的過程を計算で可視化することができれば、より面白い研究になる。
３．上記の二つの過程を行うことで、計算科学の方から、このようなMOFを作れば、反応場として有用だということを示すこと。
現在の研究では、色々な配位子を場当たり的に合成して、たまたまうまく行けば良いというスタンスなので、計算して合理的にMOFを設計し、それを使って高度な重合制御ができれば非常に有用。

## Slide 13: 1: Adsorption structure of guest molecules
By using the UFF general forcefield, optimize the adsorbed guest molecule structure in the PCP [Cu2(pzdc)2(pyrazine)]n (CPL-1).
-C≡CH group of the guest molecule are hydrogen bonded to the exposed oxygen atoms of PCP pore surface.
This adsorbed structure can explain the polymerization mechanism predicted by the experimental observations.
Uemura, T.; Kitaura, R.; Ohta, Y.; Nagaoka, M.; Kitagawa, S. Angew. Chem. Int. Ed. Engl. 2006, 45, 4112–4116.
methyl propiolate
プロピオール酸メチル

## Slide 14: 2: O2 adsorption on CPL-1 (CpPy)
Nagaoka, M.; Ohta, Y.; Hitomi, H. Coord. Chem. Rev. 2007, 251, 2522–2536.
[Cu2(pzdc)2(pyz)]n （CPL-1） or CpPy ("Cu2(pzdc)2"を"Cp", "pyz"を"Py"と表記)
(pzdc: pyrazine-2,3-dicarboxylate, pyz:pyrazine)
CpPy crystal (from a –axis view)
Cp
Py
CpPy·nO2 (0 ≤ n ≤ 2)
In the O2 saturated condition, two O2 molecules align parallel to each other and indicates the properties similar to solid oxygen.
By the intermolecular interactions between the guest O2 and host PCP pore surface, the O2 dimer structure is stable up to 110 K. (the melting temperature of solid O2 is 54.3 K )
CpPy·2O2 crystal (from c –axis view)

## Slide 15: Structure optimization by three point O2 model
Forcefield parameter fit to consider quadrupole-quadrupole interaction of O2
↓
Experimental O2 structures can be obtained
Two point model (no charge on O2)
（VLJ）
Three point model（VLJ+VEQQ）
X-ray crystal structure
(80 kPa/O2 gas, 90 K)
97.71
94.76
87.71
c-axis
78.48
78.36
67.19
b-axis
11.56
11.82
24.61
a-axis
XRPD
VLJ+VEQQ
VLJ
Table. Inclination angles of O2 against three lattice axes of CpPy framework
Three point model of O2 to include quadrupole interactions

## Slide 16: Average num. of O2 by GCMC simulation
Grand canonical MC (GCMC) analysis
The thermodynamic average <A> of an observable A can be obtained by
Configurations of O2 molecules are probabilistically updated in the Metropolis algorithm. (update by O2 creation, deletion, translation, rotation)
Calculation conditions
Three point model of O2
O2 partial pressure 80 kPa (as in experimental condition)
CpPy framework structure is fixed at two structures Empty CpPy: crystal structure without O2 Apo CpPy: crystal structure with O2
8 million Monte Carlo steps
（Z: distribution function）
O2 density (green color)
by GCMC simulation

## Slide 17: Analysis of temperature dependency
Average number of absorbed O2 <N> (blue) and average adsorption energy <E> (red) in the temperature from 70 to 200 K at the two CpPy structures.
Apo-CpPy structure
Empty-CpPy structure
Connect two curves (Empty-CpPy at high temp. and Apo-CpPy at low temp.
Drastic O2 adsorption around 115 K was reproduced.
(Experimentally, adsorption occurs at 130 K)
<N>
<E>

## Slide 18: 3: Polystyrene conformation in JAST-1 pore
Uemura, T.; Horike, S.; Kitagawa, K.; Mizuno, M.; Endo, K.; Bracco, S.; Comotti, A.; Sozzani, P.; Nagaoka, M.; Kitagawa, S. J. Am. Chem. Soc. 2008, 130, 6781–6788.
Conformation of polystyrene (PSt) in the JAST-1 ([Zn2(bdc)2ted]n) pore was analyzed by MD simulation.
For short PSt chain (n=4), side chains of the terminal styrene (benzene ring) stacks with the JAST-1 pore wall and the backbone is bent.
For long PSt chain (n=9), stacking of the terminals occurs as in the short chain. However, the backbone forms linear structure.

## Slide 19: 4: Thermal transition of PEGs in JAST-1 pores
Uemura, T.; Yanai, N.; Watanabe, S.; Tanaka, H.; Numaguchi, R.; Miyahara, M. T.; Ohta, Y.; Nagaoka, M.; Kitagawa, S. Nat. Commun. 2010, 1, 83.
Prediction of the linear tetramer structure of polyethylene glycol (PEG) in the JAST-1 pores by MD simulation.
Details are explained later.
Polyethylene glycol（PEG）

## Slide 20: Current study Anisotropic behavior of guest molecules in PCP (JAST-1) pores

## Slide 21
Uemura et al. Nat. Commun. 2010
Unique thermal transition of PEG in JAST-1
What is the reason of the unique thermal transition temperature dependency ?
First, analyze the liquid-like PEG structure at high temperature.
In PCP pores, thermal transition temp. is lower in longer PEG
In bulk PEG, thermal transition temp. is higher in longer PEG
Free liquid-like PEG at high temperature
Solid-like state at low temperature
Linear PEG structure?
Thermal transition
Molecular weight
Thermal transition temp.
Inverse relation

## Slide 22
MD model of JAST-1
JAST-1 PCP
Flexible forcefield reported in J. Am. Chem. Soc. 134, 4207 (2012).
Zn ion
Organic ligands

## Slide 23
Preliminary results
PEG molecules with molecular weight 634.7 (n=14) was put in the JAST-1 pores.
Execute extremely high temperature MD at 1500 K for 100 ns to prepare random PEG distribution with fixing PCP structure
Execute MD simulation at 550 K for 100 ns with flexible PCP
Execute MD simulation at 300 K for 200 ns with flexible PCP
At 300 K, each PEG structure is bent with localized distribution.
At 550 K, each PEG structure is extended with scattered distribution.

## Slide 24: Future work Simulate polymerization reaction in PCP pores by hybrid MD/MD method Collaboration with molecular technology CREST

## Slide 25: PEG structure below thermal transition temperature
It was predicted that four linear PEG align in the JAST-1 pore below the transition temperature (about 240 K).
However, there is no direct evidence for this aligned structure.
To analyze the structural and alignment behavior of PEGs at the low temperature, usual MD simulation is not appropriate since PEGs are immobile in such low temperature.
Thus, I will use MC/MD procedure with the combination of local structural arrangement by MD and large structural changes by MC treatment.
Uemura et al. Nat. Commun. 2010
Free liquid-like PEG at high temperature
Solid-like state at low temperature
Linear PEG structure?
Thermal transition

## Slide 26: Simulate polymerization reactions in PCP pores
By the hybrid MC/MD method, simulate the polymerization reactions in PCP pores
Uemura et al., J. Am. Chem. Soc. 132, 4917–4924 (2010).
Analyze the polymer properties (e.g. tacticity)
Compare product polymers using different PCPs with several organic ligands.