## Slide 1
The 4th, CREST Workshop
Norio Takenaka1,2
Graduate School of Information Science, Nagoya University1,
Elements Strategy Initiative for Catalysts and Batteries (ESICB), Kyoto University2
Implementation of Constant Potential Method into AMBER
Thu. Dec. 3rd

## Slide 2: Background of Present Research
Figure. Charge-discharge curve in LIB
・ According to experimental researchers, the SEI film can be mainly formed in the plateau region on the charge curve, where the electric potential is constant.
・ To reproduce correctly the SEI film formation, the hybrid MC/MD simulations should be executed at the appropriate electric potential (e.g., ~ 0.2 V vs. Li+/Li in this figure).
To pursue the advancement of SEI film formation simulation, I will combine the constant (electric) potential method with the hybrid MC/MD reaction method.

## Slide 3: Constant (Electric) Potential Method①
Anode
Cathode
[1] S. K. Reed, O. J. Lanning, P. A. Madden, J. Chem. Phys., 126, 084704 (2007).
In the method, the charges on the electrode are obtained by minimizing the following potential energy under the objective electric potential difference between anode and cathode ΔV (= V+－V-).
The constant (electric) potential method can execute the classical MD simulation under the constant electric potential between the anode and cathode [1].
electrolyte
The electric potential on each charge qj (or atom j) Vj, is theoretically obtained as the derivation of Coulomb potential of the system by its charge.
Set electric potential
Arbitrary atomic charge
,

## Slide 4: Constant (Electric) Potential Method②
To minimize the potential energy , the atomic charges on the electrode are optimized so that the derivation becomes 0 through the SCF procedure like the geometry optimization with the quantum chemical calculation.
If
,
In the standard classical MD simulation, the Coulomb potential is described by the Ewald summation method to include the long-range electrostatic interactions.
Direct sum
Reciprocal sum
Self energy
Vc: volume of the system
α: Ewald coefficient
m: Reciprocal space vector
r: Real space vector
Then, the electric potential Vi on the arbitrary atomic charge i is

## Slide 5: Appropriate Ewald Method for Two-dimensional System
・ In the two-dimensional system such as the electrode surface, the conventional
three-dimensional Ewald (EW3D) method cannot be used.
・ The traditional two-dimensional Ewald (EW2D) method is reasonable, but the
calculation cost is very expensive. Therefore, a widely used approach is the
conventional EW3D method in a simulation box with large empty space that is
sufficient to avoid the artificial interactions between the periodic images.
However, it is known the calculation accuracy of this treatment is not favorable.
・ Under the circumstances, the EW3DC method have been developed [2], and it
can reproduce the identical numerical results as the EW2D method.
MD simulation box
Empty (or vacuum) region
Non-periodic direction
Typical example:
Non-periodic direction
[2] A. Bródka, A. Grzybowski, J. Chem. Phys., 117, 8208 (2002).

## Slide 6: Modified Three-dimensional Ewald Method
In the EW3DC method, the correction term is added to the EW3D method.
Vc: volume of the system
z: real space coordinate along the non-periodic direction
MD simulation box
Empty (or vacuum) region
z axis considering non-periodic
One example: Quartz/water interface system [3]
Empty region
Mass density
Orientation of water molecules
Electrostatic potential
Electric field
[3] I. Yeh, A. Wallqvist, J. Chem. Phys., 134, 055109 (2011).
The EW3DC method can improve the electrostatic potential and electric field
in the two-dimensional system.

## Slide 7: Implementation into AMBER Code
Program main
multisander
MD main
sander
Integrator
runmd
Forces
force
Ewald
ewald_force
Reciprocal sum
Recip_reg
Self energy
self
Direct sum
get_nb_energy
Existing subroutine
Modified subroutine
Optimization of charges on the electrode through the SCF with the conjugate gradient routine
Main routine for constant potential method
Direct sum
Reciprocal sum
Self energy
① Calculation of electric potential (= )
② Correction by the EW3DC method
Program architecture of AMBER

## Slide 8: Test System① (Two Electrodes Arranged as Parallel Plates)
Distance of closest approach: 100 Å
3 layers
3 layers
39.0 Å
39.0 Å
3.9 Å
x
y
(a) Side view
y
z
x
(111) planes in fcc of Pt crystal
Anode
V- = -2 [V]
Number of atoms per 1 plate: 100
Cathode
V+ = 2 [V]
(b) Front view
Non-periodic direction
Empty volume:
~ 39.0 × 39.0 × 900 [Å3]

## Slide 9: Convergence of Energy and Charges in Test System①
Anode
Cathode
Optimization cycle
Summation of electrode charge [e]
-0.333 [e]
0.333 [e]
Optimization cycle
Potential energy [kcal/mol]
(a) Potential energy
(b) Electrode charge
The convergence of potential energy and electrode charges are very good.

## Slide 10: Comparison between Calculation and Theoretical Values
Additionally, the electrode charges on each layer are ±0.268 [e] (first), ±0.068 [e] (second), ±0.002 [e] (third), meaning that the induced charges are mainly contributed by the nearest-neighbor surfaces (~80 %).
Distance: d
Surface area: A
Voltage potential difference: ΔV
Anode
Cathode
V-
V+
If the system consists of an ideal, infinite, parallel plate capacitor, we can obtain the induced charges from classical electrostatics.
The total induced charges are .
In the present system (on page 8),
Figure. Schematic illustration
(= V+－V-)
The present calculation values (±0.333 [e]) were very good agreement with the theoretical one.

## Slide 11: Test System② (Graphite Electrode/PC-based Electrolyte)
114.2 Å
Cathode
Anode
y
z
x
PF6-
Li+
PC
1.1 M LiPF6 PC-based electrolyte
Graphite
Graphite
In the present simulations, the electrolyte was first equilibrated at 0 [V]. Then, by applying the electric voltage (4 [V]), the temporal change in the electrode charges were observed with the constant potential method.
V- = -2 [V]
V+ = 2 [V]
PC: 850
Li+: 85
PF6-: 85

## Slide 12: Convergence of Energy and Charges in Test System②
Anode
Cathode
-0.282 [e]
0.282 [e]
By using the initial structure obtained via the equilibration at 0 [V], the electrode charges were optimized so that the electric potential difference becomes 4 [V].
In the electrolyte, the potential energy and electrode charges converged.
Optimization cycle
Summation of electrode charge [e]
Optimization cycle
Potential energy [kcal/mol]
(a) Potential energy
(b) Electrode charge

## Slide 13: Temporal Change in Electrode Charges and Electrolyte Structures
Time [ps]
(1) Temporal change of electrode charges
Anode
Cathode
(a) Initial structure (t = 0 [ps])
(b) Final structure (t = 50 [ps])
(2) Electrolyte structure near the anode
The induced electrode charges and electrolyte structures were obtained self-consistently with the increase in the MD time steps.
Summation of electrode charge [e]

## Slide 14: Number Density Distribution Depending on Voltage①
Gray: PC, Orange: PF6-, Blue: Li+
Chart: 
Chart: 
z [Å]
Number density
Number density
z [Å]
(a) 0 [V]
(b) 4 [V]
Li+
PC
PF6-
The electric double layer was found to be clearly formed in response to the voltage as a result from the charge separation of Li+ and PF6- in the electrolyte.
anode
cathode
anode
cathode

## Slide 15: Number Density Distribution Depending on Voltage②
Chart: 
z [Å]
Number density
Chart: 
Number density
z [Å]
Orange: -CH3, Blue: -CO3
(a) 0 [V]
(b) 4 [V]
anode
cathode
anode
cathode
negative
positive
The positive –CH3 residues were found to turn to the anode surface, which is negatively charged.

## Slide 16: Conclusion and Future Work
[4] M. K. Petersen, R. Kumar, H. S. White, G. A. Voth, J. Phys. Chem. C, 116, 4903 (2012).
To improve the SEI film formation simulation, the constant potential method was implemented into the AMBER code. At the same time, the EW3DC method was introduced for the two-dimensional system.
By using the method, the calculated electrode charges were found to be very good agreement with the theoretical one.
In the electrode-electrolyte system, the electrode charges were obtained in response to the voltage, providing the electric double layers.
However, since the present program was unstable depending on the selection of initial charges (data not shown), it should be modified.
Nevertheless, the calculation cost of constant potential method was still expensive for the hybrid MC/MD reaction simulations due to the SCF procedure. Therefore, I will examine the alternative method without SCF [4].

## Slide 17: Thank you for your attention

## Slide 18
One example: Quartz/water interface system [3]
Mass density
Orientation of water molecules
Electrostatic potential
Electric field
[3] I. Yeh, A. Wallqvist, J. Chem. Phys., 134, 055109 (2011).

## Slide 19: Fast Constant Potential Method
[4] M. K. Petersen, R. Kumar, H. S. White, G. A. Voth, J. Phys. Chem. C, 116, 4903 (2012).
Cathode
Anode
electrolyte
Considering the electrochemical cell composed of two parallel electrodes and electrolyte, the induced charges on the electrodes are obtained as follows.
qLE
qRE
Arbitrary atomic
charge
Distance: D
A: surface area of electrode
ΔV: electric potential difference between anode and cathode
z axis considering non-periodic