## Slide 1
The 3rd, CREST Workshop
Norio Takenaka1,2
Graduate School of Information Science, Nagoya University1,
Elements Strategy Initiative for Catalysts and Batteries (ESICB), Kyoto University2
On Additive Effect of Fluoroethylene Carbonate on Solid Electrolyte Interphase Film Formation in Sodium-Ion Batteries
Thu. Oct. 23th
1

## Slide 2
Elements Strategy Initiative for Catalysts and Batteries: Interplay Between Experimental and Theoretical Studies
MEXT program
Primary objective is to develop rare metals-free catalysts and batteries. To accomplish this objective, we reveal the microscopic mechanism in the catalysts and batteries which are complex materials by the interplay between the experimental and theoretical studies.
As one of specific targets,
we develop the rare metals-free secondary battery.
Li-ion battery
Na-ion battery
(Li = rare metal)
(Na = common metal)
2

## Slide 3
EC
PC
Anode material
Graphite →
Hard carbon
Solvent
Li+ → Na+
PF6-
Salt
・・・
Anode
Cathode
Solvent
Cathode material
CoO2 → MnO2, NiO2
From Li-Ion Battery to Na-Ion Battery
Salt
To produce the practical Na-ion battery, the optimized design of materials is required because Na+ is larger than Li+.
Electrolyte

## Slide 4: Background of Present Research①
Solid Electrolyte Interphase (SEI) Film
・During the initial charging cycles, the reductive reaction products of the electrolyte form a solid electrolyte interphase (SEI) film on the anode surface.
SEI Film
Inorganic Salts
(e.g. Na2CO3)
Organic Salts
(e.g. ROCO2Na)
Na+
Solvent
Block
Exchange
・The ideal SEI film can protect the electrolyte from the further reduction while maintaining Na+ exchange. Therefore, it is closely related to the lifetime of battery.
To improve the SEI film formation, the addition of additive is very important.
Na-ion battery
Reduction of electrolyte
S. Komaba et al., Adv. Funct. Mater, 21, 3859 (2011).

## Slide 5: Background of Present Research②
Additive effect on the SEI film formation
・According to the experiment by Prof. Komaba, fluoroethylene carbonate (FEC) was only an effective additive in the Na-ion battery among the FEC, DFEC, VC and ES that are well-known as the effective additive in the Li-ion battery.
・The FEC addition was found to improve the cycle performance by decreasing the irreversible capacity to form the SEI film.
S. Komaba et al., ACS Appl. Mater. Interfaces, 3, 4165 (2011).
FEC-free
FEC-added (10 vol%)
Figure. Reversible capacity versus cycle number plots in Na-ion battery

## Slide 6: Purpose of Present Research
・In the present study, to investigate the microscopic additive effects on the SEI film formation in the Na-ion cell, we have executed the atomistic reaction simulations via the recently developed hybrid MC/MD reaction method[1,2].
[1] M. Nagaoka, Y. Suzuki, T. Okamoto, NT, Chem. Phys. Lett., 583, 80 (2013).
[2] NT, Y. Suzuki, H. Sakai, M. Nagaoka, J. Phys. Chem. C, 118, 10874 (2014).
e-
Hybrid MC/MD
reaction simulation
・For this purpose, we have compared the calculation results between with and without FEC additives into the electrolyte.
Initial state
Final state

## Slide 7
Most Probable Reaction Pathway for FEC Reduction
K. Leung et al., J. Electrochem. Soc., 161(3), A213 (2014).
NaF
C2H3O
CO2
・ Quantum Chemical Calculation
・ Experimental F 1s XPS spectra
S. Komaba et al., ACS Appl. Mater. Interfaces, 3, 4165 (2011).
10 vol% FEC addition
Without FEC
Pristine
0.5 vol%
2 vol%
➤The most probable singly reduced products were predicted to be NaF, CO2 and
C2H3O molecules since the free energy of activation was smallest.
➤Experimentally, the NaF was evidently
observed as increase in the amount of
added FEC in the Na-ion cell.

## Slide 8
Simulation Model and Reaction Scheme
Carbon anode
NaPF6 electrolyte with or without FEC
y
z
x
+ e-, + Na+
+
+ NaPC
Na2CO3
+ e-, + Na+
PC
NaPC
C3H6
(CH3CHCH2OCO2Na)2
Na2DMBDC
+
+
PF3
3NaF
+ 2e-, + 3Na+
+
PF6
FEC
CO2
+
NaF
+
C2H3O
+ e-, + Na+
1.1M NaPF6 PC electrolyte
PC: 850
Na+: 87
PF6-: 85
System I
System II
(without FEC)
(with 10 vol% FEC)
PC: 850
Na+: 87
PF6-: 85
FEC: 118
Negatively Charged
(-2 e)

## Slide 9
SEI Film Formation Processes
(a) 100 cycle
(b) 500 cycle
(c) 1500 cycle
(a) 100 cycle
(b) 500 cycle
(c) 1500 cycle
NaPC
Na2DMBDC
Na2CO3
NaF
(1) FEC-free electrolyte (System I)
(2) FEC-added electrolyte (System II)
Species
➤In both systems, the SEI film is formed by aggregating the reaction products of
electrolyte via the hybrid MC/MD reaction simulations.

## Slide 10
(They are obtained by different 10 initial configurations.)
Change in Number Densities of Reaction Products
・ The composition ratio of the molecular mixture of the reaction products became
almost unchanged in the final stage of the formation processes.
Chart: 
| 0 | 40 | 80 | 120 | 160 | 200 | 240 | 280 | 320 | 360 | 400 | 440 | 480 | 520 | 560 | 600 | 640 | 680 | 720 | 760 | 800 | 840 | 880 | 920 | 960 | 1000 | 1040 | 1080 | 1120 | 1160 | 1200 | 1240 | 1280 | 1320 | 1360 | 1400 | 1440 | 1480 | 1520 | 1560 | 1600 | 1640 | 1680 | 1720 | 1760 | 1800 | 1840 | 1880 | 1920 | 1960 | 2000
 | 0 | 0.86442 | 1.6733 | 2.4188 | 3.0453 | 3.3387 | 3.7749 | 4.1001 | 4.2983 | 4.2666 | 4.2666 | 4.2428 | 4.1159 | 3.8939 | 3.537 | 2.7836 | 2.4347 | 2.1333 | 1.7923 | 1.5861 | 1.3958 | 1.3085 | 1.2372 | 1.2292 | 1.1975 | 1.1578 | 1.1261 | 1.0785 | 1.0627 | 1.0706 | 1.0627 | 1.0627 | 1.0548 | 1.0627 | 1.0785 | 1.0785 | 1.0706 | 0.99924 | 0.99924 | 0.99924 | 1.0072 | 1.0072 | 0.99131 | 0.99131 | 0.98338 | 0.95166 | 0.95166 | 0.95166 | 0.95959 | 0.94373 | 0.92786
 | 0 | 0 | 0.031722 | 0.063444 | 0.15068 | 0.2855 | 0.44411 | 0.61858 | 0.81684 | 1.0785 | 1.3244 | 1.5226 | 1.7923 | 2.0699 | 2.4109 | 2.8232 | 3.0691 | 3.2118 | 3.3863 | 3.5132 | 3.6163 | 3.6718 | 3.7115 | 3.7273 | 3.7352 | 3.759 | 3.767 | 3.7828 | 3.7987 | 3.7987 | 3.7987 | 3.7987 | 3.8066 | 3.8066 | 3.8066 | 3.8066 | 3.8146 | 3.8463 | 3.8463 | 3.8463 | 3.8463 | 3.8463 | 3.8542 | 3.8542 | 3.8621 | 3.878 | 3.878 | 3.8859 | 3.8859 | 3.8939 | 3.9018
 | 9.3579 | 9.2152 | 9.0487 | 8.9694 | 8.7473 | 8.6997 | 8.549 | 8.3984 | 8.2873 | 8.1684 | 8.0494 | 7.9067 | 7.7243 | 7.5736 | 7.4626 | 7.3753 | 7.3278 | 7.304 | 7.2643 | 7.2167 | 7.2167 | 7.2167 | 7.1771 | 7.1533 | 7.1453 | 7.1374 | 7.1374 | 7.1295 | 7.1295 | 7.1295 | 7.1216 | 7.1216 | 7.1136 | 7.1136 | 7.1136 | 7.1136 | 7.1136 | 7.1057 | 7.1057 | 7.1057 | 7.0978 | 7.0978 | 7.0978 | 7.0898 | 7.0898 | 7.0898 | 7.0898 | 7.0898 | 7.0898 | 7.0898 | 7.0898
 | 0 | 0.095166 | 0.34894 | 0.64237 | 0.80098 | 1.1023 | 1.2847 | 1.4751 | 1.7209 | 1.943 | 2.1888 | 2.4743 | 2.7122 | 2.9422 | 3.196 | 3.4339 | 3.5291 | 3.7115 | 3.7987 | 3.8304 | 3.8701 | 3.9018 | 3.9097 | 3.9097 | 3.9335 | 3.9494 | 3.9652 | 3.989 | 3.989 | 3.997 | 4.0207 | 4.0287 | 4.0366 | 4.0366 | 4.0366 | 4.0366 | 4.0366 | 4.0445 | 4.0445 | 4.0604 | 4.0604 | 4.0604 | 4.0604 | 4.0604 | 4.0604 | 4.0604 | 4.0604 | 4.0604 | 4.0763 | 4.0763 | 4.0763
 | 0 | 0.13482 | 0.31722 | 0.45997 | 0.6503 | 0.76926 | 0.89614 | 1.0072 | 1.1341 | 1.253 | 1.4116 | 1.5226 | 1.6654 | 1.8319 | 1.9668 | 2.0461 | 2.0857 | 2.1254 | 2.165 | 2.1967 | 2.1967 | 2.1967 | 2.2126 | 2.2364 | 2.2443 | 2.2523 | 2.2523 | 2.2602 | 2.2602 | 2.2602 | 2.2681 | 2.2681 | 2.276 | 2.276 | 2.276 | 2.276 | 2.276 | 2.284 | 2.284 | 2.284 | 2.2919 | 2.2919 | 2.2919 | 2.2998 | 2.2998 | 2.2998 | 2.2998 | 2.2998 | 2.2998 | 2.2998 | 2.2998
 | 67.409 | 66.4494 | 65.3232 | 64.2209 | 63.2613 | 62.3969 | 61.4611 | 60.5967 | 59.7561 | 59.0423 | 58.3048 | 57.6466 | 56.9963 | 56.4332 | 55.8543 | 55.545 | 55.3071 | 55.1405 | 55.0454 | 54.9661 | 54.9105 | 54.855 | 54.8392 | 54.8154 | 54.8074 | 54.7837 | 54.7837 | 54.7757 | 54.7599 | 54.744 | 54.7281 | 54.7202 | 54.7044 | 54.6964 | 54.6806 | 54.6806 | 54.6726 | 54.6726 | 54.6726 | 54.6568 | 54.6488 | 54.6488 | 54.6488 | 54.6488 | 54.6409 | 54.6409 | 54.6409 | 54.625 | 54.6013 | 54.6013 | 54.6013
Chart: 
| 0 | 40 | 80 | 120 | 160 | 200 | 240 | 280 | 320 | 360 | 400 | 440 | 480 | 520 | 560 | 600 | 640 | 680 | 720 | 760 | 800 | 840 | 880 | 920 | 960 | 1000 | 1040 | 1080 | 1120 | 1160 | 1200 | 1240 | 1280 | 1320 | 1360 | 1400 | 1440 | 1480 | 1520 | 1560 | 1600 | 1640 | 1680 | 1720 | 1760 | 1800 | 1840 | 1880 | 1920 | 1960 | 2000
 | 0 | 0.96752 | 1.9905 | 2.9184 | 3.5766 | 4.2031 | 4.7186 | 5.1707 | 5.5593 | 5.4958 | 5.7179 | 5.9637 | 6.3047 | 6.0747 | 6.1302 | 6.0034 | 5.5672 | 4.7979 | 4.4331 | 3.8621 | 3.2832 | 2.7677 | 2.3871 | 2.1095 | 1.9588 | 1.9033 | 1.8399 | 1.8161 | 1.7606 | 1.7288 | 1.6733 | 1.6495 | 1.6416 | 1.6257 | 1.6257 | 1.6416 | 1.6178 | 1.602 | 1.6257 | 1.602 | 1.6178 | 1.6099 | 1.5861 | 1.5544 | 1.5782 | 1.5464 | 1.5544 | 1.5464 | 1.5306 | 1.5385 | 1.5226
 | 0 | 0.0079305 | 0.023791 | 0.071374 | 0.15068 | 0.2855 | 0.4679 | 0.67409 | 0.84856 | 1.1499 | 1.364 | 1.6257 | 1.8478 | 2.1412 | 2.4822 | 2.7757 | 3.1643 | 3.6401 | 3.9573 | 4.2983 | 4.6552 | 4.9407 | 5.1231 | 5.2817 | 5.3689 | 5.4006 | 5.4324 | 5.4403 | 5.472 | 5.4958 | 5.5275 | 5.5434 | 5.5513 | 5.5593 | 5.5672 | 5.5672 | 5.583 | 5.591 | 5.5989 | 5.5989 | 5.5989 | 5.5989 | 5.6068 | 5.6227 | 5.6227 | 5.6465 | 5.6465 | 5.6465 | 5.6544 | 5.6544 | 5.6624
 | 0 | 0.071374 | 0.29343 | 0.49962 | 0.63444 | 0.85649 | 1.023 | 1.1816 | 1.4037 | 1.6416 | 1.8399 | 2.0143 | 2.2364 | 2.4822 | 2.7043 | 2.9819 | 3.2436 | 3.5291 | 3.8066 | 4.0763 | 4.2111 | 4.338 | 4.4807 | 4.5442 | 4.5759 | 4.5997 | 4.6314 | 4.6393 | 4.6393 | 4.6393 | 4.6393 | 4.6473 | 4.6631 | 4.6631 | 4.671 | 4.679 | 4.7107 | 4.7186 | 4.7266 | 4.7503 | 4.7583 | 4.7662 | 4.7821 | 4.7821 | 4.7821 | 4.7821 | 4.7821 | 4.7979 | 4.8217 | 4.8297 | 4.8297
 | 0 | 0.031722 | 0.095166 | 0.11103 | 0.12689 | 0.14275 | 0.1824 | 0.19033 | 0.19033 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412 | 0.21412
 | 67.409 | 66.3542 | 65.0774 | 63.8482 | 62.8965 | 61.7783 | 60.7315 | 59.7085 | 58.7489 | 57.9717 | 57.1231 | 56.1794 | 55.1722 | 54.5695 | 53.6099 | 52.8724 | 52.2697 | 51.8018 | 51.2546 | 50.8739 | 50.6043 | 50.4219 | 50.295 | 50.1919 | 50.1364 | 50.1047 | 50.073 | 50.073 | 50.065 | 50.0492 | 50.0412 | 50.0254 | 50.0016 | 50.0016 | 49.9778 | 49.954 | 49.9144 | 49.9064 | 49.8588 | 49.8588 | 49.835 | 49.835 | 49.8271 | 49.8271 | 49.8033 | 49.7875 | 49.7795 | 49.7716 | 49.7478 | 49.732 | 49.732
NaPC
Na2DMBDC
Na2CO3
NaF
PC
PC
FEC
(b) With FEC (System II)
MC/MD cycles
MC/MD cycles
[10-2Å-2]
[10-2Å-2]
[10-2Å-2]
[10-2Å-2]
(a) Without FEC (System I)
NaPC
Na2DMBDC
Na2CO3
NaF
・ By adding FECs, the production of NaF complexes drastically increased.

## Slide 11
Chart: 
| 0 | 40 | 80 | 120 | 160 | 200 | 240 | 280 | 320 | 360 | 400 | 440 | 480 | 520 | 560 | 600 | 640 | 680 | 720 | 760 | 800 | 840 | 880 | 920 | 960 | 1000 | 1040 | 1080 | 1120 | 1160 | 1200 | 1240 | 1280 | 1320 | 1360 | 1400 | 1440 | 1480 | 1520 | 1560 | 1600 | 1640 | 1680 | 1720 | 1760 | 1800 | 1840 | 1880 | 1920 | 1960 | 2000
 | 0 | 0.011737 | 0.027043 | 0.041397 | 0.05242 | 0.065823 | 0.078274 | 0.09009 | 0.10191 | 0.11222 | 0.12268 | 0.13387 | 0.14616 | 0.15464 | 0.16646 | 0.17661 | 0.18526 | 0.19279 | 0.20104 | 0.20754 | 0.21158 | 0.21468 | 0.21737 | 0.21904 | 0.21991 | 0.22047 | 0.2211 | 0.22118 | 0.22126 | 0.22142 | 0.2215 | 0.22174 | 0.22213 | 0.22213 | 0.22245 | 0.22277 | 0.22348 | 0.22364 | 0.22419 | 0.22443 | 0.22475 | 0.22483 | 0.22507 | 0.22507 | 0.2253 | 0.22546 | 0.22554 | 0.22578 | 0.22626 | 0.22649 | 0.22649
 | 0 | 0.012292 | 0.028312 | 0.042825 | 0.056544 | 0.068757 | 0.081684 | 0.094055 | 0.10603 | 0.11705 | 0.12792 | 0.13862 | 0.14941 | 0.15893 | 0.16876 | 0.17534 | 0.1801 | 0.1843 | 0.18732 | 0.18906 | 0.18993 | 0.19081 | 0.19144 | 0.19192 | 0.19239 | 0.19295 | 0.19327 | 0.19366 | 0.19406 | 0.19438 | 0.19485 | 0.19501 | 0.19541 | 0.19549 | 0.19557 | 0.19557 | 0.19564 | 0.1958 | 0.19588 | 0.19636 | 0.1966 | 0.19675 | 0.19683 | 0.19707 | 0.19715 | 0.19715 | 0.19715 | 0.19739 | 0.19779 | 0.19779 | 0.19779
(1) without FEC (System I)
0.23 [e Å-2]
(2) With FEC (System II)
0.20 [e Å-2]
Consumed Amount of Electrons to Form SEI Film
MC/MD cycles
Consumed amount of electrons [eÅ-2]
Without FEC
With FEC
Down
14 %!!
Total consumed electron
number to form SEI film
➤The present simulations could reproduce the experimental observations
that the irreversible capacity decrease by adding FECs.
By counting the added electrons in each MC/MD cycle through the present simulations, we estimated the integrated values per unit area of carbon anode.

## Slide 12
(b) With FEC (System II)
(a) Without FEC (System I)
10 Å
10 Å
NaPC
Na2DMBDC
Na2CO3
NaF
Species in SEI film
Atomistic Structures of SEI Film and Electrolyte
Purple: PC, Light blue: FEC, Gray: Gas, Blue: Na+, Orange: PF6-

## Slide 13
Mass Density Distributions of SEI film and Electrolyte
➤These figures clearly indicate that these SEI films can serve solvent molecules
by preventing them from approaching the anode surface.
(They are obtained by different 10 initial configurations.)
Chart: 
| 1.1999999999999993 | 3.1999999999999993 | 5.1999999999999993 | 7.1999999999999993 | 9.1999999999999993 | 11.2 | 13.2 | 15.2 | 17.2 | 19.2 | 21.2 | 23.2 | 25.2 | 27.2 | 29.2 | 31.2 | 33.200000000000003 | 35.200000000000003 | 37.200000000000003 | 39.200000000000003 | 41.2 | 43.2 | 45.2 | 47.2 | 49.2 | 51.2 | 53.2 | 55.2 | 57.2 | 59.2 | 61.2 | 63.2 | 65.2 | 67.2 | 69.2 | 71.2 | 73.2 | 75.2 | 77.2 | 79.2 | 81.2
 | 0 | 0.0035769 | 0.059195 | 0.43849 | 0.87829 | 1.5049 | 1.3652 | 1.5388 | 1.3506 | 1.297 | 1.2421 | 1.0485 | 0.87194 | 0.64375 | 0.38442 | 0.31158 | 0.22922 | 0.12767 | 0.058521 | 0.049942 | 0.0087529 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0.19014 | 0.18497 | 0.12827 | 0.090917 | 0.049989 | 0.032869 | 0.020826 | 0.016552 | 0.012259 | 0.0099984 | 0.0078783 | 0.0045724 | 0.0038793 | 0.0040532 | 0.006231 | 0.0064315 | 0.0041414 | 0.004274 | 0.0031173 | 0.0034578 | 0.0042355 | 0.0037127 | 0.0032231 | 0.0031556 | 0.0027847 | 0.002878 | 0.0034098 | 0.0031362 | 0.0026593 | 0.0030098 | 0.0032816 | 0.0039654 | 0.0045838 | 0.0047012 | 0.0040704 | 0.0045856 | 0.0039924 | 0.0028122 | 0.0022629 | 0.0020514
 | 0 | 0.0034092 | 0.04423 | 0.018965 | 0.038717 | 0.04791 | 0.069622 | 0.13279 | 0.19593 | 0.25047 | 0.31153 | 0.37913 | 0.50507 | 0.67331 | 0.78105 | 0.91627 | 0.96484 | 1.0522 | 1.0607 | 1.0812 | 1.038 | 1.0707 | 1.1001 | 1.0684 | 1.072 | 1.0776 | 1.1037 | 1.097 | 1.0954 | 1.0994 | 1.1008 | 1.0928 | 1.0984 | 1.0921 | 1.0949 | 1.1201 | 1.1175 | 1.0811 | 1.0889 | 1.1146 | 1.0996 | 1.1087 | 1.116 | 1.117
Chart: 
| 1.1999999999999993 | 3.1999999999999993 | 5.1999999999999993 | 7.1999999999999993 | 9.1999999999999993 | 11.2 | 13.2 | 15.2 | 17.2 | 19.2 | 21.2 | 23.2 | 25.2 | 27.2 | 29.2 | 31.2 | 33.200000000000003 | 35.200000000000003 | 37.200000000000003 | 39.200000000000003 | 41.2 | 43.2 | 45.2 | 47.2 | 49.2 | 51.2 | 53.2 | 55.2 | 57.2 | 59.2 | 61.2 | 63.2 | 65.2 | 67.2 | 69.2 | 71.2 | 73.2 | 75.2 | 77.2 | 79.2 | 81.2
 | 0 | 0.074176 | 0.15351 | 0.75863 | 1.3087 | 1.5302 | 1.4956 | 1.4775 | 1.4218 | 1.3104 | 1.167 | 0.83462 | 0.78549 | 0.71385 | 0.7215 | 0.57453 | 0.66139 | 0.53686 | 0.41182 | 0.32662 | 0.32867 | 0.23042 | 0.21523 | 0.22459 | 0.1731 | 0.12182 | 0.074319 | 0.084124 | 0.030799 | 0.010258 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0.19135 | 0.20317 | 0.089275 | 0.060526 | 0.023269 | 0.017034 | 0.008284 | 0.0056556 | 0.0013082 | 0.0024339 | 0.0023156 | 0.004978 | 0.0023477 | 0.0018956 | 0.0010746 | 0.0010235 | 0.00042903 | 0.00036889 | 0.0013673 | 0.0012099 | 0.0018013 | 0.0014766 | 0.0013713 | 0.0019216 | 0.0022955 | 0.0019687 | 0.0020038 | 0.0021512 | 0.0022214 | 0.0025271 | 0.002896 | 0.0026985 | 0.0020319 | 0.0016911 | 0.0015578 | 0.0011428 | 0.0012189 | 0.00089115 | 0.00095129 | 0.0011869
 | 0 | 0.00084334 | 0.04185 | 0.015639 | 0.048421 | 0.050998 | 0.0938 | 0.10978 | 0.15743 | 0.20345 | 0.31854 | 0.47186 | 0.49752 | 0.63506 | 0.61677 | 0.70647 | 0.67641 | 0.7668 | 0.79868 | 0.83227 | 0.86122 | 0.85799 | 0.87665 | 0.8538 | 0.90342 | 0.92255 | 0.94291 | 0.97856 | 0.96628 | 1.0085 | 1.0046 | 1.0182 | 1.0449 | 1.044 | 1.0225 | 1.0464 | 1.0459 | 1.0346 | 1.0386 | 1.0356 | 1.061
(b) With FEC (System II)
(a) Without FEC (System I)
[gcm-3]
[gcm-3]
z [Å]
z [Å]
SEI film
Electrolyte solvent
Gas molecule
SEI film
Electrolyte solvent
Gas molecule

## Slide 14
Chart: 
| 1.1999999999999993 | 3.1999999999999993 | 5.1999999999999993 | 7.1999999999999993 | 9.1999999999999993 | 11.2 | 13.2 | 15.2 | 17.2 | 19.2 | 21.2 | 23.2 | 25.2 | 27.2 | 29.2 | 31.2 | 33.200000000000003 | 35.200000000000003 | 37.200000000000003 | 39.200000000000003 | 41.2 | 43.2 | 45.2 | 47.2 | 49.2 | 51.2 | 53.2 | 55.2 | 57.2 | 59.2 | 61.2 | 63.2 | 65.2 | 67.2 | 69.2 | 71.2 | 73.2 | 75.2 | 77.2 | 79.2 | 81.2
 | 0 | 0.0035769 | 0.059195 | 0.43849 | 0.87829 | 1.5049 | 1.3652 | 1.5388 | 1.3506 | 1.297 | 1.2421 | 1.0485 | 0.87194 | 0.64375 | 0.38442 | 0.31158 | 0.22922 | 0.12767 | 0.058521 | 0.049942 | 0.0087529 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0.19014 | 0.18497 | 0.12827 | 0.090917 | 0.049989 | 0.032869 | 0.020826 | 0.016552 | 0.012259 | 0.0099984 | 0.0078783 | 0.0045724 | 0.0038793 | 0.0040532 | 0.006231 | 0.0064315 | 0.0041414 | 0.004274 | 0.0031173 | 0.0034578 | 0.0042355 | 0.0037127 | 0.0032231 | 0.0031556 | 0.0027847 | 0.002878 | 0.0034098 | 0.0031362 | 0.0026593 | 0.0030098 | 0.0032816 | 0.0039654 | 0.0045838 | 0.0047012 | 0.0040704 | 0.0045856 | 0.0039924 | 0.0028122 | 0.0022629 | 0.0020514
 | 0 | 0.0034092 | 0.04423 | 0.018965 | 0.038717 | 0.04791 | 0.069622 | 0.13279 | 0.19593 | 0.25047 | 0.31153 | 0.37913 | 0.50507 | 0.67331 | 0.78105 | 0.91627 | 0.96484 | 1.0522 | 1.0607 | 1.0812 | 1.038 | 1.0707 | 1.1001 | 1.0684 | 1.072 | 1.0776 | 1.1037 | 1.097 | 1.0954 | 1.0994 | 1.1008 | 1.0928 | 1.0984 | 1.0921 | 1.0949 | 1.1201 | 1.1175 | 1.0811 | 1.0889 | 1.1146 | 1.0996 | 1.1087 | 1.116 | 1.117
Chart: 
| 1.1999999999999993 | 3.1999999999999993 | 5.1999999999999993 | 7.1999999999999993 | 9.1999999999999993 | 11.2 | 13.2 | 15.2 | 17.2 | 19.2 | 21.2 | 23.2 | 25.2 | 27.2 | 29.2 | 31.2 | 33.200000000000003 | 35.200000000000003 | 37.200000000000003 | 39.200000000000003 | 41.2 | 43.2 | 45.2 | 47.2 | 49.2 | 51.2 | 53.2 | 55.2 | 57.2 | 59.2 | 61.2 | 63.2 | 65.2 | 67.2 | 69.2 | 71.2 | 73.2 | 75.2 | 77.2 | 79.2 | 81.2
 | 0 | 0.074176 | 0.15351 | 0.75863 | 1.3087 | 1.5302 | 1.4956 | 1.4775 | 1.4218 | 1.3104 | 1.167 | 0.83462 | 0.78549 | 0.71385 | 0.7215 | 0.57453 | 0.66139 | 0.53686 | 0.41182 | 0.32662 | 0.32867 | 0.23042 | 0.21523 | 0.22459 | 0.1731 | 0.12182 | 0.074319 | 0.084124 | 0.030799 | 0.010258 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0.19135 | 0.20317 | 0.089275 | 0.060526 | 0.023269 | 0.017034 | 0.008284 | 0.0056556 | 0.0013082 | 0.0024339 | 0.0023156 | 0.004978 | 0.0023477 | 0.0018956 | 0.0010746 | 0.0010235 | 0.00042903 | 0.00036889 | 0.0013673 | 0.0012099 | 0.0018013 | 0.0014766 | 0.0013713 | 0.0019216 | 0.0022955 | 0.0019687 | 0.0020038 | 0.0021512 | 0.0022214 | 0.0025271 | 0.002896 | 0.0026985 | 0.0020319 | 0.0016911 | 0.0015578 | 0.0011428 | 0.0012189 | 0.00089115 | 0.00095129 | 0.0011869
 | 0 | 0.00084334 | 0.04185 | 0.015639 | 0.048421 | 0.050998 | 0.0938 | 0.10978 | 0.15743 | 0.20345 | 0.31854 | 0.47186 | 0.49752 | 0.63506 | 0.61677 | 0.70647 | 0.67641 | 0.7668 | 0.79868 | 0.83227 | 0.86122 | 0.85799 | 0.87665 | 0.8538 | 0.90342 | 0.92255 | 0.94291 | 0.97856 | 0.96628 | 1.0085 | 1.0046 | 1.0182 | 1.0449 | 1.044 | 1.0225 | 1.0464 | 1.0459 | 1.0346 | 1.0386 | 1.0356 | 1.061
(b) With FEC (System II)
(a) Without FEC (System I)
[gcm-3]
[gcm-3]
z [Å]
z [Å]
57 Å
39 Å
➤By adding FECs, the SEI film thick was found to be reduced by 32 %, meaning
that the SEI film can be efficiently formed by enhancing the aggregation.
Mass Density Distributions of SEI film and Electrolyte

## Slide 15
Smoothness of SEI Films – without and with FECs –
(b) With FEC (System II)
(a) Without FEC (System I)
VS.
➤In the FEC-added electrolyte, the surface structure of SEI film in contact with
the electrolyte became smooth by suppressing its undesirable growing.

## Slide 16
FEC
Additional Hybrid MC/MD Reaction Simulation
・ Same Simulation Model
・ Different Reaction Scheme
To clarify the effect of FEC reduction reactions on the SEI film formation, we have executed additional hybrid MC/MD reaction simulations which artificially restrict only the chemical reactions of FECs in the FEC-added electrolyte.
FEC-added electrolyte
(System II)
PC: 850
Na+: 87
PF6-: 85
FEC: 118

## Slide 17
Chart: 
| 0 | 40 | 80 | 120 | 160 | 200 | 240 | 280 | 320 | 360 | 400 | 440 | 480 | 520 | 560 | 600 | 640 | 680 | 720 | 760 | 800 | 840 | 880 | 920 | 960 | 1000 | 1040 | 1080 | 1120 | 1160 | 1200 | 1240 | 1280 | 1320 | 1360 | 1400 | 1440 | 1480 | 1520 | 1560 | 1600 | 1640 | 1680 | 1720 | 1760 | 1800 | 1840 | 1880 | 1920 | 1960 | 2000
NaPC (mono) | 0 | 1.023 | 2.2205 | 2.7043 | 3.307 | 3.4735 | 3.6718 | 3.8542 | 3.9018 | 3.9811 | 3.7432 | 3.5053 | 3.1484 | 2.9263 | 2.6091 | 2.1888 | 1.7606 | 1.5385 | 1.3958 | 1.3482 | 1.253 | 1.2213 | 1.2213 | 1.2372 | 1.2292 | 1.2372 | 1.1737 | 1.1341 | 1.1182 | 1.1023 | 1.1023 | 1.0865 | 1.0865 | 1.0706 | 1.0865 | 1.0944 | 1.0548 | 1.031 | 1.031 | 1.0389 | 1.023 | 1.0151 | 0.99924 | 0.99924 | 0.99924 | 0.99924 | 1.0151 | 0.98338 | 0.99131 | 0.99131 | 0.99131
NaPC (poly) | 0 | 0.015861 | 0.023791 | 0.071374 | 0.21412 | 0.38859 | 0.57099 | 0.80891 | 1.0944 | 1.372 | 1.713 | 2.0064 | 2.3157 | 2.5695 | 2.8629 | 3.1008 | 3.3387 | 3.4656 | 3.5528 | 3.5846 | 3.648 | 3.6718 | 3.6877 | 3.6877 | 3.6956 | 3.7035 | 3.7352 | 3.759 | 3.767 | 3.7749 | 3.7749 | 3.7749 | 3.7749 | 3.7828 | 3.7828 | 3.7828 | 3.7987 | 3.8146 | 3.8146 | 3.8146 | 3.8225 | 3.8225 | 3.8304 | 3.8304 | 3.8304 | 3.8304 | 3.8304 | 3.8463 | 3.8463 | 3.8463 | 3.8463
FEC | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579 | 9.3579
Na2CO3 | 0 | 0.071374 | 0.30929 | 0.79305 | 1.0072 | 1.4037 | 1.6654 | 1.8875 | 2.1016 | 2.2998 | 2.6091 | 2.9501 | 3.2674 | 3.5132 | 3.7035 | 3.9177 | 4.0207 | 4.1159 | 4.1794 | 4.1873 | 4.2111 | 4.2111 | 4.2111 | 4.219 | 4.2269 | 4.2428 | 4.2507 | 4.2507 | 4.2587 | 4.2745 | 4.2745 | 4.2904 | 4.2904 | 4.2904 | 4.2904 | 4.2904 | 4.2983 | 4.3062 | 4.3142 | 4.3221 | 4.3221 | 4.33 | 4.33 | 4.3459 | 4.3855 | 4.4014 | 4.4014 | 4.4014 | 4.4014 | 4.4014 | 4.4093
NaF | 0 | 0 | 0.015861 | 0.071374 | 0.071374 | 0.095166 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896 | 0.11896
PC | 67.409 | 66.2828 | 64.8316 | 63.7689 | 62.6665 | 61.7545 | 60.9298 | 60.0495 | 59.2168 | 58.3841 | 57.6307 | 56.9407 | 56.3618 | 55.8305 | 55.3705 | 55.1009 | 54.9502 | 54.8233 | 54.7281 | 54.7044 | 54.6488 | 54.633 | 54.6013 | 54.5775 | 54.5616 | 54.522 | 54.514 | 54.5061 | 54.4982 | 54.4823 | 54.4823 | 54.4823 | 54.4823 | 54.4823 | 54.4664 | 54.4585 | 54.4585 | 54.4426 | 54.4347 | 54.4189 | 54.4189 | 54.4189 | 54.4189 | 54.403 | 54.3633 | 54.3475 | 54.3316 | 54.3316 | 54.3237 | 54.3237 | 54.3158
PC
FEC
MC/MD cycles
[10-2Å-2]
[10-2Å-2]
NaPC
Na2DMBDC
Na2CO3
NaF
constant
Change in Number Densities and Consumed Electrons
Chart: 
| 0 | 40 | 80 | 120 | 160 | 200 | 240 | 280 | 320 | 360 | 400 | 440 | 480 | 520 | 560 | 600 | 640 | 680 | 720 | 760 | 800 | 840 | 880 | 920 | 960 | 1000 | 1040 | 1080 | 1120 | 1160 | 1200 | 1240 | 1280 | 1320 | 1360 | 1400 | 1440 | 1480 | 1520 | 1560 | 1600 | 1640 | 1680 | 1720 | 1760 | 1800 | 1840 | 1880 | 1920 | 1960 | 2000
 | 0 | 0.011975 | 0.029184 | 0.044728 | 0.057972 | 0.070978 | 0.08216 | 0.092866 | 0.10373 | 0.11356 | 0.12427 | 0.1345 | 0.14362 | 0.15123 | 0.15766 | 0.16273 | 0.16559 | 0.16828 | 0.16987 | 0.17058 | 0.17146 | 0.17154 | 0.17209 | 0.17249 | 0.17273 | 0.1732 | 0.17344 | 0.17352 | 0.17368 | 0.17399 | 0.17399 | 0.17415 | 0.17431 | 0.17431 | 0.17447 | 0.17455 | 0.17455 | 0.17479 | 0.17495 | 0.17518 | 0.17518 | 0.17526 | 0.17526 | 0.17542 | 0.17621 | 0.17653 | 0.17669 | 0.17677 | 0.17693 | 0.17701 | 0.17717
Total electron number: 0.18 [e Å-2]
MC/MD cycles
Consumed amount of electrons [eÅ-2]
・ By limiting the reduction reactions of FECs, the production of NaF complexes
was found to be drastically reduced.
・ The total consumed number of electrons per unit area of carbon anode was
obtained to be 0.18 [e Å-2], which is smaller than that without FECs (0.23).

## Slide 18
Mass Density Distributions of Reaction Products in SEI Film
➤The FEC addition should enhance forming the compact SEI film without the
presence of NaF complexes generated from FECs.
(They are obtained by different 10 initial configurations.)
39 Å
43 Å
57 Å
➤This means that the intact FECs strongly contribute the SEI film formation
on the anode surface.
(System I)
(System II)
(Additional simulation)

## Slide 19
Molecular Configurations of NaF in the SEI Film
Green: SEI film, Yellow: F-, Red CO32-
➤Most of NaF complexes (Yellow) came into the formation of inorganic
clusters by coordinating with the Na2CO3 complexes (Red) in the SEI film.
Front Views
➤The generated NaF should not contribute the enhancement in the SEI film
formation although such cluster size should increase by adding FECs.

## Slide 20
Intact FECs enhance the aggregation.
➤The intact FECs before reductive reaction should enhance the aggregation of
reaction products during the overall processes of SEI film formation owing to
the strong electronegativity of their fluorine atoms.
Bridge between reaction products
FEC
Na2DMBDC
NaPC
Na+
Figure. Typical snapshot of film formation process (500 MC/MD cycle)
Strong electronegativity
FEC
System II

## Slide 21
Summary
・The present simulations could reproduce the experimental observations that the irreversible capacity decreases by adding FEC.
・In the present study, we have investigated the microscopic FEC additive effect on the SEI film formation in the Na-ion battery with the hybrid MC/MD reaction method.
・By adding FECs, the SEI film thick was found to be reduced by suppressing its undesirable growing. This means that the SEI film can be effectively formed so as to decrease the irreversible capacity.
・Through the additional simulations which restrict only the FEC reduction, we concluded that the intact FECs strongly contribute to the SEI film formation owing to the strong electronegativity of their fluorine atoms.