## Slide 1
Masayoshi Takayanagi
Graduate School of Information Science, Nagoya University
Reactivity of Monomers with Radical Polymer Produced by Radical Copolymerization in a PCP channel
FY2015 The 9th CREST Workshop 2016, March 18

## Slide 2
Target system for radical copolymerization
Hexagonal channel in PCP framework
5-vinylisophthalic acid (S)
Compose wall of the hexagonal channel
Vinyl group exists in the channel
Acrylonitrile (A)
Filled in the hexagonal channel
+ AIBN
radical copolymerization of A and S
70℃, 48 h
S
A
A
A
Problem
How is the sequence?
A-A-S? A-A-A-S? A-A-A-A-S?
c
Cb
Cb

## Slide 3
Location between two S for radical elongation
⑨
⑩
⑪
Sequence
Locations between two S
In the previous report: To find the locations of S units to which terminal radical atom can approach, I executed replica exchange MD (REMD) simulations of several radical terminals (SAA･, SAAA･, SAAAA･).
vdW interaction between C･ and Cb
r = 3.816 Å
e = 0.0860 kcal/mol
EvdW(3.2 Å) = 0.217 kcal/mol
EvdW(2.7 Å) = 4.09 kcal/mol

## Slide 4
x
y
z
z
y
x
②
②
③
SAA･ terminal case
15 ns REMD trajectory at 343 K, save snapshots every 0.2 ps, 75,000 snapshots
If C･-Cb(S) distance is shorter than 3.2 Å, the Cb(S) is drawn by purple sphere.
Frequency of approach
② > ③
Shortest C･-Cb(S) distance location ② 2.765 Å location ③ 3.047 Å
Shortest C･-Cb(A) distance 2.874 Å

## Slide 5
DFT calculation of SAA･+S at location ②
From the shortest C･-Cb(S) distance (2.765 Å) snapshot at location ②, I executed DFT calculations to obtain the reaction barrier.
DFT calculation details and model system preparation ・DFT level at UM06-2X/6-311+G(2df,p)//UB3LYP/6-31G(d) in vacuum
・Extract SAA･ + S ・Substitute COO- groups of S units with H atoms This substitution resulted in less than 0.3 kcal/mol reaction barrier differences. ・Constrain substituted H and H-bound C atoms at the snapshot structure.
１．Optimize structure with C･-Cb(S) constraint at 3.2 Å (reactant)
２．Optimize TS structrure
３．Optimize product structure
0 kcal/mol
7.2 kcal/mol
-18.5 kcal/mol
Reaction barrier
Locations of atoms with red circles are constrained during optimizations.

## Slide 6
DFT calculation of SAA･+S at location ③
0 kcal/mol
9.9 kcal/mol
-19.4 kcal/mol
Constrain at 3.2 Å
TS
Product
3.2 Å
2.313 Å
1.568 Å
From the shortest C･-Cb(S) distance (3.047 Å) snapshot at location ③, I executed DFT calculations as that in location ②.

## Slide 7
DFT calculation of SAA･+A
0 kcal/mol
7.3 kcal/mol
-21.9 kcal/mol
Constrain at 3.2 Å
TS
Product
From the shortest C･-Cb(A) distance (2.874 Å) snapshot, I executed DFT calculations as that with S.
In this A case, the positional constraint of S is not imposed.
3.2 Å
2.298 Å
1.566 Å

## Slide 8
Discussion of reactivity of SAA･
Reaction barriers SAA･ + S (loc. ②) 7.2 kcal/mol SAA･ + S (loc. ③) 9.9 kcal/mol SAA･ + A 7.3 kcal/mol
SAA･ can react with A and S (loc. ②) with identical energy barrier.
However, the radical atom of SAAS･ produced by SAA･ + S(loc. ②) cannot approach to monomer A because the radical atom is completely covered by SAAS･ chain. (right Fig.)
→ SAAS･ (loc. ②) can be produced but the elongation reaction never proceeds from this. Thus, the reverse reaction SAAS･ to SAA･ + S should occur to elongate the radical chain.
Therefore, most of cases, SAA･ should react with monomer A.
A part of SAA･ can react with S at location ③. Energy barrier difference 2.6 kcal/mol exp( (2.6 kcal/mol) / kBT) ~ 2%

## Slide 9
SAAA･ terminal case
15 ns REMD trajectory at 343 K, save snapshots every 0.2 ps, 75,000 snapshots
If C･-Cb(S) distance is shorter than 3.2 Å, the Cb(S) is drawn by purple sphere.
Frequency of approach
③＞⑨＞⑤≒②＞④
Shortest C･-Cb(S) distance location ③ 2.812 Å location ② 3.133 Å location ⑨ 3.008 Å location ④ 3.141 Å location ⑤ 3.004 Å
Shortest C･-Cb(A) distance 2.862 Å
⑨

## Slide 10
DFT calculation of SAAA･+S at location ③
From the shortest C･-Cb(S) distance (2.812 Å) snapshot at location ③, I executed DFT calculations.
0 kcal/mol
8.7 kcal/mol
-22.0 kcal/mol

## Slide 11
DFT calculation of SAAA･+A
From the shortest C･-Cb(A) distance (2.862 Å) snapshot, I executed DFT calculations.
0 kcal/mol
9.8 kcal/mol
-26.8 kcal/mol
Constrain at 3.2 Å
TS
Product
3.2 Å
2.270 Å
1.566 Å

## Slide 12
Discussion of reactivity of SAAA･
Reaction barriers SAAA･ + S (loc. ③) 8.7 kcal/mol SAAA･ + A 9.8 kcal/mol
SAAA･ can react with A and S (loc. ②) with similar energy barrier.
If the energy difference 1.1 kcal/mol is meaningful (the accuracy of DFT calculations can be as large as 1 kcal/mol order), reactivity with S (loc. ③) is 5-times higher than that with A.
This suggests SAAA･ react with monomer S more than 80%. → consistent with experimental ratio A:S = 3:1
SAAAS･ can continue the elongation by its open radical atom.

## Slide 13
DFT calculation of SAAA･+S without constraint
0 kcal/mol
5.3 kcal/mol
-30.3 kcal/mol
Constrain at 3.2 Å
TS
Product
3.2 Å
2.339 Å
1.568 Å
From the shortest C･-Cb(S) distance (2.812 Å) snapshot at location ③, I executed DFT calculations without positional constraint.
The barrier 5.3 kcal/mol with S without positional constraint (lower than that with A, 9.8 kcal/mol) is consistent.
In bulk copolymerization of A and S, the alternating sequence ASASAS･･･ is reported, meaning that terminal A･ prefers S. To check this preference, I executed the reaction barrier of SAAA･ + S without constraint.

## Slide 14
Summary
SAA･
SAAS(②)･
No approach of monomer to the radical atom
Reverse rection to SAA･
SAAA･
SAAS(③)･
Reaction barrier 7.2 kcal/mol
9.9 kcal/mol
7.3 kcal/mol
SAAAS(③)･
SAAAA･
8.7 kcal/mol
9.8 kcal/mol
Main reaction
route
Main reaction route suggests the sequence of copolymer SAAASAAASAAA･･･
Consistent with the experimental ratio A:S = 3:1
DE = 2.6 kcal/mol gives 98:2 from exp(-DT/kBT)
DE = 1.1 kcal/mol gives 80:20 from exp(-DT/kBT)