## Slide 1: 4th CREST Workshop Uppula Purushotham
Sodium Ions as Electrolyte Additive for Lithium Ion Batteries

## Slide 2
In Na+ added electrolyte, the irreversible capacity is reduced, and a higher reversible capacity of 352 mAhg-1 was obtained.
The homogeneous, uniform and smooth SEI layer on the graphite surface was confirmed in Na added system.
Figure : Initial charge-discharge curves of natural graphite electrodes without and with Na+ additive (by dissolving 0.22 mol dm-3 NaClO4) in 1 mol dm-3 LiClO4/EC–DEC (1:1 by volume). Current density: 17 mA g-1.

## Slide 3
Z origin
34.1 Å
z
x
EC: 850
Li+: 69
PF6-: 80
Na+: 13
300.0 Å
Temperature ：298K
1.1M LiPF6 EC electrolyte + 0.22M NaPF6
Z origin
34.1 Å
z
x
EC: 850
Li+: 69
PF6-: 67
300.0 Å
Temperature ：298K
1.1M LiPF6 EC electrolyte
+ e-
+ e-
+
+ Li/NaEC
EC
EC-
Li/NaEC
C2H4
Li/NaCO3-
Li2 /Na2BDC
+ 2e-
+
3 ×
F-
PF6-
PF3
Li/NaF
+ Li+/Na+
Li+/Na+
Li+/Na+
Li2/Na2CO3
Model Systems and Reaction Scheme
In previous model system the concentration of Na+ ions are not resemble with experimental system.
Thus, I have estimated the volume of system by NPT ensemble simulation.
The concentration of 13 Na+ ions met the experimental criteria 0.22 mol/dm3.

## Slide 4
EC
BDC
CO3-2
PF3
C2H4
Na
Li
Reductive Products of EC Electrolyte
In both the systems the SEI film is formed by the combination of electrolyte reductive products after every MC/MD cycle.
200 Cycle
800 Cycle
1600 Cycle
2000 Cycle
Na-free EC electrolyte system
200 Cycle
800 Cycle
1600 Cycle
2000 Cycle
Na-added EC electrolyte system

## Slide 5
Li and Na atoms are distributed homogeneously in the Na-added system, which is responsible for smoother SEI film surface.
Comparison of Results
Na Na-added
Li Na-added
Li Na-free

## Slide 6
[10-3Å-2]
[10-3Å-2]
[10-3Å-2]
Figure : Comparison of the Change in the surface number densities of solvent molecules and reductive products with respect to the MC/MD cycles of EC electrolyte with Na added and Na free systems.
Surface Number Density Analysis
Chart: 
| 20 | 60 | 100 | 140 | 180 | 220 | 260 | 300 | 340 | 380 | 420 | 460 | 500 | 540 | 580 | 620 | 660 | 700 | 740 | 780 | 820 | 860 | 900 | 940 | 980 | 1020 | 1060 | 1100 | 1140 | 1180 | 1220 | 1260 | 1300 | 1340 | 1380 | 1420 | 1460 | 1500 | 1540 | 1580 | 1620 | 1660 | 1700 | 1740 | 1780 | 1820 | 1860 | 1900 | 1940 | 1980 | 2000
Li2/Na2BDC | 0 | 0.079 | 0.952 | 2.458 | 4.044 | 6.265 | 9.199 | 12.055 | 15.782 | 18.478 | 21.095 | 24.109 | 26.884 | 31.008 | 34.498 | 38.145 | 42.745 | 45.838 | 49.01 | 52.975 | 56.148 | 60.43 | 63.602 | 67.171 | 69.312 | 72.088 | 74.705 | 76.45 | 77.719 | 78.512 | 79.225 | 79.622 | 80.177 | 80.256 | 80.494 | 80.494 | 80.494 | 80.494 | 80.653 | 80.653 | 80.653 | 80.653 | 80.732 | 80.732 | 80.812 | 80.891 | 80.891 | 80.891 | 81.049 | 81.129 | 81.129
Li2/Na2CO3 | 0.714 | 3.331 | 5.392 | 6.582 | 8.01 | 9.358 | 10.231 | 10.944 | 11.896 | 12.61 | 13.958 | 14.592 | 15.544 | 16.337 | 17.685 | 18.954 | 20.223 | 21.809 | 23.395 | 24.902 | 27.122 | 29.026 | 30.453 | 31.881 | 32.912 | 34.735 | 35.608 | 36.401 | 36.877 | 37.511 | 37.67 | 37.828 | 37.908 | 38.066 | 38.146 | 38.225 | 38.225 | 38.225 | 38.384 | 38.463 | 38.542 | 38.621 | 38.621 | 38.621 | 38.621 | 38.621 | 38.621 | 38.621 | 38.78 | 38.78 | 38.78
Li/NaEC | 9.596 | 19.509 | 29.66 | 36.797 | 42.825 | 48.138 | 50.438 | 53.848 | 53.61 | 57.417 | 59.479 | 63.999 | 66.457 | 67.092 | 67.409 | 66.695 | 63.682 | 64.713 | 62.73 | 59.399 | 57.734 | 50.517 | 46.631 | 41.873 | 39.176 | 33.546 | 28.47 | 25.219 | 22.919 | 21.254 | 19.906 | 19.033 | 17.844 | 17.526 | 16.971 | 16.892 | 17.051 | 17.051 | 16.575 | 16.495 | 16.495 | 16.416 | 16.258 | 16.258 | 16.099 | 15.94 | 15.94 | 15.94 | 15.465 | 15.306 | 15.306
PF3 | 0.238 | 0.317 | 0.397 | 0.397 | 0.397 | 0.555 | 0.714 | 0.793 | 1.031 | 1.031 | 1.031 | 1.031 | 1.031 | 1.19 | 1.19 | 1.19 | 1.19 | 1.269 | 1.269 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348 | 1.348
LI/NaF | 0.476 | 0.714 | 0.952 | 0.952 | 0.952 | 0.952 | 1.19 | 1.427 | 1.903 | 2.062 | 2.062 | 2.062 | 2.062 | 2.141 | 2.3 | 2.379 | 2.379 | 2.538 | 2.617 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776 | 2.776
Li | 10.151 | 23.236 | 37.273 | 47.266 | 57.258 | 67.092 | 75.736 | 84.301 | 91.518 | 100.003 | 107.854 | 117.45 | 125.301 | 133.311 | 140.449 | 147.824 | 153.772 | 161.861 | 166.699 | 172.25 | 179.466 | 183.432 | 187.318 | 190.014 | 192.155 | 194.138 | 195.486 | 196.755 | 197.231 | 197.548 | 197.707 | 197.786 | 197.944 | 198.024 | 198.024 | 198.024 | 198.103 | 198.103 | 198.262 | 198.341 | 198.5 | 198.579 | 198.579 | 198.579 | 198.579 | 198.579 | 198.658 | 198.658 | 198.817 | 198.896 | 198.896
Na | 1.586 | 4.441 | 7.217 | 10.072 | 12.213 | 15.227 | 17.447 | 20.302 | 23.316 | 25.853 | 28.074 | 30.295 | 32.356 | 35.053 | 38.463 | 40.525 | 43.459 | 46.076 | 48.931 | 51.231 | 53.134 | 54.324 | 55.751 | 58.289 | 59.796 | 61.382 | 61.937 | 62.492 | 63.206 | 64.078 | 64.316 | 64.475 | 64.475 | 64.554 | 64.633 | 64.713 | 64.792 | 64.792 | 64.792 | 64.792 | 64.792 | 64.792 | 64.792 | 64.792 | 64.792 | 64.792 | 64.792 | 64.871 | 65.03 | 65.03 | 65.03
EC | 663.78 | 651.091 | 637.133 | 625.793 | 615.166 | 604.063 | 595.023 | 585.189 | 577.021 | 567.108 | 558.463 | 547.281 | 538.32 | 528.645 | 520.001 | 512.15 | 504.695 | 495.892 | 489.944 | 483.838 | 476.938 | 473.687 | 469.801 | 465.994 | 463.377 | 461.632 | 460.601 | 459.571 | 458.857 | 458.302 | 458.064 | 457.984 | 457.984 | 457.984 | 457.984 | 457.984 | 457.826 | 457.826 | 457.826 | 457.826 | 457.747 | 457.747 | 457.747 | 457.747 | 457.747 | 457.747 | 457.747 | 457.747 | 457.747 | 457.747 | 457.747
Chart: 
| 20 | 60 | 100 | 140 | 180 | 220 | 260 | 300 | 340 | 380 | 420 | 460 | 500 | 540 | 580 | 620 | 660 | 700 | 740 | 780 | 820 | 860 | 900 | 940 | 980 | 1020 | 1060 | 1100 | 1140 | 1180 | 1220 | 1260 | 1300 | 1340 | 1380 | 1420 | 1460 | 1500 | 1540 | 1580 | 1620 | 1660 | 1700 | 1740 | 1780 | 1820 | 1860 | 1900 | 1940 | 1980 | 2000
Li2/Na2BDC | 0 | 0.317 | 0.634 | 1.824 | 4.362 | 6.027 | 9.279 | 11.896 | 14.909 | 17.685 | 20.46 | 22.602 | 26.171 | 29.739 | 32.832 | 36.639 | 40.921 | 45.045 | 49.248 | 54.086 | 57.417 | 61.699 | 64.475 | 66.299 | 67.092 | 67.647 | 67.806 | 68.043 | 68.361 | 68.678 | 69.074 | 69.074 | 69.233 | 69.392 | 69.55 | 69.55 | 69.55 | 69.55 | 69.55 | 69.63 | 69.63 | 69.63 | 69.63 | 69.63 | 69.63 | 69.63 | 69.63 | 69.709 | 69.868 | 69.868 | 69.868
Li2CO3 | 0.881 | 3.348 | 6.08 | 8.635 | 10.222 | 11.632 | 12.865 | 14.011 | 15.068 | 15.949 | 16.478 | 17.095 | 18.769 | 19.738 | 21.5 | 22.822 | 24.408 | 26.435 | 28.021 | 29.695 | 31.458 | 33.132 | 33.925 | 34.277 | 34.718 | 34.806 | 34.894 | 35.247 | 35.247 | 35.335 | 35.511 | 35.687 | 35.687 | 35.775 | 35.775 | 35.775 | 35.863 | 35.863 | 35.863 | 35.863 | 35.951 | 35.951 | 36.04 | 36.04 | 36.04 | 36.04 | 36.04 | 36.04 | 36.04 | 36.04 | 36.04
LiEC | 9.676 | 19.112 | 29.026 | 34.418 | 37.908 | 44.49 | 46.076 | 49.328 | 51.231 | 53.927 | 57.496 | 63.761 | 62.889 | 63.523 | 63.206 | 62.016 | 58.289 | 55.513 | 50.755 | 44.173 | 39.335 | 30.612 | 25.06 | 21.729 | 20.143 | 19.112 | 18.954 | 18.319 | 17.844 | 17.368 | 16.495 | 16.337 | 16.099 | 15.702 | 15.385 | 15.385 | 15.306 | 15.306 | 15.306 | 15.147 | 15.068 | 15.068 | 14.989 | 14.989 | 14.989 | 15.068 | 15.068 | 14.989 | 14.672 | 14.672 | 14.672
PF3 | 0.079 | 0.159 | 0.238 | 0.238 | 0.476 | 0.476 | 0.476 | 0.555 | 0.634 | 0.634 | 0.714 | 0.714 | 0.714 | 0.714 | 0.714 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793 | 0.793
LI/NaF | 0.159 | 0.238 | 0.714 | 0.714 | 1.11 | 1.269 | 1.269 | 1.507 | 1.745 | 1.745 | 1.745 | 1.983 | 1.983 | 1.983 | 1.983 | 2.141 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22 | 2.22
Li | 11.5 | 27.281 | 44.252 | 57.258 | 69.709 | 82.953 | 93.659 | 104.682 | 115.151 | 125.381 | 135.611 | 148.062 | 157.658 | 167.492 | 176.929 | 186.049 | 193.979 | 203.099 | 209.602 | 215.947 | 221.656 | 224.988 | 226.891 | 228.318 | 229.111 | 229.349 | 229.825 | 230.301 | 230.459 | 230.777 | 231.015 | 231.173 | 231.252 | 231.332 | 231.332 | 231.332 | 231.411 | 231.411 | 231.411 | 231.411 | 231.49 | 231.49 | 231.57 | 231.57 | 231.57 | 231.649 | 231.649 | 231.728 | 231.728 | 231.728 | 231.728
EC | 663.621 | 650.774 | 637.451 | 627.141 | 616.911 | 605.65 | 596.371 | 586.775 | 577.814 | 568.614 | 558.939 | 547.599 | 539.748 | 530.945 | 523.332 | 515.639 | 509.295 | 501.999 | 496.923 | 492.244 | 488.517 | 486.93 | 485.979 | 485.106 | 484.71 | 484.551 | 484.234 | 484.076 | 483.917 | 483.679 | 483.6 | 483.6 | 483.52 | 483.52 | 483.52 | 483.52 | 483.52 | 483.52 | 483.52 | 483.52 | 483.52 | 483.52 | 483.52 | 483.52 | 483.52 | 483.441 | 483.441 | 483.362 | 483.362 | 483.362 | 483.362
MC/MD cycles
MC/MD cycles
Na added system
Na free system
The composition ratio of the reaction products became almost unchanged in the final stage, which shows the formation of SEI film.
The number of MC/MD cycles are increased to form SEI film after addition of Na ions.
In Na added system more electrolyte molecules (~26 molecules) are consumed to form SEI film.
1140
1060
457
483

## Slide 7
Figure: Comparison of mass density distribution of the final reductive products along Z axis incase of EC electrolyte with Na+ ions as additive (a) and with out Na+ ions as additive (b).
Mass Density Analysis
Thickness of the SEI film has been increased after addition of Na due to the more number of reductive products.
Z Å
Z Å
ρ [gcm-3]
ρ [gcm-3]
a)
b)
Chart: 
| 1 | 3 | 5 | 7 | 9 | 11 | 13 | 15 | 17 | 19 | 21 | 23 | 25 | 27 | 29 | 31 | 33 | 35 | 37 | 39 | 41 | 43 | 45 | 47 | 49 | 51 | 53 | 55 | 57 | 59
EC | 0 | 0 | 0 | 0.018 | 0.147 | 0.089 | 0.076 | 0.092 | 0.086 | 0.05 | 0.062 | 0.062 | 0.08 | 0.082 | 0.054 | 0.106 | 0.053 | 0.023 | 0.028 | 0.024 | 0.007 | 0.015 | 0.005 | 0 | 0 | 0 | 0 | 0 | 0 | 0
BDC | 0 | 0 | 0.119 | 0.429 | 0.911 | 0.911 | 1.031 | 1.011 | 0.873 | 0.969 | 1.006 | 0.862 | 0.951 | 0.765 | 0.732 | 0.516 | 0.296 | 0.27 | 0.173 | 0.114 | 0.101 | 0.025 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
CO3 | 0 | 0.005 | 0.203 | 0.33 | 0.336 | 0.204 | 0.121 | 0.105 | 0.063 | 0.068 | 0.107 | 0.104 | 0.051 | 0.048 | 0.046 | 0.044 | 0.024 | 0.035 | 0.012 | 0.025 | 0.007 | 0.002 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
F | 0 | 0 | 0 | 0 | 0.001 | 0.006 | 0.004 | 0.004 | 0.007 | 0.007 | 0.005 | 0.002 | 0.005 | 0.009 | 0.002 | 0.002 | 0.001 | 0.001 | 0.002 | 0.001 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
C2H4 | 0 | 0.046 | 0.503 | 0.091 | 0.065 | 0.025 | 0.025 | 0.01 | 0.01 | 0.01 | 0.008 | 0.006 | 0.003 | 0.002 | 0.004 | 0.002 | 0.002 | 0.002 | 0.002 | 0.003 | 0.004 | 0.006 | 0.006 | 0.007 | 0.008 | 0.007 | 0.005 | 0.005 | 0.005 | 0.004
PF3 | 0 | 0 | 0.045 | 0.01 | 0.008 | 0.004 | 0.006 | 0.002 | 0 | 0 | 0 | 0 | 0 | 0 | 0.005 | 0.001 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.001 | 0.002 | 0.002 | 0.003 | 0.003 | 0.002 | 0.002
Na | 0 | 0.015 | 0.049 | 0.109 | 0.108 | 0.105 | 0.086 | 0.064 | 0.066 | 0.058 | 0.056 | 0.059 | 0.049 | 0.059 | 0.059 | 0.039 | 0.028 | 0.026 | 0.028 | 0.021 | 0.011 | 0.009 | 0.003 | 0.001 | 0 | 0 | 0 | 0 | 0 | 0
Li | 0 | 0.002 | 0.031 | 0.08 | 0.117 | 0.118 | 0.106 | 0.084 | 0.073 | 0.072 | 0.087 | 0.081 | 0.087 | 0.062 | 0.053 | 0.035 | 0.033 | 0.023 | 0.018 | 0.02 | 0.012 | 0.003 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: 
| 1 | 3 | 5 | 7 | 9 | 11 | 13 | 15 | 17 | 19 | 21 | 23 | 25 | 27 | 29 | 31 | 33 | 35 | 37 | 39 | 41 | 43 | 45 | 47 | 49 | 51 | 53 | 55 | 57 | 59 | 61 | 63 | 65 | 67 | 69 | 71 | 73 | 75 | 77 | 79 | 81 | 83 | 85 | 87 | 89 | 91 | 93 | 95 | 97 | 99 | 101
EC | 0 | 0 | 0 | 0.013 | 0.097 | 0.081 | 0.091 | 0.1 | 0.118 | 0.083 | 0.122 | 0.072 | 0.065 | 0.093 | 0.07 | 0.054 | 0.019 | 0.005 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
BDC | 0 | 0 | 0.159 | 0.623 | 0.951 | 1.099 | 1.045 | 1.059 | 1.156 | 1.041 | 0.772 | 0.791 | 0.732 | 0.447 | 0.289 | 0.12 | 0.039 | 0.01 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
CO3 | 0 | 0.004 | 0.193 | 0.333 | 0.293 | 0.194 | 0.109 | 0.102 | 0.076 | 0.135 | 0.109 | 0.143 | 0.125 | 0.053 | 0.039 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
F | 0 | 0 | 0 | 0 | 0.002 | 0.005 | 0.004 | 0.005 | 0.005 | 0.004 | 0.005 | 0.011 | 0.002 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
C2H4 | 0 | 0.043 | 0.47 | 0.082 | 0.083 | 0.028 | 0.022 | 0.008 | 0.006 | 0.005 | 0.002 | 0.003 | 0.004 | 0.002 | 0.003 | 0.005 | 0.003 | 0.003 | 0.003 | 0.004 | 0.005 | 0.005 | 0.006 | 0.007 | 0.006 | 0.006 | 0.005 | 0.005 | 0.005 | 0.004 | 0.005 | 0.005 | 0.004 | 0.001 | 0.001 | 0.001 | 0 | 0 | 0 | 0 | 0 | 0.002 | 0.009 | 0.015 | 0.011 | 0.005 | 0.003 | 0 | 0 | 0 | 0
PF3 | 0 | 0 | 0.032 | 0.009 | 0.016 | 0.001 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.003 | 0.002 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Li | 0 | 0.003 | 0.041 | 0.111 | 0.158 | 0.147 | 0.131 | 0.103 | 0.108 | 0.11 | 0.116 | 0.106 | 0.092 | 0.065 | 0.035 | 0.017 | 0.006 | 0.002 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0

## Slide 8
Figure: Comparison of the SEI film thickness based on percentage of Li along the Z-axis incase of EC electrolyte with Na+ ions as additive and EC electrolyte with out Na+ ions.
Z-axis Å
Thickness of SEI Film Based on Li Atom Percentage
Percentage of Li
Chart: 
| 1 | 3 | 5 | 7 | 9 | 11 | 13 | 15 | 17 | 19 | 21 | 23 | 25 | 27 | 29 | 31 | 33 | 35 | 37 | 39 | 41 | 43 | 45 | 47 | 49 | 51
EC_20%Na | 0 | 2.034 | 25.932 | 67.542 | 99.237 | 100 | 89.831 | 70.763 | 62.203 | 60.847 | 73.475 | 68.305 | 73.814 | 52.627 | 44.746 | 29.661 | 28.051 | 19.831 | 15.424 | 16.61 | 9.915 | 2.373 | 0.339 | 0 | 0 | 0
EC_NoNa | 0 | 1.893 | 22.831 | 70.147 | 99.982 | 87.316 | 81.085 | 61.397 | 62.279 | 66.36 | 71.471 | 69.026 | 59.614 | 39.375 | 20.809 | 10.625 | 3.511 | 0.901 | 0.018 | 0 | 0 | 0 | 0 | 0 | 0 | 0
EC_20%Na (0Å to 41Å)
EC_NoNa (0Å to 31Å)
In Na added system the thickness of SEI film has been increased by 10Å.

## Slide 9
The ratio of fractional accessible volume in the interface structure of Na added EC-based electrolyte is 0.27
Standard deviation is 0.02
The ratio of fractional accessible volume in the interface structure of Na added EC-based electrolyte is 0.27
Standard deviation is 0.01
Na added EC electrolyte
Na free EC electrolyte
Cavity size
In both the systems ratio of fractional accessible volume is similar.

## Slide 10
Figure: Comparison of amount of electrons consumed during the formation of SEI film incase of EC electrolyte with Na+ ions as additive and EC electrolyte with out Na+ ions.
Chart: 
| 20 | 60 | 100 | 140 | 180 | 220 | 260 | 300 | 340 | 380 | 420 | 460 | 500 | 540 | 580 | 620 | 660 | 700 | 740 | 780 | 820 | 860 | 900 | 940 | 980 | 1020 | 1060 | 1100 | 1140 | 1180 | 1220 | 1260 | 1300 | 1340 | 1380 | 1420 | 1460 | 1500 | 1540 | 1580 | 1620 | 1660 | 1700 | 1740 | 1780 | 1820 | 1860 | 1900 | 1940 | 1980 | 2000
EC_NoNa | 14.4 | 34.3 | 54.8 | 71 | 86.6 | 102.5 | 115.7 | 129.4 | 142.2 | 155 | 168.1 | 183.4 | 195.3 | 207.7 | 219.5 | 231 | 240.9 | 252.4 | 260.6 | 268.5 | 275.6 | 279.8 | 282.2 | 284 | 285 | 285.3 | 285.9 | 286.5 | 286.7 | 287.1 | 287.4 | 287.6 | 287.7 | 287.8 | 287.8 | 287.8 | 287.9 | 287.9 | 287.9 | 287.9 | 288 | 288 | 288.1 | 288.1 | 288.1 | 288.2 | 288.2 | 288.3 | 288.3 | 288.3 | 288.3
EC_20%Na | 15 | 34 | 54 | 70 | 85 | 102 | 114 | 128 | 140 | 153 | 166 | 181 | 193 | 207 | 220 | 231 | 242 | 255 | 265 | 275 | 286 | 293 | 299 | 306 | 311 | 315 | 318 | 320 | 321 | 323 | 323 | 324 | 324 | 324 | 324 | 324 | 324 | 324 | 325 | 325 | 325 | 325 | 325 | 325 | 325 | 325 | 325 | 325 | 325 | 325 | 325
Number of electrons consumed
MC/MD cycles
324
288
The total consumed number of electrons for the formation of SEI film has been estimated by adding electrons in each MC/MD cycle in the present simulations.
More number of electrons are consumed to form SEI film in Na added EC electrolyte than Na free electrolyte.
The present results could not reproduce the experimental observation that the irreversible capacity is decreased by adding Na ions.
Consumed Number of Electrons to Form SEI Film

## Slide 11
Addition of Na ions increased the consumption of EC molecules (~32) and formation of CO3-2 molecules (~4).
Figure: Comparison of the number of CO3-2 and EC molecules used in SEI film formation of Na added and Na free EC electrolyte systems.
Chart: 
| 20 | 60 | 100 | 140 | 180 | 220 | 260 | 300 | 340 | 380 | 420 | 460 | 500 | 540 | 580 | 620 | 660 | 700 | 740 | 780 | 820 | 860 | 900 | 940 | 980 | 1020 | 1060 | 1100 | 1140 | 1180 | 1220 | 1260 | 1300 | 1340 | 1380 | 1420 | 1460 | 1500 | 1540 | 1580 | 1620 | 1660 | 1700 | 1740 | 1780 | 1820 | 1860 | 1900 | 1940 | 1980 | 2000
Li2CO3_20%Na | 0.714 | 3.093 | 4.917 | 6.106 | 7.217 | 8.089 | 8.803 | 9.358 | 10.072 | 10.627 | 11.658 | 12.213 | 13.086 | 13.641 | 14.434 | 15.623 | 16.654 | 18.161 | 19.192 | 20.302 | 22.205 | 23.712 | 24.902 | 25.695 | 26.25 | 27.439 | 28.233 | 28.708 | 28.946 | 29.184 | 29.264 | 29.343 | 29.422 | 29.501 | 29.501 | 29.501 | 29.501 | 29.501 | 29.66 | 29.739 | 29.819 | 29.898 | 29.898 | 29.898 | 29.898 | 29.898 | 29.898 | 29.898 | 29.977 | 29.977 | 29.977
Na2CO3_20%Na | 0.079 | 0.317 | 0.634 | 0.634 | 0.952 | 1.507 | 1.665 | 1.824 | 2.062 | 2.22 | 2.617 | 2.696 | 2.776 | 3.013 | 3.648 | 3.727 | 3.965 | 4.044 | 4.599 | 4.996 | 5.472 | 5.868 | 6.186 | 6.9 | 7.375 | 8.168 | 8.248 | 8.565 | 8.803 | 9.2 | 9.279 | 9.358 | 9.358 | 9.437 | 9.517 | 9.596 | 9.596 | 9.596 | 9.596 | 9.596 | 9.596 | 9.596 | 9.596 | 9.596 | 9.596 | 9.596 | 9.596 | 9.596 | 9.675 | 9.675 | 9.675
Li2CO3_No_Na | 0.881 | 3.348 | 6.08 | 8.635 | 10.222 | 11.632 | 12.865 | 14.011 | 15.068 | 15.949 | 16.478 | 17.095 | 18.769 | 19.738 | 21.5 | 22.822 | 24.408 | 26.435 | 28.021 | 29.695 | 31.458 | 33.132 | 33.925 | 34.277 | 34.718 | 34.806 | 34.894 | 35.247 | 35.247 | 35.335 | 35.511 | 35.687 | 35.687 | 35.775 | 35.775 | 35.775 | 35.863 | 35.863 | 35.863 | 35.863 | 35.951 | 35.951 | 36.04 | 36.04 | 36.04 | 36.04 | 36.04 | 36.04 | 36.04 | 36.04 | 36.04
Chart: 
| 20 | 60 | 100 | 140 | 180 | 220 | 260 | 300 | 340 | 380 | 420 | 460 | 500 | 540 | 580 | 620 | 660 | 700 | 740 | 780 | 820 | 860 | 900 | 940 | 980 | 1020 | 1060 | 1100 | 1140 | 1180 | 1220 | 1260 | 1300 | 1340 | 1380 | 1420 | 1460 | 1500 | 1540 | 1580 | 1620 | 1660 | 1700 | 1740 | 1780 | 1820 | 1860 | 1900 | 1940 | 1980 | 2000
EC_No Na | 13.2 | 29.4 | 46.2 | 59.2 | 72.1 | 86.3 | 98 | 110.1 | 121.4 | 133 | 145.2 | 159.5 | 169.4 | 180.5 | 190.1 | 199.8 | 207.8 | 217 | 223.4 | 229.3 | 234 | 236 | 237.2 | 238.3 | 238.8 | 239 | 239.4 | 239.6 | 239.8 | 240.1 | 240.2 | 240.2 | 240.3 | 240.3 | 240.3 | 240.3 | 240.3 | 240.3 | 240.3 | 240.3 | 240.3 | 240.3 | 240.3 | 240.3 | 240.3 | 240.4 | 240.4 | 240.5 | 240.5 | 240.5 | 240.5
EC_20%Na | 13 | 29 | 47 | 61 | 74 | 88 | 100 | 112 | 122 | 135 | 146 | 160 | 171 | 183 | 194 | 204 | 214 | 225 | 232 | 240 | 249 | 253 | 258 | 262 | 266 | 268 | 269 | 271 | 271 | 272 | 272 | 273 | 273 | 273 | 273 | 273 | 273 | 273 | 273 | 273 | 273 | 273 | 273 | 273 | 273 | 273 | 273 | 273 | 273 | 273 | 273
MC/MD cycles
MC/MD cycles
Number of CO3-2 Molecules
Number of EC Molecules
36
30
10
273
241
Various Reductive Products

## Slide 12
Conclusions
Homogeneous distribution of Na and Li atoms are appeared in the Na-added system.
After addition of Na the thickness of SEI film has increased by 10Å.
More number of electrons are consumed to form SEI film in Na added system than Na free system, which could not reproduce the experimental observation that the irreversible capacity is decreased by adding Na ions.
In next plan we would like to improve the simulation results by adding the effect of solvent co-interaction on graphite in the MC/MD simulations.

## Slide 13
Background of Present Research
According to the experimental results[1], fluoroethylene carbonate (FEC) is the only an effective additive for Na-ion battery among the FEC, DFEC, VC and ES.
The FEC addition improved the cycle performance by decreasing the irreversible capacity to form the SEI film. In case of DFEC, performance is decreased by lowering reversible capacity.
In the present study we would like to investigate the origin of mechanism to form SEI film in DFEC additive PC electrolyte Na-ion battery.
In this regard we have planned to compare the MC/MD simulation results of FEC and DFEC additive PC electrolyte Na-ion battery.
Figure : Reversible capacity versus cycle number plot of PC electrolyte Na-ion battery.
[1] S. Komaba et al., ACS Appl. Mater. Interfaces, 3, 4165 (2011).

## Slide 14
+ e-
PC3
DF3
DF3
+ e-
DF_PC
C2F2
CO3
Na2CO3
DF2
DF1
DF4
Di-Fluoro Ethylene Carbonate Reaction Route
DF_F
+ e-
DF_A
DF_G
DF_H
DFC2OF
CO2
reaction route_1
reaction route_2
To perform MC/MD simulation, I have prepared the reaction scheme which consists a list of elementary reactions involved in the formation of SEI film.
The reaction scheme of DFEC has been prepared similar to the FEC reaction scheme[2].
The reaction profile of DFEC also modelled by using DFT methods.
[2] P. B. Balbuena et al. J. Electrochem. Soc. 161, A213 (2014).

## Slide 15
Chart: 
| DF1_Na | DF1_Na_IN1 | DF_Na_TS1 | DF1_Na_IN2 | DF_Na_TS2 | DF_C2F2_CO3
 | 0 | -5.3289 | 16.4077 | -15.3309 | 9.0389 | -50.0536
 | 0 | -21.0531 | -6.7809 | -40.5065 | -14.7146 | -130.852
Relative energy in kcal/mol
11.080
14.272
Gas phase
Solvent phase
6.292
25.793
Method: B3LYP/6-31+G(d)
Solvent: Propylene carbonate
Reaction products
Figure: Computed reaction profile for Di-fluoro ethylene carbonate reaction route_1.
Reaction Profile of DFEC

## Slide 16
Chart: 
| DFEC_A | DFEC_TS1 | DFEC_F | DFEC_TS2 | DFEC_G | DFEC_H | DFEC_TS3 | DFEC_C2OF_CO2
Gas phase | 0 | 14.302 | 3.654 | 4.548 | 2.846 | 26.11 | 33.322 | -8.007
Solvent phase | 0 | 1.645 | -15.328 | -13.414 | -17.735 | -10.437 | -3.553 | -44.487
Relative energy in kcal/mol
10.648
1.702
13.638
4.321
7.212
6.884
Reaction products
Method: B3LYP/6-31+G(d)
Solvent: Propylene carbonate
Figure: Computed reaction profile for Di-fluoro ethylene carbonate reaction route_2.
Reaction Profile of DFEC

## Slide 17
Conclusions and Future Plan
The DFEC reaction route_2 is preferable than reaction route_1, which is also similar in case of FEC.
To prepare the DFEC model system for MC/MD simulations I have to estimate the volume of DFEC molecules.
By using that information I will prepare the model system which resembles with experimental conditions.
Further I will perform the MC/MD simulations on the above system.

## Slide 18
THANK YOU