## Slide 1
FY2015’s 5th, CREST Workshop
Norio Takenaka1,2
Graduate School of Information Science, Nagoya University1,
Elements Strategy Initiative for Catalysts and Batteries (ESICB), Kyoto University2
Theoretical Investigation of Ion Transport Pathway in Solid Electrolyte Interphase Film
Tue. Oct. 6th

## Slide 2: Background
・Li+ (or Na+) transfer at an anode/electrolyte interface is an essential process of the charge-discharge reaction in LIB (or NIB).
Fig. Schematic illustrations of an anode/electrolyte interface
・According to experimental investigations, there are two possibilities of the rate-determining step on this process, i.e., (1) desolvation of Li+ (or Na+) and (2) Li+ (or Na+) transfer inside the SEI film.
It is necessary to investigate the ion transfer at the atomistic level.

## Slide 3: Purpose of Present Research
・Recently, we could obtain the realistic computational models of SEI film using a hybrid MC/MD reaction method [1,2].
[1] NT et al., J. Phys. Chem. C, 118(20), 10874 (2014); [2] NT et al., J. Phys. Chem. C, 119(32), 18046 (2015).
e-
Hybrid MC/MD
reaction simulation
・Using these computational models, the ion transport pathways in the SEI film have been investigated without and with additives (i.e., FEC or DFEC).
SEI

## Slide 4: Model System
SEI film
(a) Side View (SEI film, surface view; Na+ and PF6-, van der Waals view; PC and Gas, stick view)
(b) Front view of SEI film from the side of anode
(0 < z < 20 Å)
Anode
・ For this purpose, I employed the system including NaPF6-PC electrolyte solution and SEI film without and with FEC or DFEC additives.
Species in SEI film

## Slide 5
Algorithm to obtain migration pathway of Na+
・The migration pathways were investigated by using a following procedure.
(1) First, the total system is divided to discrete grid points (grid size = 0.3 Å).
(2) Next, at each grid point, we obtain a sphere which contacts with the SEI film.
If the radius R is smaller than a van del Waals radii of Na+ (1.84 Å), this grid
point becomes the possible cavities for the migration pathway.
(3) Finally, we connect the cavities from the anode surface to the bulk electrolyte
to search for the migration pathways as the connective cavities.
Grid point
R
SEI

## Slide 6
One of obtained migration pathway
z [Å]
Chart: 
| 4.3999999999999986 | 5.3999999999999986 | 6.3999999999999986 | 7.3999999999999986 | 8.3999999999999986 | 9.3999999999999986 | 10.399999999999999 | 11.399999999999999 | 12.399999999999999 | 13.399999999999999 | 14.399999999999999 | 15.399999999999999 | 16.399999999999999 | 17.399999999999999 | 18.399999999999999 | 19.399999999999999 | 20.399999999999999 | 21.4 | 22.4 | 23.4 | 24.4 | 25.4 | 26.4 | 27.4
 | 5.164 | 5.4049 | 4.8755 | 4.2813 | 4.0191 | 3.9767 | 4.0009 | 3.9428 | 3.782 | 3.631 | 3.5924 | 3.5703 | 3.6422 | 3.8858 | 3.9725 | 4.0554 | 4.3955 | 4.7077 | 5.1675 | 5.945 | 6.5202 | 6.9489 | 7.2825 | 7.661
origin of z axis
Purple: migration pathway
Fig. Change in the cavity radius
Rmin = 3.8 Å
・ This pathway must be reasonable because the minimum radius Rmin (3.8 Å) on the pathway was larger than a van del Waals radii of Na+ (1.84 Å).
R [Å]
(anode)
(bulk electrolyte)

## Slide 7
SEI film and migration pathway of Na+ (without additive)
1 pathway
No pathway
No pathway
1 pathway
No pathway
No pathway
1 pathway
No pathway
1 pathway
1 pathway
10 Å
Number of pathways：5, Average of minimum radius：2.6 Å
➤ There were some pathways in the SEI film obtained by the hybrid MC/MD reaction method. Actually, such cavities were formed by the organic salts.
Front view of SEI film

## Slide 8
10 Å
2 pathways
1 pathway
1 pathway
1 pathway
1 pathway
1 pathway
1 pathway
1 pathway
1 pathway
No pathway
➤Since the surface of SEI film became smooth by adding FEC, the number of pathways was found to increase.
Front view of SEI film
Number of pathways：10, Average of minimum radius：2.8 Å
SEI film and migration pathway of Na+ (with FEC)

## Slide 9
10 Å
2 pathways
1 pathway
2 pathways
No pathway
1 pathway
2 pathways
1 pathway
2 pathways
1 pathway
2 pathways
➤Although the number of pathways increased by adding DFEC, the average of minimum radius increased in comparison to that in the FEC-added SEI film.
SEI film and migration pathway of Na+ (with DFEC)
Front view of SEI film
Number of pathways：14, Average of minimum radius：3.1 Å

## Slide 10
z [Å]
Solvation number
Chart: 
| 4.3999999999999986 | 5.3999999999999986 | 6.3999999999999986 | 7.3999999999999986 | 8.3999999999999986 | 9.3999999999999986 | 10.399999999999999 | 11.399999999999999 | 12.399999999999999 | 13.399999999999999 | 14.399999999999999 | 15.399999999999999 | 16.399999999999999 | 17.399999999999999 | 18.399999999999999 | 19.399999999999999 | 20.399999999999999 | 21.4 | 22.4 | 23.4 | 24.4 | 25.4 | 26.4 | 27.4
 | 5.164 | 5.4049 | 4.8755 | 4.2813 | 4.0191 | 3.9767 | 4.0009 | 3.9428 | 3.782 | 3.631 | 3.5924 | 3.5703 | 3.6422 | 3.8858 | 3.9725 | 4.0554 | 4.3955 | 4.7077 | 5.1675 | 5.945 | 6.5202 | 6.9489 | 7.2825 | 7.661
z [Å]
Solvation number of ion on a migration pathway
(b) Change in the cavity radius
(a) Solvation number
R [Å]
・It was found that the solvation number decreases as the ion moves from the bulk electrolyte to anode surface.
・The solvation number around the Na+ was estimated by executing 1.0 ns MD simulations, fixing only the z coordinate at each positon.
Chart: 
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30
 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.986 | 0.734 | 0.097 | 0.619 | 2.518 | 0.461 | 2.857 | 4.09 | 2.388 | 4.493
(anode)
(anode)

## Slide 11: Summary
・In the present study, I have investigated the migration pathways of Na+ in the SEI film by using a new algorithm.
・It was found that the solvation number decreases as the ion moves from the bulk electrolyte to anode surface.
・By using the present algorithm, all the possible pathways can be obtained at the lower calculation cost than that of the TMD method.
・As a result, the number of pathways were found to increase by adding the additives into the electrolyte.
・In future, the activation free energy should be estimated on the obtained pathways to compare it with the experimental values.

## Slide 12: Thank you for your attention