## Slide 1
Masayoshi Takayanagi
Graduate School of Information Science, Nagoya University
Tacticity of dimeric and trimeric MMA radicals estimated by DFT calculation
DFT 計算による二量体・三量体 MMA ラジカルの 立体規則性（タクティシティ）解析
2015/February/10

## Slide 2
Tacticity of polymethyl methacrylate (PMMA) (known as "acrylic resin" アクリル樹脂)
Tacticity is defined by the extended conformation of the polymer.
Tacticity of diad (by two adjacent groups) racemo (r) CH3 group on the opposite side meso (m) CH3 group on the same side
Tacticity of triad (by three adjacent groups) rr, rm, mr, mm
Tacticity of Tetrad (by four adjacent groups) rrr, rrm, rmr, mrr, rmm, mrm, mmr, mmm
Tacticity of Pnetad, Hexad, ...
m
r
r
diad
rm
mr
triad
rmr
tetrad

## Slide 3
Tacticity of PMMA produced by bulk & inside PCP polymerization
Tacticity of PMMA can be controlled by using PCP channels for radical polymerization.
1 = Cu, 2 = Zn b c d
Macromolecules 2008, 41, 87.
Tacticity of product PMMA (meso diad ratio)
In bulk 22% In (1) X=Cl 30%
In 2b 28% In (1) X=NH2 27%
In 2c 30% In (1) X=CH3 36%
In (2) X=CH3 37%
In (2) X=OCH3 53%
JACS 2010, 132, 4917–4924.
Tacticity observation by H1 NMR

## Slide 4
Before MC/MD polymerization simulation, check the GAFF force field quality for tacticity prediction
Energy difference of each conformers are very small.
Check the force field (GAFF) parameters of PMMA.
For this purpose, I first need the most stable conformers of small oligomers. (dimer, trimer, ...)
Methyl methacrylate (MMA) monomers confined in the PCP channels
Most stable
+0.154 kcal/mol

## Slide 5
MMA monomer
MMA radical
Check the DFT functional and basis sets
B3LYP (ROB3LYP) / 6-31G(d,p) is good enough
Focus on the energy difference with respect to the most stable structure
&
Check the consistency with a reference calculation by
MP2/cc-pvtz
ROB3LYP is faster than UB3LYP
Single point calculation of the MMA radical (4 CPU parallel)
UB3LYP/6-31G(d,p) 27 sec
ROB3LYP/6-31G(d,p) 22 sec
B3LYP (ROB3LYP) / 6-311G(d,p) is better than 6-31G(d,p)

## Slide 6
radical
C5
O2
C4
O1
O2
C3
C4
O1
C5
CT
mmm residue
(methyl methacrylate middle)
mrd residue
(methyl methacrylate radical)
Angles in this conformation
Many conformations even in the dimer radical
tmt residue
(terminal methyl)
Rough estimation: each dihedral angle (7 dihedrals) has 2~3 stable angles
conformers
C1
C2
C3
C2
C1

## Slide 7
racemoOpt.log DE = 0 kcal/mol (as a standard)
racemoOpt2.log DE = -0.63 kcal/mol
Most stable?
180° rotation & opt
180° rotation & opt
racemoOpt4.log DE = +0.42 kcal/mol
+70° rotation & opt
racemoOpt5.log
DE = +0.51 kcal/mol
Manual optimization to search the most stable conformation UB3LYP/6-311G(d,p)
Very difficult to obtain the most stable conformation by manual search → Necessity of automatic search

## Slide 8
Automatic conformation search by classical MD simulation in vacuum
Prepare MMA dimer radical prmtop file with GAFF force field (with the radical "cr" atom type)
Execute conformation sampling MD (CSMD) simulation of MMA dimer radical in vacuum for 100 ns at high temperature 500 K, reset velocity every 5 ps from a Maxwellian distribution at 500 K ignore dihedral angle & improper terms (set 0 weight) save snapshots every 10 ps, in total 10,000 snapshots
mdin for CSMD in AMBER pmemd MD solver, repeat 1000 times
&cntrl
DT = 0.002, NSTLIM = 50000,
NTB = 0, CUT = 99,
NTT = 1, TEMP0 = 500, VRAND=2500, TAUTP=0.5
ntpr = 2500, ntwx = 2500,
nmropt = 1,
&end
&wt
type='TORSION', value1 = 0.0,
&end
&wt
type='IMPROP', value1 = 0.0,
&end
&wt
type='END',
&end
Weight 0 for dihedral (torsion) and improper terms
During the CSMD, all the dihedral angles frequently rotate without barrier.
All the 10,000 CSMD snapshots are optimized by MM force field.
Classify the 10,000 optimized snapshots into 500 clusters by clustering with k-means method. More than two clusters often have the same conformation.
Extract a representative structure from each cluster (in total, 500 representative structures).
All 500 representative structures are optimized by DFT calculation (Gaussian09) ROB3LYP/6-31G(d,p) ROB3LYP/6-311G(d,p)
Check the most stable structure & distribution of energy.
CSMD
MM optimization & clustering
Cluster ID
1
2
3
4&5

## Slide 9
most stable in page 7
Most stable 12 conformers by ROB3LYP/6-31(d,p)
most stable
+0.04 kcal/mol
+0.09 kcal/mol
+0.13 kcal/mol
+0.25 kcal/mol
+0.33 kcal/mol
+0.39 kcal/mol
+0.62 kcal/mol
+0.65 kcal/mol
+0.76 kcal/mol
+0.81 kcal/mol
+0.91 kcal/mol

## Slide 10
most stable in page 7
Most stable 12 conformers by ROB3LYP/6-311(d,p)
most stable
+0.06 kcal/mol
+0.12 kcal/mol
+0.18 kcal/mol
+0.27 kcal/mol
+0.36 kcal/mol
+0.61 kcal/mol
+0.83 kcal/mol
+0.85 kcal/mol
+0.39 kcal/mol
not in 6-31G(d,p) 12 confomers
+0.65 kcal/mol
+0.73 kcal/mol
not in 6-31G(d,p) 12 confomers
not in 6-31G(d,p) 12 confomers

## Slide 11
Density of conformers against relative energy in a dimer radical
ROB3LYP/6-31(d,p)
ROB3LYP/6-311(d,p)
Relative energies of several conformers differ between 6-31G(d,p) and 6-311G(d,p).
However, most stable conformers (in this case, up to 8) are common with almost the same relative energy.
The 6-31(d,p) is good enough to estimate the most stable conformers and relative energies.
in total, 113 confomers
in total, 121 confomers

## Slide 12
Conformatio Sampling MD (CSMD) for trimer radical
The dimer radical has one chiral carbon and there is a pair of enantiomers. There is no physical quantity (energy) difference between a pair of enantiomers, so I ignored chirality.
The trimer radical has two chiral carbons and there are enantiomers and diastereomers. There are physical quantity (energy) differences between diastereomers, so it is necessary to consider chirality to sample all possible configurations of a trimer radical.
Add chiral inversion process to the CSMD process.
Execute CSMD for 100 ps, and select one chiral carbon by random number and invert CH3 - COOCH3 groups by reflection. After reflection, minimize the structure to remove steric collisions created by the inversion.
chiral carbon
chiral inversion by reflection
Repeat 100 ps CSMD & chiral inversion for 1,000 times, in total 100 ns trajectory with 10,000 snapshots.
Optimize with ROB3LYP/6-31G(d,p) level of DFT calculation.
a pair of enantiomers

## Slide 13
C3
C2
C3
C2
C2
C3
C1
C1
C1
C3
C2
C3
C2
C2
C3
C1
C1
C1
Definition of tacticity & enantiomer elimination
A pair of enantiomers have the same energy, so I don't focus on the enantiomers.
Enantiomer elimination was realized as follows. when the dihedral angle Dt = (C1-C2-C2-C1) < 0˚, multiply -1 to D.
Tacticity of a trimer radical can be defined as D = Dihedral (C1-C2-C2-C1) - Dihedral (C3-C2-C2-C3)
-60˚ < D < 60˚ → meso otherwise → racemo
Dihedral (C1-C2-C2-C1) = 93˚ Dihedral (C3-C2-C2-C3) = -26˚
D = 93 - (-26) = 119˚
racemo
rotate toward extended conformer
Dihedral (C1-C2-C2-C1) = -117˚ Dihedral (C3-C2-C2-C3) = -104˚
D = (-117) - (-104) = -13˚
meso

## Slide 14
Most stable 12 conformers of a trimer radical
most stable
+0.13 kcal/mol
+0.17 kcal/mol
+0.41 kcal/mol
+0.45 kcal/mol
+0.58 kcal/mol
+0.63 kcal/mol
+0.65 kcal/mol
+0.68 kcal/mol
+0.74 kcal/mol
+0.75 kcal/mol
+0.80 kcal/mol
meso
meso
racemo
racemo
racemo
racemo
racemo
racemo
racemo
racemo
racemo
racemo

## Slide 15
Density of conformers against relative energy in a trimer radical
Estimated tacticity ratio well corresponds with experimental bulk polymerization products.
Diad | racemo | meso
No. conformers | 209 | 221
Ratio | 75.5% | 24.5%
bulk polymerization | 78% | 22%
r
r
m
r
r
m
Relative energy (kcal/mol) | Diad | Ratio by Boltzmann factor
0.00 | r | 6.54%
0.13 | r | 5.40%
0.17 | r | 5.09%
0.41 | r | 3.61%
0.45 | r | 3.38%
0.58 | m | 2.79%
0.63 | m | 2.61%
0.65 | r | 2.52%
... | ... | ...

## Slide 16
Reason of the very unstable conformers (>15 kcal/mol)
Most unstable conformer (+17.70 kcal/mol)
By the rotation of the CH3 at the COOCH3 group.
Future work
Execute tetramer (4-mer) and hexamer (6-mer) radical calculations. - Check higher order tacticity - Check the dependency of tacticity on the radical length
Discuss how the PCP channel space enhances the meso tacticity.
Check the quality of GAFF force field to predict conformers with enough accurate energy. If the correspondence is bad, modify the force field parameters.