## Slide 1: Graphene Electrode Dependency on the Reduction Mechanism of Propylene Carbonate in Sodium-ion Batteries: A Density Functional Theory Study
25/7/2016
1
CREST Work Shop
Uppula Purushotham

## Slide 2
Background of Present Research
Recent theoretical studies revealed that electrolyte decomposition is strongly depend on the electrolyte-electrode interactions in presence of the electrode. [1-2]
Thus, to investigate the microscopic mechanism of the SEI film formation, it is essential and inevitable to consider explicitly the electrolyte-electrode interactions.
In the present study we have consider the graphene electrode effect on the reductive decomposition of propylene carbonate (PC).
In addition, effect of solvation and sodium ion concentration on the PC decomposition has been addressed by using sophisticated computational methods.
1. Ma, Y.; Balbuena, P. B. J. Electrochem. Soc. 2014, 161, E3097.
2. Martinez de la Hoz, J. M.; Leung, K.; and Balbuena, P. B. ACS Appl. Mater. Interfaces, 2013, 5, 13457.
Fig. Reduction mechanisms of ethylene carbonate on Si anodes of lithium-ion batteries
Slide from previous presentation

## Slide 3
Computational Details
Slide from previous presentation
Method | ILS
B3LYP-D3/6-31G(d) | 3.308
B3LYP/6-31G(d) | 3.712
M06-2X/6-31G(d) | 3.245
HF/6-31G(d) | 3.957
Fig. Optimized geometry of graphene dimer at B3LYP-D3/6-31G(d) level of theory.
3.308
C84H36 Point Group: C2h
Experimental Inter Layer Spacing ̴ 3.353 (±0.04) Å1
B3LYP-D3/6-31G(d) method provides reasonable Inter Layer Spacing than other methods.
All geometry optimizations and frequency analysis in this study was carried using above method.
1Y. Baskin et al., Phys. Rev. 1955, 100, 544.
Table: Inter Layer Spacing (ILS in Å) of the 3X3 graphene dimer model system at various level of theories

## Slide 4
Graphene: G
Propylene carbonate: PC
Sodium: Na
GPCNa
GPCNa2
GPC2Na
Nomenclature
PC decomposition on GPC surface and solvent effect using GPC2Na model system was discussed in the previous presentations. In this presentation I will discuss the effect of Na concentration with using GPCNa2 model system.
5

## Slide 5
1
2
3
4
5
6
7
Figure: Various possible adsorption positions for additional Na adsorption on GNa+ complex
Possible Na Adsorption Positions
To investigate the concentration effect of adsorbed Na on the graphene surface, we added additional Na to the GNa+ complex.
4

## Slide 6
Figure: the optimized geometries of various GNa2+ complexes along with relative energy in kcal/mol at B3LYP-D3/6-31G(d) level of theory.
GNa2-1 3.995
GNa2-2 4.708
GNa2-3 0.850
GNa2-4 7.433
GNa2-5 0.746
GNa2-6 1.178
GNa2-7 0.00
Geometries of GNa2+ Complexes
Based on the energetics and orientation, we have considered the GNa2-5 complex as a surface for the reductive decomposition of PC electrolyte.
6

## Slide 7
Figure: The optimized geometries of various GPCNa2+ complexes along with relative energy in kcal/mol at B3LYP-D3/6-31G(d) level of theory.
Geometries of Various GPCNa2+ Complexes
Presence of distinct non-covalent interactions between Na2PC and graphene dimer in GPCNa2-1 complex, increased the stability in comparison to other GPCNa2 complexes.
GPCNa2-3 10.153
GPCNa2-1 0.000
GPCNa2-2 5.078
7

## Slide 8
Figure: Optimized geometries of GPCNa2-1 complex after 1-electron (GPCNa2-1e) and 2-electron (GPCNa2-2e) reduction with relative energy in kcal/mol at B3LYP-D3/6-31G(d) level of theory.
One and Two Electron Reduction Products
Similar to GPCNa, GPC2Na complexes, the one and two electron transfer in GPCNa2 complex also highly exothermic.
The negative reaction energies suggests that electron transfer to PC on the graphene surface is thermodynamically favorable.
GPCNa2-2e -153.846
GPCNa2-1 0.000
GPCNa2-1e -103.166
8

## Slide 9
C4-O3 Bond Cleavage Products
Activation energy barrier of C4-O3 bond cleavage in GPCNa (22.740 kcal/mol) and GPCNa2 (28.631 kcal/mol) complexes are comparable.
However, the product formed in GPCNa2 complex is thermodynamically stable with lower energy (-19.823 kcal/mol) than the product of GPCNa complex (13.211 kcal/mol).
C4-O3
GPCNa2-1e 0.000
GPCNa2-1e-TS1 28.631
GPCNa2-1e-IN1 -19.823
Fig. Calculated transition state (GPCNa2-1e-TS1) and product (GPCNa2-1e-IN1) of PC C4-O3 bond cleavage after one electron reduction in GPCNa2 complex and their relative free energies (RE) at B3LYP-D3/6-31G(d) level of theory.
9

## Slide 10
In GPCNa2 complex, C4-O3 bond cleavage is favorable (28.631 kcal/mol) than C5-O1 bond cleavage (32.569 kcal/mol).
C5-O1
GPCNa2-1e 0.000
GPCNa2-1e-TS2 32.569
GPCNa2-1e-IN2 -18.216
Fig. Calculated transition state (GPCNa2-1e-TS2) and product (GPCNa2-1e-IN2) of PC C4-O3 bond cleavage after one electron reduction in GPCNa2 complex and their relative free energies (RE) at B3LYP-D3/6-31G(d) level of theory.
C5-O1 Bond Cleavage Products
10

## Slide 11
PC Decomposition After One Electron Reduction
GPCNa | GPCNa2 | GPC2Na
Activation barrier energy (in kcal/mol) |  | 
22.740 | 28.631 | 21.407
Reaction energy (in kcal/mol) |  | 
13.211 | -19.823 | 7.080
Table: Activation energy barrier and reaction energy of product after one electron reduction through C4-O3 bond cleavage in gas phase at B3LYP-D3/6-31G(d) level of theory.
The PC decomposition reaction through C4-O3 bond cleavage after one electron reduction is thermodynamically favorable at higher sodium concentration.
In real situation at lower electrode potential the Na concentration is high thus, this results shows that at lower electrode potential PC decomposition is thermodynamically favorable.
11

## Slide 12
Conclusions
In the present study I have investigated the effect of concentration of adsorbed Na on the reductive decomposition of propylene carbonate.
Similar to GPCNa, GPC2Na complexes, the one and two electron transfer in GPCNa2 complex also highly exothermic.
In GPCNa2 complex, C4-O3 bond cleavage is favorable with lower activation barrier (28.631 kcal/mol) than C5-O1 bond cleavage (32.569 kcal/mol).
The PC decomposition reaction after one electron reduction through C4-O3 bond cleavage is favorable at lower electrode potentials.
12