## Slide 1: Mechanistic study of Propylene Polymerization Catalyzed by Kaminsky Complex
Sandhya. K. S
28/7/14

## Slide 2: Outline
Introduction to polymerization
Polymerization reaction of propylene using Kaminsky catalyst.
Results and discussion
Future work
Summary

## Slide 3: Introduction to polymerization reaction
What is polymer
What is monomer
Various type of polymer preparation
Radical chain growth polymerization
Anionic chain growth polymerization
Cationic chain growth polymerization
Organometallic polymerization
Isotactic
Syndiotactic
Atactic
R= alkyl or any group
Kaminsky catalysts
Ziegler-Natta catalysts

## Slide 4: Four mechanistic proposal
Chemical Reviews, 2000, 100, 1260
Four plaussible mechanism of polymerization

## Slide 5: Present work of polymerization reaction of propylene by Kaminsky catalyst
First step

## Slide 6: Benchmark studies for the first insertion of propylene
E(B3LYP-3D) = 10.56 kcal/mol
 E(B3LYP-2D) = 10.29 kcal/mol
 E(B3LYP) = 11.23 kcal/mol
 E(M06L) = 10.55 kcal/mol
 E(M06) = 8.46 kcal/mol
 E(TPSSTPSS) =6.91 kcal/mol
 E(wB97XD) = 9.85 kcal/mol
 E(M052X) =8.90 kcal/mol
Activation barrier
23.51
24.69
14.43
22.78
20.82
14.42
23.96
21.00
Complexation energy/
binding energy (kcal/mol)
Basis set for Zr LanL2DZ, all other atoms 6-31++G(d,p)
Notes: Lose Alamose National laboratory 2 double zeta

## Slide 7: Real models
E = 8.38 kcal/mol
A type attack
TS

## Slide 8: Schematic representation of overall mechanism

## Slide 9: First insertion Reaction
P1A
P1C
P1B
P1D

## Slide 10: Energy profile for the first propylene insertion reaction
Chart: Reaction Coordinates
| 1 | 2 | 3
A type approach | 0 | 10.5675 | -2.7251
B | 0 | 13.9305 | -3.3578
C | 0 | 10.7515 | -2.6031
D | 0 | 19.94 | 4.5349
Chart: Reaction Coordinates
| 1 | 2 | 3
A type approach | 0 | 8.4608 | -5.8646
B | 0 | 13.1598 | -3.4683
C | 0 | 8.3603 | -5.4203
D | 0 | 18.586 | 1.0448
Chart: Reaction Coordinates
| 1 | 2 | 3
A type approach | 0 | 9.8562 | -6.1046
B | 0 | 13.6004 | -4.1156
C | 0 | 9.8631 | -5.7991
D | 0 | 19.4964 | 0.42888
TS1
TS1
TS1
B3LYP-3D

## Slide 11: Second Insertion Reaction  Two possibilities
P2AA
P2AC
P2AB
P2AD
P2BA
P2BC
P2BB
P2BD

## Slide 12: Different possibilities for the agostic interaction

## Slide 13: Energy profile for the second propylene insertion reaction from P1A products

## Slide 14: Energy profile for the second propylene insertion reaction from P1B products

## Slide 15: Overall energy profile starting from A/C attack of propylene
Chart: Reaction coordinates
| cation complex | c-pi complex | TS1 | P1 | R2 | TS2 | P2
 | 0 | -20.8248 | -12.6395 | -26.6894 | -39.7844 | -37.5693 | -51.8976
Chart: Reaction coordinates
| cation complex | c-pi complex | TS1 | P1 | R2 | TS2 | P2
 | 0 | -20.8248 | -12.6395 | -26.4201 | -35.6677 | -33.3107 | -50.8415
Isotactic polymerization
(A approach)
Syndiotactic polymerization
(C approach)

## Slide 16: Overall energy profile starting from A/C attack of propylene
Chart: Reaction coordinates
| cation complex | c-pi complex | TS1 | P1 | TSrotn | Protn | R2 | TS2 | P2
 | 0 | -20.8248 | -12.6395 | -26.6894 | -23.6984 | -29.2999 | -41.9546 | -31.6162 | -51.4041
Chart: Reaction coordinates
| cation complex | c-pi complex | TS1 | P1 | TSrotn | Protn | R2 | TS2 | P2
 | 0 | -20.8248 | -12.6395 | -26.6894 | -23.6984 | -29.2999 | -42.2817 | -25.3996 | -48.7355
Atactic polymerization
(D approach)
Atactic polymerization
(B approach)
∆E=10.3
∆E=16.4

## Slide 17: Optimized transition state of second insertion (Isotactic)
OPTIMIZED PRODUCT AFTER
SECOND INSERTION

## Slide 18: Overall energy profile starting from B/D attack of propylene
Isotactic polymerization
(D approach)
Syndiotactic polymerization
(B approach)
Chart: Coordinates
| Intl | R1 | TS1 | P1 | R1 | TS2 | P2
Isotatic | 0 | -20.0494 | -6.8896 | -23.5177 | -31.234 | -17.7375 | -42.9765
Chart: Coordinates
| Intl | R1 | TS1 | P1 | Tsal | Pb | Tsbet | R1 | TS2 | P2
 | 0 | -20.0494 | -6.8896 | -23.5177 | -20.5295 | -26.4201 | -8.6813 | -29.5173 | -25.9717 | -47.6878
∆E=13.49kcal/ml
∆E=17.73kcal/ml

## Slide 19: Overall energy profile starting from B/D attack of propylene
Chart: Coordinates
| Intl | R1 | TS1 | P1 | Tsal | Pb | Tsbet | R1 | TS2 | P2
 | 0 | -20.0494 | -6.8896 | -23.5177 | -20.5295 | -26.4201 | -8.6813 | -32.9053 | -31.9374 | -52.5128
Chart: Coordinates
| Intl | R1 | TS1 | P1 | Tsal | Pb | Tsbet | R1 | TS2 | P2
 | 0 | -20.0494 | -6.8896 | -23.5177 | -20.5295 | -26.4201 | -8.6813 | -32.9053 | -31.9374 | -52.5128
Atactic polymerization ( A and B approach)

## Slide 20: Present work
Counter anion effect
B(C6F5)3CH3-
Work plan for the next four month
MC/MD simulation to study the polymerization reaction
for the whole process.

## Slide 21: Summary
Propylene polymerization using Kaminsky catalyst has been studied by M06/6-31++ G(d,p).
Different orientation of propylene considered at first insertion as well as second insertion.
In the first insertion, two different products of pairs are formed.
In the second insertion starting from the A/C products, A type approach of propylene results in the isotactic products while the C approach leads to the syndiotactic products.
In the second insertion from B/D products, D style approach of propylene leads to isotactic polymer whereas B style approach gives syndiotactic polymer.
Remaining products are atactic polymers.
The process are extended in the presence of counter anions, B(C6F5)3CH3-.
For the large polymer can be studied with help of molecular dynamics in order to study the whole process.

## Slide 22
Thank you