## Slide 1
FY2015’s 1th, CREST Workshop
Norio Takenaka1,2
Graduate School of Information Science, Nagoya University1,
Elements Strategy Initiative for Catalysts and Batteries (ESICB), Kyoto University2
Hybrid MC/MD Reaction Simulation with Constant Potential Method
Fri. Apr. 17th

## Slide 2
Elements Strategy Initiative for Catalysts and Batteries: Interplay Between Experimental and Theoretical Studies
MEXT program
Primary object is
・ To develop rare metals-free high performance catalysts and batteries
・ To understand the principle of material science
As one of specific targets,
we develop the rare metals-free secondary battery.
Li-ion battery
Na-ion battery
(Li = rare metal)
(Na = common metal)
2

## Slide 3: Background of present research①
Solid Electrolyte Interphase (SEI) Film
・During the initial charging cycles, the reductive reaction products of the electrolyte form a solid electrolyte interphase (SEI) film on the anode surface.
SEI Film
Inorganic Salts
(e.g. Na2CO3)
Organic Salts
(e.g. ROCO2Na)
Na+
Solvent
Block
Exchange
・The ideal SEI film can protect the electrolyte from the further reduction while maintaining Na+ exchange. Therefore, it is closely related to the lifetime of battery.
Na-ion battery
Reduction of electrolyte
S. Komaba et al., Adv. Funct. Mater, 21, 3859 (2011).

## Slide 4: Background of present research②
Hybrid MC/MD reaction simulation
[1] M. Nagaoka, Y. Suzuki, T. Okamoto, NT, Chem. Phys. Lett., 583, 80 (2013).
[2] NT, Y. Suzuki, H. Sakai, M. Nagaoka, J. Phys. Chem. C, 118, 10874 (2014).
e-
Hybrid MC/MD
reaction simulation
Initial state
Final state
・ In the previous simulations, we have investigated the SEI film formation on the carbon anode surface with the hybrid Monte Calro (MC)/molecular dynamics (MD) reaction method [1,2].
・ In these simulations, the atomic charges on the anode surface was constant. However, in the real cell, such electrode charges can change according to the SEI film formation at the given voltage.

## Slide 5: Purpose of this study
・ To improve the calculation accuracy of the previous SEI film formation simulations, I aim to realize the hybrid MC/MD reaction simulation under the constant electric voltage.
・ For this purpose, three methods have implemented into the AMBER program.
① Ewald summation method for the two dimensional system [3]
② Constant electric potential method [4]
③ Cation (Li+ or Na+) insertion method into the electrolyte
[3] A. Bródka, A. Grzybowski, J. Chem. Phys., 117, 8208 (2002).
[4] M. K. Petersen, R. Kumar, H. S. White, G. A. Voth, J. Phys. Chem. C, 116, 4903 (2012).

## Slide 6: EW method for 2D system
・ In the EW3DC method, the empty region is introduced along the non-periodic direction. Next, the correction term is added to the EW3D method.
Vc: volume of the system
z: real space coordinate along the non-periodic direction
MD simulation box
Empty (or vacuum) region
z axis considering non-periodic
→ The EW3DC method improves the electrostatic potential and electric field in 2D system.
・ In the two-dimensional (2D) system, the conventional three-dimensional (3D) Ewald summation method (EW3D) cannot be used. To improve the calculation accuracy, the use of EW3DC method [3] is very efficient.
Electrostatic potential
Electric field
[3] A. Bródka, A. Grzybowski, J. Chem. Phys., 117, 8208 (2002).

## Slide 7: Constant electric potential method
[4] M. K. Petersen, R. Kumar, H. S. White, G. A. Voth, J. Phys. Chem. C, 116, 4903 (2012).
Cathode
Anode
electrolyte
・ In this method, considering the electrochemical cell composed of two parallel
electrodes and electrolyte, the induced charges on the electrodes are obtained:
qLE
qRE
Distance: D
A: surface area of electrode
ΔV: electric potential difference between anode and cathode
z axis considering non-periodic
・ There are some methods to apply the constant voltage for the MD simulations.
Among them, the fastest method [4] is employed in the present study.

## Slide 8: Cation insertion method into electrolyte
・ In the SEI film formation simulations, the same number of cations as that of injected electrons was additionally placed in the electrolyte to neutralize the whole system whenever the electrolyte molecules are reduced on the anode surface.
e-
Li+ (or Na+)
Half-cell system
(Previous)
(b) Full-cell system
(Present)
anode
e-
anode
Li+ (or Na+)
・ In contrast to the previous half-cell system, there is no empty region in the system to add cation. Therefore, such cation should be directly inserted by increasing gradually the interactions between the inserted cation and others.

## Slide 9: Calculation model
y
z
x
164.2 Å
PF6-
Li+
EC: 1700
Li+: 134
PF6-: 134
EC
Graphite
Graphite
1.1 M LiPF6 EC-based electrolyte
Cathode
Anode
Temperature: 298 K
Voltage: 0 V or 4 V
The origin of z coordinate （z = 0) is taken at the cathode surface.

## Slide 10: Elementary chemical reaction processes
+ e-, + Li+
+
+ LiEC
Li2CO3
EC
LiEC
C2H4
radical polymerization
(CH2CH2OCO2Li)2, Li2BDC
(dilithium butylene dicarbonate)
+ e-, + Li+
+
3 ×
PF6-
PF3
+ 2e-, + 3Li+
(EC)
(PF6-)
In the present hybrid MC/MD reaction simulations, I employed the same elementary chemical reaction processes as the previous ones [2].
[2] N. Takenaka, Y. Suzuki, Y. Sakai, M. Nagaoka, J. Phys. Chem. C, 118, 10874 (2014).

## Slide 11: Snapshots of hybrid MC/MD reaction simulation
Reaction product
Li2BDC
LiEC
Li2CO3
C2H4
LiF
PF3
(b) 4 V
Initial State (0 MC/MD cycle)
(a) 0 V
anode
cathode
anode
cathode

## Slide 12: Snapshots of hybrid MC/MD reaction simulation
100 MC/MD cycle
(b) 4 V
(a) 0 V
Reaction product
Li2BDC
LiEC
Li2CO3
C2H4
LiF
PF3
anode
cathode
anode
cathode

## Slide 13: Changes in the electrode charges
MC/MD Cycle
Charge [e]
The electrode charges frequently changed depending on the reduction reactions so as to keep the voltage.
The electrode charges at 4 V (~±7.4 e) were larger than those at 0 V (±0.4 e). At 4 V, such large negative charge on the anode surface should enhance the dissolution of the reaction products.
Relaxation time: 4 ps
Chart: 
| 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
 | 0.90053 | 0.1204 | 0.89157 | 0.22962 | 0.67283 | 0.38605 | -0.050296 | 0.35459 | 0.4204 | 0.35815 | 0.40693
 | -0.91885 | -0.13858 | -0.90961 | -0.24764 | -0.69085 | -0.40405 | 0.032256 | -0.37261 | -0.4383 | -0.37599 | -0.42475
 | 7.5813 | 7.3454 | 7.1006 | 7.1244 | 7.3259 | 8.1471 | 8.1795 | 7.1372 | 6.8745 | 7.1404 | 7.6982
 | -7.5996 | -7.3635 | -7.1186 | -7.1423 | -7.3438 | -8.1648 | -8.1972 | -7.1548 | -6.8913 | -7.1571 | -7.7146
Cathode (0 V)
Anode (0 V)
Cathode (4 V)
Anode (4 V)
4 V
4 V
0 V
0 V

## Slide 14
Conclusion and future work
To realize the hybrid MC/MD reaction simulation at the given voltage, three methods have implemented to AMBER program.
In future, by executing long-time MC/MD simulations, I will investigate the dependency of the SEI film formation on the voltage value.
During the present simulations, the electrode charges frequently changed so as to reproduce the set electric voltage in contrast to the previous simulation.
By using the present program, we can simulate the complex chemical reaction processes on the anode surface under the constant electric potential.
At the high voltage (4 V), the dissolution of the reaction products should be enhanced due to the strong electrostatic repulsions.

## Slide 15: Thank you for your attention