## Slide 1: Application of hybrid MC/MD reaction method to the study of CALB catalyzed ring-opening polymerization of β -lactam
Chantal Barberot, Ikuo Kurisaki, Yuichi Suzuki, Masataka Nagaoka
Graduate School of Information Science,Nagoya University

## Slide 2: Enzymatic polymerization
Increased interest in the area of in vitro enzyme-catalyzed organic reaction
Many families of enzyme can be used for transforming not only their natural substrates but a wide range of unnatural compounds
Using enzymes in organic synthesis have several advantages
  High catalytic activity
  Mild reaction conditions (solvent, temperature, pressure, pH)
  Regio, stereo and enantio-selectivity
  Non-toxic natural catalyst
In living system, polymers can be produced by enzymatic catalysis
Synthesis of polymers with enzymatic catalysis have more and more study
  Production of biodegradable and biocompatible materials
  Application in medicine, packaging industry
Lipase enzymes are widely used for enzymatic polymerization

## Slide 3: Enzymatic polymerization
In living system, lipase hydrolyze triglycerides into fatty acids and glycerol
In organic media, lipase can catalyze the reverse reaction (esterification)
The most commonly biocatalyst used in enzymatic polymerization is Candida Antartica Lipase B (CALB) come from yeast
  High stability at elevated temperature
  Good activity in organic solvent
  Accept various substrate
polyester
polyamide

## Slide 4: Example of CALB catalyzed polymerization
Ring-opening polymerization of β-Lactam
  Reaction yield = 37%
  Maximum degree of polymerization (DP) = 40 monomeric units
  Average DP = 12 monomeric units
Ring-opening polymerization of ε-caprolactone (ε-CL)
  Reaction yield = 65%
  DPmax = 78 monomeric units
  Average DP = 29 monomeric units
K. Loos et al. Biomacromolecules 2014 15, 234-241
→ polymer size and the reaction yield dependent of the nature of starting material

## Slide 5: Example of CALB catalyzed polymerization
Ring-opening copolymerization of ε-CL and β-Lactam
  Different feed ratios of ε-CL/β-lactam tested: 75:25, 50:50 and 25:75
  DPmax = 12
  9 different structures of poly(ε-CL-co-β-lactam) was observed with a ratio of 50:50 ε-CL/β-lactam
A better understanding of the polymerization process can allow to regulate the copolymer structure (molecular weight, nature)
K. Loos et al. Biomacromolecules 2014, 15, 234-241
Feed ratio |  | Conversion |  | 
ε-CL | β-Lactam | ε-CL | β-Lactam | Yield
0 | 100 |  |  | 37
25 | 75 | 72 | 57 | 12
50 | 50 | 73 | 90 | 50
75 | 25 | 78 | 95 | 44
100 | 0 |  |  | 65

## Slide 6: Target goal
For the polymerization process, some mechanism were already proposed
  Some mechanism based on experimental observations was given
  A theoretical mechanism of β-Lactam polymerization catalyzed by CALB was proposed1
    They only model the polymerization process until the formation of the dimer
    This mechanism do not explain the rate-determining step of the polymerization reaction
Simulation of the whole polymerization process seems to be important to clarify the CALB catalyzed copolymerization mechanism
We propose to simulate the CALB catalyzed copolymerization process by using the hybrid MC/MD reaction method2
First, we will study the CALB-catalyzed polymerization of β-Lactam and ε-Caprolactone process individually
1G. Felds et al. ACS Catal. 2011, 1, 323-336
2M. Nagaoka et al. Chem. Phys. Letters 2013, 583, 80-86

## Slide 7: Hybrid MC/MD Reaction Simulation
Mechanism proposed for the hybrid MC/MD reaction process
G. Felds et al. ACS Catal. 2011, 1, 323-336
initiation
propagation
Active site
- two bond breaking
- two bond formation

## Slide 8: Adaptation of hybrid MC/MD Reaction simulation
Run MD simulation until satisfying necessary conditions
Virtually react and relax the whole system
Accept or reject the reaction under the Metropolis scheme
lactam
acylated serine
Thr40
Gln106
dimer
Ser105
OG
Thr40
Gln106
oxyanion hole

## Slide 9: Simulation of the first polymerization process steps
Model system
  Acylated Serine
  One β–lactam in the active site
  In a water box (Size box: 67*86*74 Å)
  Force field: ff99SB and GAFF, RESP charge procedure
  Periodic boundary condition
100 ps of heating up to the desired temperature (300 K) with a Langevin thermostat
1 ns of NPT-MD equilibration under a pressure of 1 bar and temperature of 300 K
NVT-MD time is 10 ps with a temperature of 300 K for each MC/MD cycle
SHAKE method used to constrain the bond involving hydrogen atom
Acylated Serine
His224
Β-lactam
Thr40

## Slide 10: Simulation of the first polymerization process steps
Lactam opening
Polymerization
Formation of acylated complexe
Acylated Serine
His224
Β-lactam
Thr40
Acylated Serine
His224
Thr40
Open latam
His224
Thr40
Dimer
Ser105
Acylated Serine
His224
Thr40

## Slide 11: Next implementation in the hybrid MC/MD reaction method
To realize the next step of polymerization process, another lactam molecule should approach and bind to the active site
Spontaneous lactam binding to the active site is time consuming with a standard MD simulation
Add a docking procedure to force the lactam to be bound to the active site

## Slide 12: Conclusion
Modelisation of the first steps of the CALB catalyzed polymerization by the hybrid MC/MD approach shows that this method can be used to study enzymatic catalysis
After having successfully completes each step of the polymerization process, we will modelize the CALB-catalyzed polymerization of β-Lactam by varying the reaction condition (temperature, solvent)
Being able to use the hybrid MC/MD method for this complex reaction would allow us to extent its scope of study to other complex system

## Slide 13: Thank you for your attention